Post Synthesis Treatment of CsPbBr3 Nanocrystals to Suppress Surface Traps and Non-Radiative Recombination Rates

Ranadeep Raj Sumukam and Banavoth Murali*

Solar Cells and Photonics Research Laboratory, School of Chemistry, University of Hyderabad, Prof. C R Rao Road, Hyderabad -500046, Telangana State, India.

*Email: murali.banavoth@uohyd.ac.in

Abstract

Perovskite nanocrystals have very high surface to volume ratio so the surface chemistry of the nanocrystals plays a vital role in determining the photophysical and electronic properties of the material to be utilized in the optoelectronic and photovoltaic devices. However, there is a major challenge, even in good quality perovskites nanocrystals, is the presence of surface defects due to halide vacancies and open surface sights caused by the weakly bonded conventional surface ligands. These defects trap the excited carriers and hinder the radiative recombination process which impends the overall performance of the material. Therefore, finding a simple strategy and molecules to reduce the surface defect is the need of the hour. Here in this work, we have chosen well explored post synthesis treatment to tackle this issue with a range of different types of salts as the post synthesis treatment agents and validated performance of each with proper insights and their impact on the carrier dynamics of the CsPbBr3 nanocrystals. The treated CsPbBr3 nanocrystals have exhibited dramatic increase in the PLQY and reduced non- radiative recombination rate constant without impacting the intrinsic structure of the parent CsPbBr3 nanocrystal.

Introduction

Metal halide perovskites have emerged as a highly prominent class of materials, garnering significant attention due to their intrinsic properties, such as suitable narrow direct bandgap, high extinction coeﬃcient, colour purity, low Urbach energy, small Stokes shift, long charge-carrier diﬀusion lengths, high charge carrier mobility, high photoluminescence quantum yield (PLQY), and solution processability, conferring perovskites a colossal potential in the field of photovoltaics and optoelectronics. Though the perovskites have captivated the photovoltaics research evident by sky rocketed efficiencies comparable to polycrystalline silicon solar cell in short period,1, 2 after the initial reports on colloidal Lead Halide Perovskite Nanocrystals (LHPe NCs) as highly luminescent material in the year 2014 by Galian and Pérez-Prieto through a ligand assisted reprecipitation technique led to exponential growth in the publications on LHPe NCs as an active material for Light Emitting Diodes (LEDs).3-6 Colloidal nanocrystals are also known as Quantum dots, composed of hundreds to thousands of atoms with a size in the range of 2-20 nm.7, 8 They are stabilized by the long-chain surface ligands, which prevent nanocrystals from aggregation and also protect nanocrystals from the ambient environment. Owing to their size and the surface passivation by the ligands, colloidal nanocrystals exhibit quantum and dielectric confinement effects, which increase the bandgap and exciton binding energy, respectively. These features, along with the intrinsic compositional dependent bandgap tuning, help in tailoring the optical and electronic properties of the nanocrystals led to their breakthroughs in the realm of optoelectronic and photovoltaic devices.8 Currently, LHPe NCs-based LEDS have demonstrated the external quantum efficiencies (EQEs) of more than 20 % in both red and green LEDs.9-11  On the other hand, LHPe NC-based solar cell devices have outperformed the conventional PbS solar cells, manifesting LHPe NC’s capability to be the material of next generation quantum dots based solar cells.12-17 Furthermore,  recently LHPe NCs have also been utilized for the fabrication of lasers, phototransistors, photodetectors, and luminescent solar concentrators.18-21 Among LHPe NCs, all-inorganic LHPe NCs, particularly CsPbX3 (where X represents Cl, Br, or I), have been a significant focus of research owing to their inherent defect tolerance (resistance to forming deep state defects) and stability in comparison to other counterparts.22, 23

Despite these remarkable properties and significant achievements, several challenges and research gaps impede their widespread practical application and commercialization. LHPe NCs are highly susceptible to developing surface defects, which are inevitable during their synthesis and purification processes, as LHPe NCs are ionic (not covalent like classical semiconductors), so the majority of the ligands bind electrostatically and are prone to getting detached.24-26 These surface defects often act as non-radiative recombination centres and significantly lower their Photoluminescence Quantum Yield (PLQY) and would cause aggregation of the nanocrystals, which eventually results in loss of structural integrity.27, 28 In contrary, the presence of excessive long-chain organic ligands at the nanocrystal surface, which are required for size control and colloidal stability, is detrimental to the effective carrier transport in LHPe NCs-based devices as they are insulating in nature.29, 30  Therefore, trade-off between colloidal stability and charge carrier mobility is pivotal to get an optimized film for the real time usage.

Considering the high surface-to-volume ratio in the NCs, these insights depict the key role of surface engineering in determining their optical and electronic properties. Therefore, to address the associated challenges related to surface defects and halide vacancies that contribute to non-radiative recombination centres, various strategies have been explored, such as modifying synthesis and purification protocols, strategic ligand engineering, metal doping, and encapsulating the nanocrystals within stable matrices.31-34  In general, surface terminations of LHPe NCs are A-site cations or lead halide octahedral units, depending on their synthesis, purification, and post-synthesis treatment.24, 35 Among all the approaches, post-synthesis treatments are designed particularly to modify these terminations. Herein, weakly bound long-chain ligands will be replaced by the strongly binding short-chain ligands, which bestow better stability and charge transport. In addition, passivation of the surface halide vacant sites with the same or other halides or pseudohalides will enhance the performance by reducing the number of trap states that are the root cause of non-radiative recombination process and ion migration.36, 37 Therefore, herein we have focused on the facile post-synthesis surface treatment method leveraging a wide range of small molecules.

Figure 1: a) Synthesis procedure of the CsPbBr3 Nanocrystals, b) Synthesis procedure of Cesium Oleate, and c) UV-Vis absorption and PL emission of the as-synthesized CsPbBr3 Nanocrystals.

Results and Discussion

In this work, we have chosen CsPbBr3 NCs to perform post-synthesis treatments and investigate the photophysical properties. CsPbBr3 NCs were synthesized using the standard hot injection synthesis procedure (Experimental section) as shown in Figure 1(a and b) proposed by Protesescu et al., where LHPe NCs adopt cuboidal morphology with the (001) and (110) facets as surface terminations.4 Then the crude nanocrystals were washed using anhydrous toluene and stored in anhydrous toluene. Before going ahead for post synthesis surface treatment, we performed optical and structural measurements on the as-synthesised CsPbBr3 NCs. As shown in Figure 1c the absorption spectrum is broad with max at 507 nm, and the PL emission peak is at 518 nm with a full width half maximum (FWHM) of 20.53 nm, and the photoluminescence quantum yield (PLQY) of the spin-coated NC film is ~65%. From the TEM images of the pristine CsPbBr3 NCs shown in Figure 2 and narrow FWHM emission, we confirmed that the as-synthesised CsPbBr3 NCs have a narrow size distribution and are cubic with ~ 12-17 nm edge size.

Figure 2. TEM images showing a narrow size distribution of the pristine CsPbBr3 NCs

Thereafter, the dispersed purified NCs were utilized to perform surface treatment by stirring them with various passivating agents that include alkali thiocyanates (Guanidinium Thiocyanate:GuSCN, KSCN, NH4SCN), metal chloride (YCl3), bulky diammonium (1,4-Phenylenediammonium Dibromide:PDABr2), and quaternary ammonium bromide (Choline Bromide:CB), in different concentrations (0.25, 0.5, 0.75, 1.0, 1.25, 1.5, 1.75, 2.0, 2.25 millimoles) individually, for 30 minutes at ambient conditions. It is worth mentioning that we have observed significant changes in the nanocrystals' properties in the initial 10-15 minutes.

Figure 3. Comparison of photoluminescence spectra of surface-treated CsPbBr3 with respect to the concentrations of (a) YCl3, (b) PDABr2, (c) Choline bromide, (d) GuSCN, (e) NH4SCN, and (f) KSCN.

On post-synthesis treatment with different passivating salts, we observed a dramatic impact on the PL emissions of the treated NCs based on the passivating agent utilized, which could demonstrate that surface modifications happened to the CsPbBr3 NCs. Among all the molecules listed above, addition of some particular amounts of YCl3, PDABr2, GuSCN, and NH4SCN have significantly enhanced the emission intensities as a result of efficient vacant site passivation on the NCs surface, as shown in Figure 3. It is worth mentioning that, we have observed hypsochromic peak position shift in the case of YCl3. The peak shift in YCl3:CsPbBr3 NCs attributes to the replace of Bromide ions or filling halide vacancies by Chloride ions on the CsPbBr3 NCs surface. In general, it is an intrinsic character of perovskites, based on the molecular orbitals, halide’s p atomic level determines the valence band maximum (ionization energy) and the atomic level p of Pb determines the conduction band minimum (electron affinity).38 Therefore change in the electronegativity of halides has a direct impact on the bandgap of the NCs. On the other side we have observed drop in the PL emissions of CsPbBr3 NCs on treating with KSCN and Choline Bromide, which clearly represents that both cation and anion of the salt play a crucial role in deciding the final properties of the NCs. We have provided summarised results for each post synthesis treatment performed in the Table 1 and molecular structurers of all the compounds used for post treatment is shown in the Figure 4a.

Table 1: Summarized results of the post synthesis treatments

| S. No | Treatment Agent | Result | Reason for Outcome |
| --- | --- | --- | --- |
| 1 | Pristine (Reference) | Moderate Luminescence | The as-synthesized CsPbBr3 NCs have a high density of surface defects (halide vacancies, undercoordinated Pb²⁺), leading to significant non-radiative recombination. |
| 2 | 1,4-Phenylenediammonium Dibromide (PDABr₂) | Improved Luminescence | The bulky, rigid diammonium ligand provides extensive surface coverage. PDABr₂ forms Dion-Jacobson 2D perovskite layer which passivates the surface. 2D feature is confirmed from P-XRD data where a peak is observed at 4° as shown in supporting information (Figure S1). |
| 3 | Guanidinium Thiocyanate (GuSCN) | Improved Luminescence | The thiocyanate (SCN⁻) ion strongly binds to Pb²⁺ defects and the Guanidinium (Gu⁺) cation passivates the bromide-rich surface. This dual-action passivation drastically reduces the suface trap states. |
| 4 | Yttrium Chloride (YCl₃) | Improved Luminescence | The Cl⁻ ions can fill Br⁻ vacancies, and Y³⁺ ions can passivate the surface to some extent. |
| 5 | Ammonium Thiocyanate (NH₄SCN) | Improved Luminescence | The SCN⁻ provides good passivation, and the NH₄⁺ cation is a moderately effective surface stabilizer. It provides a net improvement over the pristine sample. |
| 6 | Choline Bromide (CB) | Quenched Luminescence | The choline cation is ineffective at passivating the surface and likely displaces the native, more effective capping ligands. This leads to further increase in surface defects, causing a drop in PL. |
| 7 | Potassium Thiocyanate (KSCN) | Quenched Luminescence | While SCN⁻ is a good passivator, the small, inorganic K⁺ ion might have disrupted the native ligand layer or crystal lattice and led to increase in defect states. |

As shown in the Figure 3 PL emission spectra, the photoluminescence enhancement is in trend with the concentration of the passivating agents till a particular point; thereafter, with further increase in the concentration of passivating agents resulted in deterioration of photoluminescence emission. The implication for the change in emission intensity with respect to concentrations of passivating compounds is; initially, all the surface halide vacancies and ligand vacancies present on the surface of NCs get passivated; thereafter, the further increase in concentration of the passivating agents causes etching of NC’s surface forming the trap sites by stripping away the original essential ligands.

Figure 3. (a) Structures of the molecules used for the post treatment of the CsPbBr3 NCs, (b) Time-resolved PL of all samples. All samples refer to pristine CsPbBr3 and four post synthesis treated CsPbBr3 NCs as marked in the panel, (c) Powder XRD spectra of the CsPbBr3 NCs thin films on glass.

Considering only the cases where PL emission intensities are improved, we have investigated the impact of the post-synthesis treatment on the PL decay profiles of treated NCs  PDABr₂:CsPbBr3, GuSCN:CsPbBr3, YCl₃:CsPbBr3, and NH₄SCN:CsPbBr3 in comparison to the pristine CsPbBr3 NCs. We have performed these studies leveraging Time Correlated Single Photon Count (TCSPC), one of the methods of Time Resolved Photoluminescence (TRPL), to get the insights into the level of defect passivation achieved and materials quality that promoted the PLQY of the NCs. The PL decay curves of pristine CsPbBr3 and post synthesis treated CsPbBr3 NCs are shown in the Figure 4b. The TRPL decay curves were fitted using a bi-exponential decay model where Equation 1 describes the shape of the decay and Equation 2 used for the calculation of the intensity-averaged lifetime (τavg).

I(t)=A1exp(−t/τ1)+A2exp(−t/τ2)+C   (1)

τavg​= (A1​τ12​+A2​τ22)/ (A1​τ1​+A2​τ2)  ​​(2)

Here, τ1 and τ2 are the short and long lifetime components with their respective amplitudes A1 and A2. We have observed that through post synthesis treatment τavg of the NCs has increased drastically from 5.73 ns for the pristine CsPbBr3 NCs to 13.32 ns for the best performed PDABr2 treated CsPbBr3 NCs, which clearly demonstrates that trap states are passivated effectively by the post synthesis treatment. To further gain the understanding of the recombination kinetics, we measure the PLQYs of all the samples on thin films where pristine CsPbBr3 NCs achieved ~65% and it is improved to ~94% for the best performed PDABr2 treated CsPbBr3 NCs. Thereafter, obtained TRPL and PLQY results are utilized to derive the radiative (kr​) and non-radiative (knr​) decay rates. The relation between these three can be explained by the Equations 3, 4, and 5. The τavg ​is inversely proportional to the sum of these rates, while the PLQY is the ratio of the radiative rate to the total decay.

τavg​=1/kr​+knr​   ​(3)

PLQY= kr​/kr​+knr​   ​​(4)

kr​= PLQY/τavg​ ​ (5)

knr​=1- PLQY/ τavg​  (6)

As shown in the Table 2, knr shows a clear dip in the post synthesis treated samples from 0.061 ns-1 for pristine CsPbBr3 to 0.004 ns-1 for the best performed PDABr2 treated CsPbBr3 NCs. On the other side, kr remained relatively constant or slightly reduced across all samples (0.074-0.113 ns⁻¹), which is expected as surface treatments should not significantly affect the intrinsic radiative process of the NC’s core. The slight reduction in kr for the treated samples attributes to the electronic interaction between the passivating ligands and the nanocrystal surface. Based on this outcome we can infer that the neutralizing surface defects effectively shut down the non-radiative recombination pathways and lead to simultaneous increase in both average lifetime (up to 13.36 ns) and PLQY (up to 94%). Moreover, it is worth mentioning that all the ligands utilized for the post-synthesis treatment are short-chain ligands, which would help in electronic coupling of the nanocrystals and improve the overall conductivity of the perovskite layer when the treated CsPbBr3 NCs are utilized in the devices.

Table 2: Consolidated data of TRPL, PLQY, radiative (kr) and non-radiative (knr) decay rates

| Sample | τ1 (ns) | A₁ (%) | τ2 (ns) | A₂ (%) | τavg (ns) | X² | PLQY | kr (ns⁻¹) | knr (ns⁻¹) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Pristine | 3.54 | 71.2 | 8.11 | 28.8 | 5.74 | 0.9989 | 65% | 0.113 | 0.061 |
| YCl₃-Treated | 3.82 | 60.8 | 9.65 | 39.2 | 7.43 | 0.9991 | 75% | 0.101 | 0.034 |
| NH₄SCN-Treated | 4.05 | 50.7 | 11.1 | 49.3 | 9.17 | 0.9994 | 84% | 0.092 | 0.017 |
| GuSCN-Treated | 4.26 | 41.5 | 12.78 | 58.5 | 11.15 | 0.9995 | 91% | 0.082 | 0.008 |
| PDABr₂-Treated | 4.51 | 30.9 | 14.6 | 69.1 | 13.36 | 0.9997 | 94% | 0.07 | 0.004 |

Finally, we performed structural characterization to check if any structural modifications have occurred while doing post synthesis treatment. Based on the TEM images we observed no changes are observed in the nanocrystals' morphology and size (Supporting information: Figure S2); moreover, there was no significant change observed in the lattice spacing of treated CsPbBr3 NCs with respect to that of pristine CsPbBr3 NCs. In support to the morphological studies, XRD patterns of the pristine and treated CsPbBr3 NCs are very similar, with no changes in the peak positions (Figure 4c). We observed a peak around 15.6° corresponding to the orthorhombic 3D perovskite phase for all the samples coated on the glass slide, and in the case of PDABr2 treated CsPbBr3 NCs an extra peak around 4° corresponding to the 2D phase of the perovskite is observed. Both of these studies confirm that there are no morphological and crystal structure (at NCs core level) changes have occurred because of the post-synthesis treatment using the above-mentioned surface passivating salts.

Conclusion:

The advancement of perovskite LEDs based on the NCs paves the way for the next generation flexible lighting technologies. However, significant non-radiative recombination channels and instability due to weakly bonded passivating ligands lead to the formation of surface trap states, which severely affect the performance of NC-based PeLEDs. Though various approaches have been investigated to enhance the performance of NC-based PeLEDs, a simple and faster technique is need of the hour.

In this work, we tried to minimize the surface halide vacancies and ligand vacancies via facile surface treatment using various passivating agents and compared the photoluminescence of the pristine CsPbBr3 NCs with the surface-treated CsPbBr3 NCs. Herein, we used PDABr2, GuSCN, YCl3, KSCN, Choline Bromide, and NH4SCN for the surface treatment of the NCs. Out of all salts, only PDABr2, GuSCN, YCl3, and NH4SCN in particular amounts have enhanced the performance with respect to pristine CsPbBr3 NCs, which confirms that both cation and anion of the salt used for the post synthesis treatment are crucial in deciding the final photophysical properties of the NCs. Moreover, emission peak shift was noticed in YCl3 treated CsPbBr3 NCs, which is attributed to the electronegativity difference between the Chloride against Bromide (native halide in CsPbBr3 NCs). To further study the carrier recombination dynamics, we have performed TRPL and PLQY studies which are aligned with the PL data obtained where post synthesis treatment has significantly reduced the surface trap states and improved overall emission of the NCs. As the ligands used are small molecules, they would also help in CsPbBr3 NCs coupling and conductivity of the perovskite layer in the device point of view. Finally, via TEM and P-XRD studies we have confirmed that even after post synthesis treatment CsPbBr3 NC’s morphology and structure are preserved. This study provided a facile way to minimize the surface defects in NCs which helps on realization of the stable and efficient CsPbBr3 NCs based devices.

References:

1.	Jiao, B.;  Tan, L.;  Ye, Y.;  Ren, N.;  Li, M.;  Li, H.;  Li, X.; Yi, C., One-stone-two-birds: over 26% efficiency in perovskite solar cells via synergistic crystallization & interface regulation. Energy & Environmental Science 2025, 18 (11), 5437-5447.

2.	Wang, D.;  Liu, Z.;  Qiao, Y.;  Jiang, Z.;  Zhu, P.;  Zeng, J.;  Peng, W.;  Lian, Q.;  Qu, G.;  Xu, Y.;  Zhang, Y.;  Li, F.;  Yan, L.;  Wang, X.;  Wang, Y.-G.;  Jen, A. K. Y.; Xu, B., Rigid molecules anchoring on NiO<sub>x</sub> enable &gt;26% efficiency perovskite solar cells. Joule 2025, 9 (3).

3.	Song, J.;  Li, J.;  Li, X.;  Xu, L.;  Dong, Y.; Zeng, H., Quantum Dot Light-Emitting Diodes Based on Inorganic Perovskite Cesium Lead Halides (CsPbX3). Advanced Materials 2015, 27 (44), 7162-7167.

4.	Protesescu, L.;  Yakunin, S.;  Bodnarchuk, M. I.;  Krieg, F.;  Caputo, R.;  Hendon, C. H.;  Yang, R. X.;  Walsh, A.; Kovalenko, M. V., Nanocrystals of Cesium Lead Halide Perovskites (CsPbX3, X = Cl, Br, and I): Novel Optoelectronic Materials Showing Bright Emission with Wide Color Gamut. Nano Letters 2015, 15 (6), 3692-3696.

5.	Zhang, F.;  Zhong, H.;  Chen, C.;  Wu, X.-g.;  Hu, X.;  Huang, H.;  Han, J.;  Zou, B.; Dong, Y., Brightly Luminescent and Color-Tunable Colloidal CH3NH3PbX3 (X = Br, I, Cl) Quantum Dots: Potential Alternatives for Display Technology. ACS Nano 2015, 9 (4), 4533-4542.

6.	Schmidt, L. C.;  Pertegás, A.;  González-Carrero, S.;  Malinkiewicz, O.;  Agouram, S.;  Mínguez Espallargas, G.;  Bolink, H. J.;  Galian, R. E.; Pérez-Prieto, J., Nontemplate Synthesis of CH3NH3PbBr3 Perovskite Nanoparticles. Journal of the American Chemical Society 2014, 136 (3), 850-853.

7.	García de Arquer, F. P.;  Talapin, D. V.;  Klimov, V. I.;  Arakawa, Y.;  Bayer, M.; Sargent, E. H., Semiconductor quantum dots: Technological progress and future challenges. 2021, 373 (6555), eaaz8541.

8.	Kagan, C. R.;  Lifshitz, E.;  Sargent, E. H.; Talapin, D. V., Building devices from colloidal quantum dots. 2016, 353 (6302), aac5523.

9.	Chiba, T.;  Hayashi, Y.;  Ebe, H.;  Hoshi, K.;  Sato, J.;  Sato, S.;  Pu, Y.-J.;  Ohisa, S.; Kido, J., Anion-exchange red perovskite quantum dots with ammonium iodine salts for highly efficient light-emitting devices. Nature Photonics 2018, 12 (11), 681-687.

10.	Fang, T.;  Wang, T.;  Li, X.;  Dong, Y.;  Bai, S.; Song, J., Perovskite QLED with an external quantum efficiency of over 21% by modulating electronic transport. Science Bulletin 2021, 66 (1), 36-43.

11.	Lee, S.;  Kim, J.;  Kim, H.;  Kim, C.;  Kim, S.;  Kim, C.;  Lee, H.;  Choi, B.;  Muthu, C.;  Kim, T.;  Lee, J.;  Lee, S.;  Ihee, H.; Lee, J.-Y., Brightening deep-blue perovskite light-emitting diodes: A path to Rec. 2020. 2024, 10 (20), eadn8465.

12.	Hao, M.;  Bai, Y.;  Zeiske, S.;  Ren, L.;  Liu, J.;  Yuan, Y.;  Zarrabi, N.;  Cheng, N.;  Ghasemi, M.;  Chen, P.;  Lyu, M.;  He, D.;  Yun, J.-H.;  Du, Y.;  Wang, Y.;  Ding, S.;  Armin, A.;  Meredith, P.;  Liu, G.;  Cheng, H.-M.; Wang, L., Ligand-assisted cation-exchange engineering for high-efficiency colloidal Cs1−xFAxPbI3 quantum dot solar cells with reduced phase segregation. Nature Energy 2020, 5 (1), 79-88.

13.	Liu, F.;  Ding, C.;  Zhang, Y.;  Ripolles, T. S.;  Kamisaka, T.;  Toyoda, T.;  Hayase, S.;  Minemoto, T.;  Yoshino, K.;  Dai, S.;  Yanagida, M.;  Noguchi, H.; Shen, Q., Colloidal Synthesis of Air-Stable Alloyed CsSn1–xPbxI3 Perovskite Nanocrystals for Use in Solar Cells. Journal of the American Chemical Society 2017, 139 (46), 16708-16719.

14.	Liu, L.;  Najar, A.;  Wang, K.;  Du, M.; Liu, S., Perovskite Quantum Dots in Solar Cells. 2022, 9 (7), 2104577.

15.	Shaikh, J. S.;  Shaikh, N. S.;  Mali, S. S.;  Patil, J. V.;  Beknalkar, S. A.;  Patil, A. P.;  Tarwal, N. L.;  Kanjanaboos, P.;  Hong, C. K.; Patil, P. S., Quantum Dot Based Solar Cells: Role of Nanoarchitectures, Perovskite Quantum Dots, and Charge-Transporting Layers. 2019, 12 (21), 4724-4753.

16.	Wang, Y.;  Duan, C.;  Zhang, X.;  Sun, J.;  Ling, X.;  Shi, J.;  Hu, L.;  Zhou, Z.;  Wu, X.;  Han, W.;  Liu, X.;  Cazorla, C.;  Chu, D.;  Huang, S.;  Wu, T.;  Yuan, J.; Ma, W., Electroluminescent Solar Cells Based on CsPbI3 Perovskite Quantum Dots. Advanced Functional Materials 2022, 32 (6), 2108615.

17.	Chi, W.; Banerjee, S. K., Application of Perovskite Quantum Dots as an Absorber in Perovskite Solar Cells. Angewandte Chemie International Edition 2022, 61 (9), e202112412.

18.	Chen, J.;  Du, W.;  Shi, J.;  Li, M.;  Wang, Y.;  Zhang, Q.; Liu, X., Perovskite quantum dot lasers. 2020, 2 (1), 170-183.

19.	Chen, Y.;  Chu, Y.;  Wu, X.;  Ou-Yang, W.; Huang, J., High-Performance Inorganic Perovskite Quantum Dot–Organic Semiconductor Hybrid Phototransistors. 2017, 29 (44), 1704062.

20.	Bai, T.;  Yang, B.;  Chen, J.;  Zheng, D.;  Tang, Z.;  Wang, X.;  Zhao, Y.;  Lu, R.; Han, K., Efficient Luminescent Halide Quadruple-Perovskite Nanocrystals via Trap-Engineering for Highly Sensitive Photodetectors. 2021, 33 (8), 2007215.

21.	Li, Z.;  Johnston, A.;  Wei, M.;  Saidaminov, M. I.;  Martins de Pina, J.;  Zheng, X.;  Liu, J.;  Liu, Y.;  Bakr, O. M.; Sargent, E. H., Solvent-Solute Coordination Engineering for Efficient Perovskite Luminescent Solar Concentrators. Joule 2020, 4 (3), 631-643.

22.	Huang, H.;  Bodnarchuk, M. I.;  Kershaw, S. V.;  Kovalenko, M. V.; Rogach, A. L., Lead Halide Perovskite Nanocrystals in the Research Spotlight: Stability and Defect Tolerance. ACS Energy Letters 2017, 2 (9), 2071-2083.

23.	Kang, J.; Wang, L.-W., High Defect Tolerance in Lead Halide Perovskite CsPbBr3. The Journal of Physical Chemistry Letters 2017, 8 (2), 489-493.

24.	Wang, S.;  Yousefi Amin, A. A.;  Wu, L.;  Cao, M.;  Zhang, Q.; Ameri, T., Perovskite Nanocrystals: Synthesis, Stability, and Optoelectronic Applications. Small Structures 2021, 2 (3), 2000124.

25.	Kim, Y.;  Yassitepe, E.;  Voznyy, O.;  Comin, R.;  Walters, G.;  Gong, X.;  Kanjanaboos, P.;  Nogueira, A. F.; Sargent, E. H., Efficient Luminescence from Perovskite Quantum Dot Solids. ACS Applied Materials & Interfaces 2015, 7 (45), 25007-25013.

26.	Li, H.;  Qian, Y.;  Xing, X.;  Zhu, J.;  Huang, X.;  Jing, Q.;  Zhang, W.;  Zhang, C.; Lu, Z., Enhancing Luminescence and Photostability of CsPbBr3 Nanocrystals via Surface Passivation with Silver Complex. The Journal of Physical Chemistry C 2018, 122 (24), 12994-13000.

27.	Li, Z.;  Chen, Z.;  Yang, Y.;  Xue, Q.;  Yip, H.-L.; Cao, Y., Modulation of recombination zone position for quasi-two-dimensional blue perovskite light-emitting diodes with efficiency exceeding 5%. Nature Communications 2019, 10 (1), 1027.

28.	Xie, K.;  Zhang, S.;  Wang, X.;  Gong, C.;  Zheng, C.;  Xiao, W.; Li, F., Post-synthetic ammonium hexafluorophosphate treatment enables CsPbBr3 perovskite quantum dots exhibiting robust photoluminescence and environmental stability for white light-emitting diodes. Journal of Luminescence 2022, 252, 119401.

29.	Chen, F.;  Imran, M.;  Pasquale, L.;  Salerno, M.; Prato, M., Long-term optical and morphological stability of CsPbBr3 nanocrystal-based films. Materials Research Bulletin 2021, 134, 111107.

30.	Zhang, X.;  Huang, H.;  Zhao, C.; Yuan, J., Surface chemistry-engineered perovskite quantum dot photovoltaics. Chemical Society Reviews 2025, 54 (6), 3017-3060.

31.	Woo, J. Y.;  Kim, Y.;  Bae, J.;  Kim, T. G.;  Kim, J. W.;  Lee, D. C.; Jeong, S., Highly Stable Cesium Lead Halide Perovskite Nanocrystals through in Situ Lead Halide Inorganic Passivation. Chemistry of Materials 2017, 29 (17), 7088-7092.

32.	Krieg, F.;  Ochsenbein, S. T.;  Yakunin, S.;  ten Brinck, S.;  Aellen, P.;  Süess, A.;  Clerc, B.;  Guggisberg, D.;  Nazarenko, O.;  Shynkarenko, Y.;  Kumar, S.;  Shih, C.-J.;  Infante, I.; Kovalenko, M. V., Colloidal CsPbX3 (X = Cl, Br, I) Nanocrystals 2.0: Zwitterionic Capping Ligands for Improved Durability and Stability. ACS Energy Letters 2018, 3 (3), 641-646.

33.	Imran, M.;  Caligiuri, V.;  Wang, M.;  Goldoni, L.;  Prato, M.;  Krahne, R.;  De Trizio, L.; Manna, L., Benzoyl Halides as Alternative Precursors for the Colloidal Synthesis of Lead-Based Halide Perovskite Nanocrystals. Journal of the American Chemical Society 2018, 140 (7), 2656-2664.

34.	Seth, S.;  Ahmed, T.;  De, A.; Samanta, A., Tackling the Defects, Stability, and Photoluminescence of CsPbX3 Perovskite Nanocrystals. ACS Energy Letters 2019, 4 (7), 1610-1618.

35.	Shamsi, J.;  Urban, A. S.;  Imran, M.;  De Trizio, L.; Manna, L., Metal Halide Perovskite Nanocrystals: Synthesis, Post-Synthesis Modifications, and Their Optical Properties. Chemical Reviews 2019, 119 (5), 3296-3348.

36.	Akhil, S.;  Dutt, V. G. V.;  Singh, R.; Mishra, N., Post-synthesis Treatment with Lead Bromide for Obtaining Near-Unity Photoluminescence Quantum Yield and Ultra-stable Amine-Free CsPbBr3 Perovskite Nanocrystals. The Journal of Physical Chemistry C 2022, 126 (26), 10742-10751.

37.	Park, J.;  Park, S.;  Cho, S.;  Kim, Y.;  Kim, H.;  Jeong, S.; Woo, J. Y., Air-stable cesium lead bromide perovskite nanocrystals via post-synthetic treatment with oleylammonium bromides. New Journal of Chemistry 2022, 46 (40), 19514-19522.

38.	Sumukam, R. R.;  Kumar, G. S.;  Savu, R. N.; Murali, B., Strategic Compositional Engineering in Quasi-2D Ruddlesden–Popper Perovskites to Decipher Deep Blue Emission. The Journal of Physical Chemistry Letters 2023, 14 (2), 395-402.