Cheminformatics and Machine Learning for Quasi-2D Perovskites: Emission Energy Prediction and the Limits of EQE Modelling

Ranadeep Raj Sumukam, Ramu Naidu Savu, Santhosh Rompivalasa and Banavoth Murali*

Solar Cells and Photonics Research Laboratory, School of Chemistry, University of Hyderabad, Prof. C R Rao Road, Hyderabad -500046, Telangana State, India.

*Email: murali.banavoth@uohyd.ac.in

Abstract

Layered quasi-two-dimensional metal-halide perovskites (Q2DPes) have captivated researchers in the field of light-emitting diodes (LEDs) owing to their facile solution-processing and highly tunable optoelectronic properties. Compared with other dimensional perovskite counterparts, Q2DPes offer more parameters to tune their properties, providing a wider scope for control and making them a complex system. Therefore, exploring their vast compositional parameter space remains a major experimental challenge. Machine learning (ML) has emerged as a powerful paradigm for understanding patterns in complex systems with nonlinear relationships among multiple parameters. In recent times, ML has been used extensively across all fields to accelerate research and reduce costs by strategizing work rather than relying on trial-and-error experimentation. In this work, we developed two distinct sets of hyperparameter-tuned ML models using data compiled from the literature, where the first set is focused on materials-level intrinsic emission properties and the second one is on device-level external quantum efficiency (EQE). Among all models, the Support Vector Regression model with a radial basis function kernel (SVR–RBF) achieved an outstanding coefficient of determination (R2) of 0.953 and a low root-mean-square error (RMSE) of 0.074 eV with the emission energy prediction window covering a major part of the visible spectrum. In contrast, predicting device EQE using the same workflow and style of data with additional device-level details resulted in an R2 of only 0.57 at best. Finally, model decisions were thoroughly validated using Kernel SHAP analysis, confirming that the algorithmic rankings align with confinement physics and halide chemistry trends.

4.1. Introduction

Metal halide perovskites have attracted attention in the field of optoelectronics for their exceptional absorption coefficients, tunable band gaps, high colour purity, and solution-processability, enabling rapid progress in solar cells, photodetectors, lasers, and light-emitting diodes (LEDs).1-5 Among low-dimensional variants, layered quasi-two-dimensional metal-halide perovskites (Q2DPes) have emerged as a versatile material for perovskite LEDs (PeLEDs).6-10 Structurally, Q2DPe materials are formed by intercalating bulky organic spacer cations into the 3D framework, which slices the inorganic octahedra into layers of thickness n. These Q2DPes are primarily categorized into Ruddlesden–Popper (RP) phases with the general formula L2An-1PbnX3n+1 (A = small organic cation or inorganic cation, X = halide ion) where monovalent spacer cations (L) form van der waals gaps between the inorganic layers and Dion–Jacobson (DJ) phases with general formula L′An-1PbnX3n+1 where divalent diammonium cations (L′) bond directly to adjacent inorganic sheets eliminating the van der Waals gap. By tuning their quantum and dielectric confinements using organic spacer chemistry and halide composition, we can cover a wide portion of the visible spectrum while retaining solution processability and improved environmental stability relative to their three-dimensional counterparts.5, 11

Since the parameter space is large in Q2DPes, unlike in their 3D counterparts, their outcomes are not always predictable from the main stoichiometry alone. Research groups struggle to explore this space experimentally because they can only vary one variable at a time. Traditional materials development for perovskite optoelectronics has always depended on trial-and-error experimentation, density functional theory (DFT) and high-throughput screening. Now, Machine Learning (ML), which relies on statistical models, has emerged as a complementary fourth paradigm that can learn patterns from curated datasets, reduce experimental waste, and is not limited by the theoretical rules/laws as physical models like DFT, which enlarges the scope for finding new relations and empirical laws. Therefore, ML models have been adopted in perovskite photovoltaics and, more recently, in LED work, to extract patterns from curated datasets.12-17

Materials-focused ML workflows typically comprise data collection, data cleaning, feature engineering (molecular descriptor generation, correlation filtering, and feature selection), model training, and performance evaluation, along with insights from interpretability tools such as SHAP (Shapley Additive exPlanations) to connect predictions with physicochemical mechanisms.17-20 In general, data-driven ML studies on perovskite optoelectronics focus on active-layer optimisation, transport-layer selection, interface engineering, and mechanism elucidation. To date, there are very few ML-based reports focused on the emission of Q2DPes and LEDs. Prior work on Q2DPes demonstrated that photon energy can be estimated from precursor composition and lipophilicity (XLogP3) of organic ligand, leveraging a random-forest model with root-mean-square errors on the order of ~0.05 eV. 21 Work on PeLED additives reached good accuracy only when the dataset was built from a single device architecture.22 However, several gaps persist relative to the needs of Q2DPes based LED researchers working across full visible-range color tuning. Our objective is to address the pain point where published ML studies are confined to a narrow spectral window (for example, green or blue Br/Cl systems) or a reduced feature set based solely on precursor ion ratios limited to single organic ligand systems, without explicitly encoding primary and secondary organic spacer structures through cheminformatics descriptors. In addition, we tried to answer whether external quantum efficiency (EQE) can be predicted with comparable confidence to the literature data available under the same curation rules.

Figure 4.1: End-to-end workflow from literature extraction to predicted Eph. SMILES conversion, descriptor calculation, correlation pruning, parallel RFECV (31 features) and SelectFromModel (13 features) for feature selection, hyperparameter-tuned regressors, and SHAP analysis.

In this work, we built ML models that address the aforementioned gaps, leveraging a dataset of Q2DPes extracted from the literature for training and testing. Herein, we built two primary sets of ML models: one targeting emission energy (Eph) prediction, which is a material’s intrinsic properties, and the other targeting EQE, which is a device-based metric. After preparing the first version of the dataset, we performed initial cleanup and harmonisation, which included halide flags, precursor-ratio normalisation, and mixed-spacer indicators, in the Snowflake data warehouse using Structured Query Language (SQL). Datasets are available on the GitHub account for reference. On top of the resulting dataset in Snowflake, the remaining data engineering operations were performed in Python (Jupyter Notebook) using the pandas dataframes. Thereafter, Simplified Molecular Input Line Entry System (SMILES) strings were generated programmatically for each organic ligand from its IUPAC name using the Chemical Identifier Resolver API hosted by the National Cancer Institute Computer-Aided Drug Design Group (nih.gov). Then, two-dimensional molecular descriptors per spacer (Primary and secondary) were generated using RDKit library structures using the SMILES. After generating molecular descriptors, high-dimensional feature extraction produced a dataset in which the number of features exceeded the number of observations, leading to the curse of dimensionality. So, to handle the curse of dimensionality, we applied a couple of feature elimination techniques in a sequential order: 1) Pairwise Pearson correlation and 2a) SelectFromModel for one set of models and 2b) Recursive Feature Elimination using Cross Validation (RFECV) for another set of models. After the model training and evaluation, we further performed an in-depth SHAP analysis. Figure 4.1 gives the holistic view of the workflow. All the codes for building different models and datasets are available on GitHub.

4.2 Results and Discussion

4.2.1. ML Models for Emission Energy Prediction

To target emission energy prediction, we prepared a curated dataset of 283 records for ML model training and testing, extracted from the available literature (dataset available on GitHub: SF_DATA_EMISSION_PEAK.xlsx, sheet SF_DATA_EMISSION_PEAK_NEW; Dataset Statistics are provided in Appendices III Table 1-3. As the objective of the work is to build an efficient ML model that covers a wide range of Eph prediction windows in the visible region, the reports that provided the data points over photon energies between 1.53 and 3.06 eV, corresponding to a peak wavelength range of 405–810 nm, were collected. As expected, the data distribution is uneven, mirroring the available literature to date. About ≈ 69% of 283 records fall between 480 nm and 550 nm (green–yellow), ≈ 12% lie in the violet/blue (400–480 nm), and ≈ 17% in deep red and near-infrared (650–900 nm), with fewer orange/red points in between (Table S2). A model trained only on typical green emission perovskite materials would underrepresent the halide and confinement extremes, thereby limits the scope to that wavelength range itself.

Figure 4.2: a) Correlation heatmap and b) feature importance scores for the 31 retained training features by the RFECV technique.

For the features, after generating two-dimensional molecular descriptors, as mentioned in the above section, the dataset had 462 columns, including compositional and halide flags, one-hot-encoded solvent columns, and Pri/Sec-prefixed RDKit descriptors organic spacers (217 descriptors for each). To maintain proper data distribution across reports with mixed organic spacers and single organic spacers, where 46 entries (~16%) are mixed primary and secondary spacers, we have used an 80/20 split stratified on the IS_MIXED_SPACERS_SPACER column, yielding 226 training and 57 test records. It is worth mentioning that mixed spacer formulations are chemically significant as the secondary ligand prominently impacts interlayer spacing and can determine which n domains contribute more to the emission. After splitting the dataset into a training and a test set, we began feature elimination to prevent the curse of dimensionality using only the training dataset, to avoid test data leakage. Initially, a Pairwise Pearson correlation was applied to the training fold with a Pearson correlation coefficient threshold of 0.9 (|r| > 0.90), and 173 redundant columns were omitted, leaving 289 candidates for selection. Starting from 289 post-correlation-based columns elimination, we applied RFECV and scikit-learn’s SelectFromModel in parallel, each fit on the 226 training records. RFECV ran a random forest regressor (max_depth = 5, min_samples_leaf = 6) with 5-fold stratified cross-validation. In this approach, features are removed one at a time until the cross-validated root mean square error (RMSE) of Eph reaches a minimum. According to RFECV, the curve in Appendices III Figure 1 shows that 31 of 289 features are optimal, as additional features stopped improving cross-validation. The correlation heatmap and the feature importance scores for the 31 features are shown in Figure 4.2. On the other hand, the SelectFromModel approach works differently. In this, a single random forest with threshold='mean' was fit on all 289 features, which means it keeps only descriptors whose impurity-based importance exceeds the forest average. Given the aggressive approach, we were left with only 13 features. The correlation heatmap and the feature importance scores for the 13 features are shown in Figure 4.3.

Figure 4.3: a) Correlation heatmap and b) feature importance scores for the 13 retained training features by the SelectFromModel technique.

Finally, multiple ML models (Regressors: random forest, CatBoost, XGBoost, Support Vector Regression (SVR), and Gaussian process) were built using the above prepared datasets. Among all the models, the SVR model outperformed the others in predicting emission energies using the dataset from the SelectFromModel approach. It is worth noting that the models built on the datasets using the RFECV technique also performed well. We have summarised all the models' performance in Table 1. Every regressor in Table 1 was tuned by randomised search (15 trials, five-fold cross-validation on the training set) before a single evaluation on the test fold. Tree ensembles can memorise rare spacer–halide combinations in 226 rows, and Gaussian Process Regressors (GPR) are sensitive to kernel length scales when the number of features (p) is large. For the thirty-one-feature RFECV matrix, tuning improved GPR’s coefficient of determination (R2) from 0.877 to 0.920, and in the case of thirteen-feature SelectFromModel matrix, SVR and GPR were improved, out of which SVR with a radial-basis-function kernel (SVR–RBF) emerged as the best, with the R2 = 0.953, RMSE = 0.074 and mean absolute error (MAE) = 0.048. Formulas for each evaluation metric are defined below (Equation 4.1-4.3), where E is the reported photon energy, Ê is the predicted photon energy by the model, and Ē is the mean of reported photon energies. All the models summaries and the SHAP analysis of the models are available in the Appendices III.

R² = 1 - [ Σᵢ (Eᵢ - Êᵢ)² ] / [ Σᵢ (Eᵢ - Ē)² ]					– Equation 4.1

RMSE = √[ (1/n) · Σᵢ (Eᵢ - Êᵢ)² ] 						– Equation 4.2

MAE = (1/n) · Σᵢ |Eᵢ - Êᵢ|							– Equation 4.3

It is crucial to understand that RFECV selects 31 features and achieves a lower training-fold cross-validation error than the 13-feature SelectFromModel channel, yet the 13-variable SVR model is unambiguously better as R2 rose from 0.920 to 0.953, and RMSE fell from 0.097 to 0.074 eV, a 24% reduction in root error at less than half the dimensionality. The performance difference between RFECV and SelectFromModel aligns well with the sample-to-feature ratio, which influences overfitting. As shown in Table S4, for 226 training points, the sample-to-feature ratio is 17.4 for the SelectFromModel set but only 7.3 for the RFECV set; therefore, the RFECV flow is more prone to overfitting, which works well on the training data but poorly on the test data.

Table 4.1. Summary of the hyperparameter-tuned models' performance in predicting the Eph.

| Feature selection | p | Model | R2 | RMSE (eV) | MAE (eV) |
| --- | --- | --- | --- | --- | --- |
| SelectFromModel | 13 | SVR (RBF) | 0.953 | 0.074 | 0.048 |
| SelectFromModel | 13 | Gaussian process | 0.920 | 0.096 | 0.061 |
| SelectFromModel | 13 | CatBoost | 0.875 | 0.121 | 0.063 |
| RFECV | 31 | SVR (RBF) | 0.920 | 0.097 | 0.054 |
| RFECV | 31 | Gaussian process | 0.877 | 0.120 | 0.073 |
| RFECV | 31 | CatBoost | 0.862 | 0.127 | 0.066 |

Apparently, the SelectFromModel-based features list is short enough to derive scientific insights rather than a black-box vector (full names in Table S5; correlation structure and feature importances in Figure 4.3). The halide flags that are based on the anion part of salts, sourcing the organic cation (CL_PRIMARY_ORGANIC_HALIDE, BR_PRIMARY_ORGANIC_HALIDE) and the inorganic lead-halide fractions (PbCl2, PbBr2) jointly determine the perovskite inorganic framework’s band edge and the halide chemical potential in the perovskite precursor. Bromide-rich precursors generally favour hypsochromic shift, whereas chloride can raise energy further, but often complicates phase purity if not balanced with stoichiometry. On the other hand, iodide-rich recipes promote bathochromic shift. The model selected these features over many unused RDKit columns, indicating a well-established relationship between halide chemistry and emission energy in perovskites.5, 12 SPACER_TO_PB_RATIO is a critical parameter that controls the average n (number of layers in the inorganic framework) in Q2DPes. A greater spacer-to-lead ratio increases the organic fraction in the film, thereby strengthening the average dielectric confinement. It fosters the dominant transition to higher Eph by shifting holistically towards lower n.1 SPACER_TO_PB_RATIO survival after aggressive selection elimination is perhaps the strongest sanity check on the ML pipeline learning on confinement physics. The A-site cation to Pb ratios (CsBr_TO_Pb, CsI_TO_Pb, FABr_TO_Pb, FAI_TO_Pb) reflect the extent of diversity hidden in the A-site cation data in the prepared dataset. Our model does not assume a single cation; it learned from the blended ratios actually reported. SOLVENT_DMF surviving selection is not surprising as DMF and DMSO are known to change Pb coordination and crystallization kinetics, which in turn changes n partitioning. That variable is a processing fingerprint no less than a compositional one. Among molecular descriptors, Pri_VSA_EState4 (Surface-area + electrotopological-state) captures how much of the primary spacer’s van der Waals surface sits in a particular electronic-state bin, which is related to heteroatom content and polarizability at the organic–inorganic interface. For the 46 mixed-spacer entries, the features that survived elimination are Sec_HallKierAlpha, which refers to the flexibility/topology of the secondary amine and Sec_PEOE_VSA6, which refers to partial-charge surface area on the secondary ligand. They capture how a second ligand perturbs interlayer spacing and local dielectric environment without requiring an explicit n-distribution label.

The 31-variable RFECV set adds few more features to the list, among others, PRIMARY_SPACER_FRACTION, SOLVENT_DMSO, several Pri_BCUT2D_* partitions, Pri_qed, rotatable-bond counts, and additional PEOE/VSA terms (full list, Table S6). They refined the picture but did not improve the test error, given the available sample size.

4.2.2 SHAP Analysis

We leveraged SHAP to move from accurate prediction to real-time actionable chemistry by assessing the impact of each feature on the model's behaviour. It provides validation that the fitted SVR ranks drivers in the same order as expected based on chemical mechanisms and confinement physics (Figure 4.4). For each test record, the SVR prediction is decomposed into the average baseline from background samples(φ₀), which is 2.33 eV from 50 randomly drawn training samples, and the Shapley contributions (φj) of descriptor j, as shown in Equation 4. A positive φj pushes the prediction to higher Eph (hypsochromic shift), and a negative φj pushes it to lower Eph (bathochromic shift). Since SVR is not a tree model, we used Kernel SHAP with the fitted f(x), standardised features, and 50 background samples. Then summarised the rankings across all 283 samples as the mean absolute contribution ⟨|φj|⟩. We have prepared Table 4.2, linking these numerical rankings to Q2DPes photophysics.

f(x) = φ₀ + φ₁(x) + φ₂(x) + … + φₚ(x)  =  φ₀ + Σⱼ φⱼ(x) 	   – Equation 4

Figure 4.4: SHAP for the select_from_model + SVR model - (champion model).

Table 4.2 SHAP summary for hyperparameter-tuned SVR–RBF (thirteen SelectFromModel features). ⟨|φ|⟩ = mean absolute Shapley contribution (eV); share = percentage of Σ⟨|φj|⟩.

| Rank | Descriptor | ⟨¦φ¦⟩ (eV) | Share (%) | Trend when feature ↑ | Chemical / physical mechanism |
| --- | --- | --- | --- | --- | --- |
| 1 | PbBr2 | 0.074 | 21.4 | hypsochromic shift (r ≈ +0.95) | Inorganic Br raises the lead-halide bandgap and favours wider-gap, more confined wells, thereby dominating the average emission colour. |
| 2 | BR_PRIMARY_ORGANIC_HALIDE | 0.059 | 17.1 | hypsochromic shift (r ≈ +0.96) | Bromide on the primary ammonium spacer increases halide incorporation on the organic site and blue-shifts the emitting manifold relative to iodide-only compostions. |
| 3 | FAI_TO_Pb | 0.031 | 8.9 | bathochromic shift (r ≈ −0.98) | Formamidinium iodide fraction enriches iodide character and lowers the effective gap—consistent with red-shifted Q2DPe PL/EL when iodide dominates. |
| 4 | FABr_TO_Pb | 0.028 | 8.0 | bathochromic shift (r ≈ −0.91) | FA bromide pathway competes with high-gap chloride/bromide routes; higher FA:Pb (Br) correlates with lower predicted Eph according to the trend in collected dataset. |
| 5 | CsI_TO_Pb | 0.027 | 7.8 | bathochromic shift (r ≈ −0.87) | Cesium iodide supply biases films toward iodide-rich, lower-gap character relative to all-bromide precursor sets. |
| 6 | PbCl2 | 0.027 | 7.7 | hypsochromic shift (r ≈ +0.97) | Chloride in the inorganic precursor raises chemical potential for wide-gap domains and correlates with higher reported Eph. |
| 7 | Pri_VSA_EState4 | 0.024 | 6.8 | bathochromic shift (r ≈ −0.79) | Primary-spacer VSA by electrotopological state—proxy for heteroatom-rich headgroups that alter hydrogen bonding and interlayer spacing at the interface. |
| 8 | CsBr_TO_Pb | 0.023 | 6.5 | Weak | CsBr fraction modulates A-site/halide balance; weaker monotonic trend because Cs appears with mixed halides across papers. |
| 9 | SOLVENT_DMF | 0.017 | 4.9 | Weak | DMF vs DMSO shifts crystallisation and phase distribution; it survives selection because the solvent is consistently reported. |
| 10 | SPACER_TO_PB_RATIO | 0.013 | 3.7 | Weak | Nominal spacer:lead stoichiometry targets average n and dielectric confinement; smaller SHAP share because processing redistributes. |
| 11 | Sec_HallKierAlpha | 0.011 | 3.3 | Weak | Secondary spacer flexibility/topology (mixed spacer rows); perturbs interlayer spacing and local dielectric environment. |
| 12 | CL_PRIMARY_ORGANIC_HALIDE | 0.008 | 2.3 | hypsochromic shift (r ≈ +0.97) | Chloride on the primary spacer; high correlation but low ⟨¦φ¦⟩ because fewer entries use chloride in primary recipes. |
| 13 | Sec_PEOE_VSA6 | 0.006 | 1.7 | Weak | Partial-charge-weighted VSA on the secondary ligand; fine tunes mixed spacer systems. |

4.2.3 External quantum efficiency: A different problem

Similar to the Eph prediction model development discussed above, now to target predicting EQEs of the Q2DPe LEDs, we prepared a curated dataset of 266 records extracted from the available literature (dataset available on GitHub: SF_DATA_EMISSION_PEAK.xlsx, sheet EQE_CLEANED and dataset statistics in Appendices III Table 10) with hole-transport material (HTL), electron-transport material (ETL), additive, and experimental processing variables (temperature, annealing time) in addition to the compositional columns used for emission. Thirty-four distinct HTLs and thirteen ETLs are available in the dataset, while EQE spans 0.002% to 30.8%. After repeating the same workflow steps for featuring engineering used above for Eph prediction models, post-recursive feature elimination to 20 descriptors, and extensive hyperparameter tuning, the best tree models achieved R2 ≈ 0.44–0.51 on the test fold (Table 4.3). We developed a CatBoost model that treats HTL, ETL, and additive as native categorical variables to encode the proper device architecture, which has raised R2 to 0.57 with RMSE ≈ 4.4% EQE. That improvement is real but modest; it explains a little more than half the variance in EQE, whereas the emission model explains about 95% of the variance in Eph, using the same split and workflow with more details. After achiving the best ML model for predicting emission colour at the materials level, one might hope EQE would follow from the same tables. Apparently, it does happen, at least not with the fields available in published PeLED reports.

Table 4.3. Summary of the hyperparameter-tuned models' performance in predicting the EQE.

| Model | R2 | RMSE (% EQE) | MAE (% EQE) |
| --- | --- | --- | --- |
| Tuned XGBoost (RFE, 20 features) | 0.512 | 5.01 | 3.77 |
| Tuned random forest | 0.478 | 5.18 | 3.88 |
| Tuned CatBoost | 0.443 | 5.35 | 3.75 |
| CatBoost (architecture features) | 0.570 | 4.42 | 3.25 |

The gap between the emission forecasting model (R2 ≈ 0.95) and the EQE forecasting model (R2 ≈ 0.5–0.6) is not a failure of the algorithms. Rather, there are straightforward, concrete reasons that caused this issue. EQE couples radiative efficiency to charge-injection balance and outcoupling. Pinhole-free morphology, interfacial trap passivation, refractive-index matching and the exact measurement protocol move EQE by several percentage points without changing the precursor stoichiometry. Different laboratories also anneal and antisolvent-quench under conditions that are described in prose but rarely discussed in the manuscripts. Zhang et al. illustrated that the data problem in device-targeted ML development persists even with careful molecular featurization.22 PeLED performance labels in the literature are sparse and heterogeneous, given the volume of available data. Therefore, we can expect the model’s predictions to be accurate only when the dataset is built from a single device architecture with in-house experiments, as fabrication conditions are consistent across devices. This infers that models are most trustworthy when inputs and labels refer to the same experimental contract, and least trustworthy when they silently average over incompatible fabrication routes.

Figure 4.5: SHAP summary for the CatBoost architecture EQE model.

4.3. Conclusions

In this work, we began by preparing two datasets from the available literature on Q2DPes, focusing on emission energy and device EQE. Then performed an initial cleanup using snowflake and pandas dataframe functions, respectively. Thereafter, molecular descriptors were generated for the organic spacers from their SMILES, and feature selection methods were applied. Finally, ML models were trained and evaluated.

Specifically, a hyperparameter-tuned SVR model utilising a feature engineered dataset of 13 variables, which include halide identity, spacer-to-lead stoichiometry, critical A-site and lead-halide fractions, DMF processing parameters, and three organic spacer topology descriptors, unambiguously outperformed a higher dimensional 31 variable RFECV feature selection routine on held-out test records. For the optimised SVR model, the 13-feature pipeline achieved a coefficient of determination (R2) of 0.953 and a low root-mean-square error (RMSE) of 0.074 eV, whereas the 31-variable RFECV channel resulted in R2 of 0.097 eV for its tuned SVR variant. This performance gap reflects a fundamental statistical reality where a training dataset with 226 records is highly prone to overfitting as the number of descriptor dimensions increases. Furthermore, SHAP analysis confirms that the variables retained by our top performing materials pipeline align cleanly with the composition and quantum confinement principles.

On the other hand, device-level EQE are less predictable when modelled using similar literature inputs with additional device-level details, yielded a weak R2 of approximately 0.5–0.6 at best. Although the integration of transport-layer labels provides a modest performance benefit, physical film morphology and specific laboratory fabrication protocols and conditions determine overall efficiency, which may vary from one laboratory report to another with the same set of recipes and device architectures. These insights establish that chemically lean ML models are accurate for predicting intrinsic material properties (Eph), but device-based metrics such as EQE remain fundamentally unlearnable across heterogeneous literature sources without strictly standardised fabrication and testing conditions.

Data Availability

Analysis code and configuration files are available at https://github.com/ranadeeprajsumukam/ML_Quasi_2D_Emission_EQE. The curated workbook is available from the corresponding author on reasonable request.

Associated Content

The Appendices III contains dataset statistics and details on all non-champion ML models and their approaches.

Author contributions

Ranadeep Raj Sumukam: conceptualisation, data curation, investigation, end-to-end analysis, methodology, writing – review & editing. Ramu Naidu Savu: formal analysis, writing – review & editing. Santosh Rompivalasa: formal analysis.  Murali Banavoth: funding, supervision, project administration, writing – review & editing. All authors have given approval to the final version of the manuscript.

Conflicts of interest

There are no conflicts to declare.

Acknowledgements

This work was supported by the School of Chemistry, University of Hyderabad. RRS acknowledges Council of Scientific and Industrial Research (CSIR) for the Senior Research Fellowship (SRF). MB acknowledges the Institute of Eminence Research grant (UOH-IOE-RC2-21-008) for funding.

References

1.	Hazra, V.;  Mandal, A.; Bhattacharyya, S., Optoelectronic insights of lead-free layered halide perovskites. Chemical Science 2024, 15 (20), 7374-7393.

2.	Sumukam, R. R.;  Sahu, P.;  Savu, R. N.;  Khanam, S. J.;  Alsulami, Q. A.; Banavoth, M., Halide Ions Distribution and Charge Dynamics in Mixed-Halide Perovskites. 2022, 16 (5), 2100576.

3.	Kumar, G. S.;  Sumukam, R. R.;  Rajaboina, R. K.;  Savu, R. N.;  Srinivas, M.; Banavoth, M., Perovskite Nanowires for Next-Generation Optoelectronic Devices: Lab to Fab. ACS Applied Energy Materials 2022, 5 (2), 1342-1377.

4.	Li, G.;  Zhang, Z.;  Agyei-Tuffour, B.;  Wu, L.;  Gries, T. W.;  Prashanthan, K.;  Frohloff, L.;  Musiienko, A.;  Li, J.;  Zhu, R.;  Hart, L. J. F.;  Wang, L.;  Li, Z.;  Hou, B.;  Koch, N.;  Saba, M.;  Barnes, P. R. F.;  Nelson, J.;  Dyson, P. J.;  Nazeeruddin, M. K.;  Li, M.; Abate, A., Stabilizing high-efficiency perovskite solar cells via strategic interfacial contact engineering. Nature Photonics 2026, 20 (1), 55-62.

5.	Karlsson, M.;  Yi, Z.;  Reichert, S.;  Luo, X.;  Lin, W.;  Zhang, Z.;  Bao, C.;  Zhang, R.;  Bai, S.;  Zheng, G.;  Teng, P.;  Duan, L.;  Lu, Y.;  Zheng, K.;  Pullerits, T.;  Deibel, C.;  Xu, W.;  Friend, R.; Gao, F., Mixed halide perovskites for spectrally stable and high-efficiency blue light-emitting diodes. Nature Communications 2021, 12 (1), 361.

6.	Kumar, G. S.;  Sumukam, R. R.; Murali, B., Quasi-2D perovskite emitters: a boon for efficient blue light-emitting diodes. Journal of Materials Chemistry C 2020, 8 (41), 14334-14347.

7.	Zhang, J.;  Yan, C.;  Zhao, H.;  Yin, C.; Bai, S., Modulations of Quasi-Two-Dimensional Metal Halide Perovskites toward High-Performance Blue Light-Emitting Diodes. Advanced Functional Materials 2026, 36 (22), 2509226.

8.	Liu, Y.;  Wang, H.;  Zhang, F.;  Chai, X.;  Liu, K.;  Zhang, S.;  Kong, M.;  Liu, H.;  Wang, X.;  Lu, M.;  Yang, Y.;  Wu, Z.;  Zhang, Y.;  Fan, C.; Bai, X., High-Efficiency and Stable Pure Bromine Blue Light-Emitting Diodes Enabled by Hybrid Quasi-2D Perovskite. Advanced Functional Materials 2026, 36 (11), e15841.

9.	Zhang, G.;  Tang, J.;  Wu, X.;  Chen, J.;  Zhang, C.;  Zhu, X.;  Yu, H.;  Shi, Y.;  Wang, X.;  Li, J.;  Wang, K.; Li, J., Synergistic Passivation via Amino Acid Derivative for Highly Efficient Quasi-2D Perovskite Green Light-Emitting Diode. ACS Applied Materials & Interfaces 2025, 17 (20), 29864-29872.

10.	Yu, A.;  Wang, J.;  Huo, Y.;  Wang, S.;  Zhang, X.;  He, T.;  Yang, S.;  Jiang, Y.;  Zhang, L.;  Liu, Z.;  Yuan, M.; Sun, C., Promoting Phase Transition in Quasi-2D Perovskites For High-Performance Pure-Red LEDs. Advanced Materials 2025, 37 (28), 2503704.

11.	Tsai, H.;  Nie, W.;  Blancon, J. C.;  Stoumpos, C. C.;  Asadpour, R.;  Harutyunyan, B.;  Neukirch, A. J.;  Verduzco, R.;  Crochet, J. J.;  Tretiak, S.;  Pedesseau, L.;  Even, J.;  Alam, M. A.;  Gupta, G.;  Lou, J.;  Ajayan, P. M.;  Bedzyk, M. J.; Kanatzidis, M. G., High-efficiency two-dimensional Ruddlesden-Popper perovskite solar cells. Nature 2016, 536 (7616), 312-6.

12.	Lu, F.;  Liang, Y.;  Wang, N.;  Zhu, L.; Wang, J., Machine learning for perovskite optoelectronics: a review. 2024, 6 %J Advanced Photonics (5), 054001.

13.	de la Asunción-Nadal, V.;  Iliffe Sprague, C.;  Guijarro-Berdiñas, B.;  Cappel, U. B.; García-Fernández, A., Machine learning for perovskite solar cells: a comprehensive review on opportunities and challenges for materials scientists. EES Solar 2025, 1 (6), 927-957.

14.	Zhang, R.;  Motes, B.;  Tan, S.;  Lu, Y.;  Shih, M.-C.;  Hao, Y.;  Yang, K.;  Srinivasan, S.;  Bawendi, M. G.; Bulović, V., Machine Learning Prediction of Organic–Inorganic Halide Perovskite Solar Cell Performance from Optical Properties. ACS Energy Letters 2025, 10 (4), 1714-1724.

15.	Toprak, A., Predicting photovoltaic output parameters of perovskite solar cells using explainable machine learning with physics-informed and simulation-derived descriptors. Materials Today Communications 2026, 52, 114968.

16.	Wang, Z.;  Chen, C.;  Qian, S.;  Jia, B.;  Xu, Y.;  Guan, X.;  Han, Z.;  Tuo, Y.;  Du, Y.;  Yun, X.;  Xie, J.;  Liu, G.; Lu, P., Data-Driven Design of Halide Perovskites for Efficient Green Light-Emitting Diodes via Machine Learning and DFT. The Journal of Physical Chemistry C 2025, 129 (30), 13542-13557.

17.	Wang, S.;  Liu, C.;  Hao, W.;  Zhuang, Y.;  Zhu, X.;  Wang, L.;  Niu, X.;  Liu, S.;  Chen, B.; Zhao, Q., From Formability to Bandgap: Machine Learning Accelerates the Discovery and Application of Perovskite Materials. ACS Nano 2025, 19 (32), 29049-29072.

18.	Wang, Y.;  Liu, J.;  Liu, Y.;  Li, S.;  Xu, X.; Lou, Z., Recent advances in lead-free halide perovskites: from synthesis to applications. Journal of Materials Chemistry C 2024, 12 (28), 10267-10329.

19.	Zhang, L.;  Lu, F.;  Tao, G.;  Li, M.;  Yang, Z.;  Wang, A.;  Zhu, W.;  Cao, Y.;  Jin, Y.;  Zhu, L.;  Huang, W.; Wang, J., Prediction of Operational Lifetime of Perovskite Light Emitting Diodes by Machine Learning. 2024, 6 (6), 2300772.

20.	Ghodeswar, U. S.;  Balpande, R. S.;  Raut, V. P.;  Waje, M. G.;  Pethe, Y. S.;  Shelke, N.;  Isleem, H. F.; Vairagade, V. S., The optimization of design and performance in hybrid organic/inorganic LEDs toward next-generation high-efficiency LEDs: application of multi-model hybrid machine learning approach. Journal of Computational Electronics 2025, 24 (3), 92.

21.	Wang, W.;  Li, Y.;  Zou, A.;  Shi, H.;  Huang, X.;  Li, Y.;  Wei, D.;  Qiao, B.;  Zhao, S.;  Xu, Z.; Song, D., Predicting the photon energy of quasi-2D lead halide perovskites from the precursor composition through machine learning. Nanoscale Advances 2022, 4 (6), 1632-1638.

22.	Zhang, L.;  Li, N.;  Liu, D.;  Tao, G.;  Xu, W.;  Li, M.;  Chu, Y.;  Cao, C.;  Lu, F.;  Hao, C.;  Zhang, J.;  Cao, Y.;  Gao, F.;  Wang, N.;  Zhu, L.;  Huang, W.; Wang, J., Deep Learning for Additive Screening in Perovskite Light-Emitting Diodes. 2022, 61 (37), e202209337.