A Synopsis of the thesis entitled

Optoelectronic Properties of Low-Dimensional Perovskites: An Experimental and Data-Driven Machine Learning Study

A thesis submitted during 2026 to the University of Hyderabad in partial fulfillment of the award of a Ph.D. degree in School of Chemistry

by

Ranadeep Raj S

School of Chemistry

University of Hyderabad

(P.O.) Central University

Gachibowli, Hyderabad – 500 046

Telangana

India

The rapid growth of display, lighting, and optoelectronic technologies has created a constant demand for materials that can deliver efficient, stable, and colour-pure emission. Conventional emitters such as OLEDs, GaN-based LEDs, and colloidal quantum dots have made major progress, but each of them still faces limitations in efficiency, spectral purity, cost, or long-term stability. In this context, low-dimensional metal halide perovskites have emerged as a highly promising class of materials because they combine high exciton binding energy, tunable band gaps, defect tolerance, and solution processability.

This thesis, titled “Optoelectronic Properties of Low-Dimensional Perovskites: An Experimental and Data-Driven Machine Learning Study”, explores two complementary directions: i) Experimental control of emission in perovskite nanocrystals and quasi-two-dimensional perovskites and ii) Machine-learning-based prediction of emission energy in quasi-two-dimensional perovskite systems. The thesis is organized into four main parts: first,  it introduces the broader materials background, then presents an experimental study on CsPbBr3 nanocrystals, followed by a detailed study of blue-emitting quasi-2D perovskites, and finally develops a data-driven machine learning framework for emission prediction and explainability.

Chapter 1

The introductory chapter sets the foundation for the entire thesis by explaining why advanced emissive materials are needed for modern lighting and display technologies, especially for blue emission, where efficiency and stability still remain major challenges. It begins with the evolution of solid-state lighting and the growing need for materials that can operate efficiently, especially in the blue region of the visible spectrum, where current emitters are still less mature. It then introduces lead halide perovskites as a family of optoelectronic materials and explains how their defect tolerance, tunable bandgap, and solution processability make them attractive for optoelectronic applications.

It then moves to perovskite nanocrystals, describing their synthesis routes and the importance of surface ligands and surface defects in determining photoluminescence and stability. Thereafter, the chapter introduces quasi-2D layered perovskites and explains how quantum confinement, dielectric confinement, phase distribution, and spacer-cation chemistry influence their emission behaviour. The main limitations of blue PeLEDs, such as phase impurity, ion migration, charge-injection mismatch, interface loss, and device degradation, are also discussed. Finally, the chapter lays the foundation for the machine-learning workflow used later in the thesis, including data collection, feature engineering, model training, cross-validation, and SHAP-based interpretation.

Chapter 2

The second chapter focuses on CsPbBr3 nanocrystals and addresses one of the most important practical issues in nanocrystal-based perovskite devices, namely surface traps and non-radiative recombination. The chapter investigates how post-synthesis surface treatment can improve optical performance without damaging the crystal core. A range of passivating agents was tested, which includes YCl3, PDABr2, GuSCN, KSCN, choline bromide, and NH4SCN, to understand how different cation-anion combinations influence the emission properties of the nanocrystals.

The results show that not all treatments are beneficial, but a few of them significantly enhance photoluminescence, especially at optimized concentrations. In particular, PDABr2, GuSCN, YCl3, and NH4SCN improved the emission intensity, while choline bromide and KSCN quenched it. The best-performing sample was PDABr2-treated CsPbBr3, which showed a large increase in average lifetime and photoluminescence quantum yield, indicating strong suppression of non-radiative pathways.

The chapter further supports these optical observations through time-resolved photoluminescence, photoluminescence quantum yield analysis, transmission electron microscopy, and powder X-ray diffraction. These studies confirmed that the treatment improved surface passivation without changing the overall nanocrystal morphology or core crystal structure. In a nutshell, this chapter offers a simple post-synthesis treatment strategy that can significantly reduce surface defects and improve the optoelectronic quality of CsPbBr3 nanocrystals.

Chapter 3

The third chapter deals with strategic compositional engineering in quasi-2D Ruddlesden–Popper perovskites for deep-blue emission. In this chapter, initial efforts are made to prepare 3D CsPbBr₁.₈Cl₁.₂ thin films to incorporate the highest possible chloride content, thereby shifting the parent perovskite emission to the lowest possible wavelength. Thereafter, quasi-2D Ruddlesden–Popper perovskites are derived from the CsPbBr₁.₈Cl₁.₂ parent 3D system, focusing on compositional engineering through the controlled addition of PEACl. The purpose of this chapter is to push the emission further into the deep-blue region while improving the film's optical quality.

As the PEACl content increases from 0% to 140%, the material gradually changes from a more 3D-like phase towards quasi-2D phases. This leads to a clear blue shift in the emission, from 477.5 nm at 0% PEACl to 443.5 nm at 120% PEACl, with optimal performance observed at 100% PEACl. At the same time, the PLQY increases from 0.075% to 16.3%, indicating that the transition to quasi-2D phases and the passivating effect of PEACl both enhance radiative emission. Beyond 100% PEACl, the PLQY decreases, attributed to reduced crystallinity and inhomogeneous halide concentration due to excess chloride. A notable point in this chapter is that all compositions show a single emission peak, suggesting efficient exciton funnelling from lower-n phases to higher-n phases. XRD, TRPL, AFM, SEM, TEM, and SAED collectively indicate that the 100% PEACl composition provides the best balance of emission wavelength, film quality, and stability, making it the best-performing sample in this study. This chapter, therefore, shows that compositional tuning can successfully shift quasi-2D perovskites into the deep-blue region while maintaining strong optical performance.

Chapter 4

The fourth chapter shifts from experiments to computation, presenting a machine-learning framework for quasi-2D perovskites. This part of the thesis uses a curated literature dataset and cheminformatics descriptors to predict emission energy and examine the limits of EQE modelling. The motivation for this chapter is that quasi-2D perovskites have a large and complex parameter space, and the experimental trial-and-error method is not efficient enough to explore it fully.

The workflow begins by collecting and cleaning reported data, then converting chemical structures into numerical descriptors, and finally selecting and training regression models to predict emission energy. For emission-energy prediction, after feature reduction, the thesis uses a set of regression models, including Random Forest, XGBoost, CatBoost, Gaussian Process Regression, and SVR. The best model obtained is SVR with SelectFromModel (a feature reduction technique), which reaches  R2of 0.953 and RMSE of 0.074 eV using 13 features. The chapter also includes model evaluation and interpretability using SHAP, which allows the identification of the most influential features behind the predictions. Consequently, the chapter not only provides predictive models but also offers chemical insight into the importance of certain compositions and descriptors over others.

On the other hand, device-level EQE are less predictable when modelled using similar literature inputs with additional device-level details, yielding a weak R2 of approximately 0.5–0.6 at best. Although the integration of transport-layer labels provides a modest performance benefit, physical film morphology and specific laboratory fabrication protocols and conditions determine overall efficiency. Therefore, the performance may vary from one laboratory report to another with the same set of recipes and device architectures. These insights establish that chemically lean ML models are accurate at predicting intrinsic material properties, but device-based metrics such as EQE remain fundamentally unlearnable across heterogeneous literature sources without strictly standardized fabrication and testing conditions.

A key value of this chapter is that it bridges materials chemistry and data science, making it useful for perovskite research. The study demonstrates that machine learning can help screen compositions, reduce trial-and-error experimentation, and guide future synthesis toward promising low-dimensional perovskite emitters. This chapter, therefore, complements the experimental chapters by showing how data-driven analysis can support rational materials design.

Conclusion

Taken together, the thesis shows that low-dimensional perovskites can be tuned effectively for optoelectronic applications through surface treatment, compositional engineering, and data-driven modelling. Chapter 1: builds the background and explains the scientific need of the work; Chapter 2: shows how post-synthesis treatment improves CsPbBr₃ nanocrystals; Chapter 3: demonstrates deep-blue tuning in quasi-2D perovskites through PEACl-based engineering; and Chapter 4: investigates how machine learning can be used to predict emission trends and interpret composition–property relationships. Overall, the thesis contributes to the development of efficient, stable, and colour-pure perovskite emitters and demonstrates how experimental chemistry and machine learning can work together to advance materials discovery.

The thesis also aligns well with SDG 7: Affordable and Clean Energy and SDG 9: Industry, Innovation and Infrastructure, as it contributes to the development of efficient lighting materials and demonstrates a data-driven approach to faster materials discovery.

Publications

- Ranadeep Raj Sumukam, R. Nie , S. H. Reddy, M. Banavoth, and S. I. Seok, “Lead-free perovskite solar cells enabled by hetero-valent substitutes,” Energy & Environmental Science, 2020, 13(8), 2363–2385.

- Gundam Sandeep Kumar, Ranadeep Raj Sumukam, and B. Murali, “Quasi-2D perovskite emitters: a boon for efficient blue light-emitting diodes,” Journal of Materials Chemistry C, 2020, 8(41), 14334–14347.

- Ranadeep Raj Sumukam, Gundam Sandeep Kumar, R. K. Rajaboina, R. N. Savu, M. Srinivas, et al., “Perovskite nanowires for next-generation optoelectronic devices: lab to fab,” ACS Applied Energy Materials, 2022, 5(2), 1342–1377.

- Ranadeep Raj Sumukam, S. H. Reddy, and B. Murali, “Can perovskite-inspired bismuth halide nanocrystals outperform their lead counterparts?”, Journal of Materials Chemistry A, 2020, 8(26), 12951–12963.

- R. Ketavath, L. Mohan, Ranadeep Raj Sumukam, Q. A. Alsulami, A. Premalatha, and B. Murali, “Can perovskites be efficient photocatalysts in organic transformations?”, Journal of Materials Chemistry A, 2022, 10(23), 12317–12333.

- Ranadeep Raj Sumukam, Gundam Sandeep Kumar, R. N. Savu, and B. Murali, “Strategic Compositional Engineering in Quasi-2D Ruddlesden–Popper Perovskites to Decipher Deep Blue Emission,” The Journal of Physical Chemistry Letters, 2023, 14(2), 395–402.

- Ranadeep Raj Sumukam, Puspanjali Sahu, R. N. Savu, S. J. Khanam, Q. A. Alsulami, and M. Banavoth, “Halide Ions Distribution and Charge Dynamics in Mixed-Halide Perovskites,” physica status solidi (RRL) – Rapid Research Letters, 2022, 16(5), 2100576.

- Ranadeep Raj Sumukam, Ramu Naidu Savu, Santhosh Rompivalasa and Banavoth Murali, “Cheminformatics and Machine Learning for Quasi-2D Perovskites: Emission Energy Prediction and the Limits of EQE Modelling”, (2026), Manuscript under review.

Conferences attended

- Poster Presentation, titled “Strategic Compositional Engineering in Quasi-2D Ruddlesden–Popper Perovskites to Decipher Deep Blue Emission” in the 3rd International Conference on Nano Materials for Energy Conversion and Storage Applications – 2024 at PDEU Gandhinagar, Gujarat, India. (Best Poster Presentation Award)

- Oral and Poster Presentation, titled “Strategic Compositional Engineering in Quasi-2D Ruddlesden–Popper Perovskites to Decipher Deep Blue Emission” in the 20th Annual In-House Symposium CHEMFEST-2023 at UoH Hyderabad, Telangana, India. (Best Oral Presentation Award)

- National Workshop on Advanced Material Characterization Techniques (NWAMCT-2018), held on 31st August 2018, conducted by the Department of Physics-2018, Osmania University (OU),Hyderabad, Telangana, India.

- Energy Materials and Innovative Challenges and its Applications, held on 6th - 10th October 2018, conducted by JNTU-(GAIN-2018)-Hyderabad, Telangana, India.

- Short Course on Spectroscopic Ellipsometry, held on 4th - 5th November, 2019, conducted by JNCASR, Bangalore, Karnataka, India.