Low-Dimensional Perovskites Optoelectronic Properties: Leveraging Practical and Data-Driven Machine Learning Approaches

1.1 Need for Exploring Advanced Emissive Materials

The historical trajectory of artificial illumination and display technologies is defined by a continuous evolution over the years from thermal incandescence to quantum-managed solid-state physics. For more than a century, the lighting industry relied on the incandescent lamp, which converted resistive Joule heating into a broad thermal emission spectrum, and the fluorescent tube, which leverages plasma-excited mercury vapour to pump phosphorescent coatings into green-biased white emission.[1] Both technologies were transformative in their period, but neither was efficient. The late 20th-century commercialisation of the Light Emitting Diode (LED) has led to a paradigm shift. By exploiting electron-hole recombination in inorganic/organic semiconductor materials, LEDs bypassed the thermodynamic bottlenecks of filaments and fluorescent tubes. LED’s working mechanism and generic device architecture are shown in Figures 1.1(a) and 1.1(b), respectively. This scalable semiconductor architecture has paved the way from the spatial illumination to digital displays, optical communication, and biomedical imaging, thereby fostering the industrialisation of modern optoelectronic technologies.[2] As fabrication techniques advanced, LEDs evolved from primitive dashboard indicator lights into the back lighting of modern liquid-crystal displays (LCDs), Organic LEDs (OLEDs), and high-density pixel backbones for emerging Micro-LED systems. Today, advanced solid-state photonics caters to all global lighting and display applications and constitutes a multi-billion-dollar industry.

In 2024, the International Energy Agency (IEA) estimated that approximately 8% of global electricity demand, which is around 2,200 TWh, was consumed by lighting in buildings and outdoor applications alone. When industrial and agricultural lighting is included, broader estimates range from 2,500 to 3,500 TWh annually. Over the past two decades, the LED revolution has already produced measurable efficiency gains, driven by global LED market penetration in building lighting rising from 17.6% in 2016 to 50.5% in 2022.[3] The chart in Figure 1.1(c)  from the IEA comparing energy consumption in the year 2014 and 2024 clearly shows that the adoption of LEDs has kept energy consumption in control over the decade. If lighting technology efficacies (lm/W) and market shares had remained constant worldwide over the past decade, annual residential lighting electricity consumption would be more than 500 TWh higher today. However, the ceiling of what solid-state emitter technology should deliver remains far above current performance. Modern display and lighting technologies are built around one central requirement that is to generate light of a specific colour at high brightness with minimal energy loss. For several decades, three main families of light-emitting materials have tried to fulfil those requirements: organic light-emitting diodes (OLEDs),[4, 5] conventional III-V inorganic LEDs based on gallium nitride (GaN) related compounds,[6, 7] and colloidal quantum dot LEDs (QLEDs) based on cadmium selenide (CdSe) or indium phosphide (InP) nanocrystals.[8, 9] Each of these material systems has delivered real progress in certain areas while falling short in others. None has fully satisfied the next-generation display standards for the Rec. 2020 colour standard (formally, ITU-R BT.2020) as shown in Figure 1.1(d) and the general illumination market, which require better-performing, efficient, and economical technology. Moreover, in conventional semiconductor systems like InP , GaAs, CdTe, and CdSe, even a small population of defects is extremely detrimental to their intrinsic photoluminescence quantum yield (PLQY), carrier mobility, and stability.[10] Given technological gaps and affordability constraints, there is room to further explore emissive materials, such as metal-halide perovskites, which are among the most promising alternatives. This thesis explores low-dimensional perovskite materials, such as zero-dimensional nanocrystals and quasi-two-dimensional layered perovskites (Q2DPe), for optoelectronic applications. In addition, because the parameter space is wider for Q2DPe, machine learning models were built to predict their emission energies.

Figure 1.1. (a) Schematics of the light emission mechanism inside an LED chip.[11]  (b) Schematic representation of the generic multilayer structure of the LED device.[12] (c) Bar graph: share of indoor lighting in buildings in electricity demand, 2014 and 2024.[3] (d) CIE 1931 chromaticity diagram showing the Rec. 2020 (UHDTV) colour space in the triangle and the location of the primary colours.[13]

1.2 Introduction to Metal Halide Perovskites

At first, the name “Perovskite” referred to CaTiO3, a mineral species which was discovered in 1839 by the German mineralogist Gustav Rose in the Russian Ural Mountains. It is named as “Perovskite” in honour of Russian mineralogist L. A. Perovski. Since CaTiO3 has the generic ABX3 crystal structure, all minerals with a similar crystal structure are referred as perovskites. Therefore, they are a broad family of materials defined by a crystal structure rather than a single chemical composition.[14] Among all types of perovskite counterparts, the solution-processed hybrid organic-inorganic lead halide perovskites (LHP), where A is a monovalent cation (MA, Cs, FA, Rb), B is divalent metal cation (Pb2), X is a halide (Cl, Br, I) in the ABX3 crystal structure as shown in Figure 1.2(a), have engrossed optoelectronics research owing to their exceptional photoelectric features. Their appeal in optoelectronics stems from the way relatively simple chemistry can produce remarkable properties such as strong light absorption, tunable band gaps, facile control of quantum and dielectric confinements, long carrier diffusion lengths, defect tolerance, and high photoluminescence efficiency.[10, 15] In LHPs, the band edges are shaped by the metal and halide orbitals in a way that often suppresses deep electronic trap states, which makes them defect-tolerant and perform well even from solution-based synthesis and not grown as perfect single crystals, unlike defect-intolerant conventional semiconductor materials (Figure 1.2(b)).[10, 16, 17] As a result, perovskites have attracted research interest at the forefront of next-generation photovoltaic[18-20] and LED[21-24] applications. LHPs have emerged as promising active emitters, with near-infrared, red, and green-emitting perovskite LEDs (PeLEDs) advancing rapidly and achieving external quantum efficiencies (EQEs) exceeding 20%.[22-24] It is noteworthy that their low temperature and easy solution-processability facilitate the utilisation of low-cost solution-based techniques such as roll-to-roll processing, screen or inkjet printing, to fabricate the cost-effective large-area flexible display devices.[25-27]

Figure 1.2. (a) Lead halide perovskite crystal structure[28] and (b) comparison of defect-tolerant electronic band structure with defect-intolerant semiconductors.[29]

Despite the immense promise of bulk 3D perovskite thin films, their low exciton binding energies are a bottleneck for their practical usage as an efficient LED material. Due to their low exciton binding energy (in meV), injected charge carriers rapidly dissociate into free charge carriers and undergo non-radiative recombination at ambient temperatures. To circumvent these spatial recombination losses, researchers have pivoted towards dimensional downscaling, which enables manipulation of confinement, exciton behaviour, and environmental stability. By restricting the inorganic framework and inserting bulky organic cations, it is very facile to form nanocrystals (NCs), quantum wires, quasi-two-dimensional (quasi-2D) layers, and related low-dimensional structures that confine charge carriers more strongly than bulk 3D LHPs. This physical confinement usually increases exciton binding energy, sharpens emission, and can help control phase stability and color purity.[30-32]

1.3 Perovskite Nanocrystals

Perovskite NCs are an important low-dimensional material of the perovskite family because they combine the intrinsic advantages of LHPs with quantum confinement. In the nanoscale, the optical properties of LHP NCs are not only dependent on halide composition but also on their size due to the quantum confinement effect. A simple way to express the quantum-confinement idea is that when a crystal becomes comparable in size to the exciton Bohr radius in any dimension, excitons are spatially confined, and their continuous energy levels become more discrete; therefore, the optical gap becomes size-dependent. This allows LHP NCs to emit at different wavelengths even when made from the same underlying material. For device fabrication, this size-dependent tunability is significant, but it also makes reproducibility and stability more challenging, as surface states and ligand chemistry play crucial roles in performance.

1.3.1 Synthetic strategies of Perovskite Nanocrystals

The bottom-up synthesis of LHP NCs fundamentally relies on controlling the balance between nucleation and growth kinetics in the colloidal environment. To restrict this spontaneous crystallization of LHPs to the nanometer scale and prevent macroscopic precipitation into bulk phases, surface-capping organic ligands must be leveraged strategically. These capping molecules are typically long-chain alkyl carboxylic acids and alkylamines. They operate by reversible coordination mechanisms at the nanocrystal surface. In general, Oleic acid (OA) and oleylamine (OAm) are prominently used in combination to establish a dynamic acid-base equilibrium in solution, generating oleate anions (R-COO⁻) and alkylammonium cations (R-NH3⁺) that serve as coordinating species. There are several methods to synthesise LHP NCs. The most widely used methods are hot-injection, ligand-assisted reprecipitation (LARP), and post-synthetic methods.

If the requirement is to synthesise high-quality and narrow-size distributed NCs with decent reproducibility, then the hot injection method is considered the best. The hot-injection method is a traditional synthesis method for metal fluoride or chalcogenide NCs.[33] Kovalenko and coworkers used this technique to synthesise LHP NCs, CsPbX3 (X = Cl, Br, I, or halide mixture) for the first time in 2015.[34] In this synthesis technique, an A cation solution (Cs-oleate or methylamine) is prepared separately and injected into the hot solution containing metal salts and surfactants, which was dried under vacuum and heated up to 200 °C under nitrogen prior to injection. As the solution is injected, a rapid salt metathesis reaction occurs, forming metal halide perovskite NCs. Then, the reaction should be quenched immediately by placing the flask in an ice-water bath to prevent further growth of LHP NCs. In this technique, we can tailor the LHP NC’s sizes and shapes by varying the reaction temperature and time.

While the hot-injection technique delivers outstanding morphologically controlled LHPs, its high energy consumption and inert-gas requirements lead to elevated processing costs, thereby limiting its viability for scalable, industrial-scale manufacturing. To circumvent these limitations, the LARP technique has emerged as a powerful, room-temperature alternative that proceeds entirely under ambient atmospheric conditions. The LARP technique is a low-cost, scalable process suitable for fabricating both all-inorganic and hybrid organic-inorganic PNCs.[14] In a typical LARP process, the perovskite ionic precursors, such as caesium halides (CsX) or organic ammonium salts CH3NH3X, along with lead halides PbX2 are completely dissolved alongside an optimised blend of organic capping ligands into a highly polar solvent. This primary carrier solvent is typically N,N-dimethylformamide (DMF) or dimethyl sulfoxide (DMSO), which possess exceptionally high dielectric constants capable of coordinating and solvating the ionic perovskite compounds into stable precursor monomers. This polar precursor mixture is then added dropwise or injected, under vigorous stirring, into a much larger volume of a nonpolar antisolvent, such as toluene or hexane. Since DMF is completely miscible with toluene, the polar carrier solvent rapidly diffuses out into the non-polar matrix. This sudden solvent migration abruptly strips away the protective solvation shells surrounding the dissolved ions, driving the increase in local monomer concentration to critical supersaturation limit. This rapid drop in solubility triggers a massive, spontaneous nucleation burst of LHP NCs at room temperature. It is noteworthy that the rapid nature of this diffusion-controlled precipitation typically results in broader particle size distributions and reduced batch-to-batch morphological reproducibility in comparison to hot-injection.

Other less-used techniques include the tip sonicator method[35] and the continuous flow methods[36], as shown in Figure 1.3. Post-synthetic methods are primarily developed to tune the optical properties and improve the stability of NCs in both the solid and liquid states. Various post-synthetic methods include surface passivation, cationic, and anionic exchange. The anion-exchange strategy is a method for synthesising one type of halide perovskite NCs from another type of halide perovskite NCs. Here, the desired halide (X) source solution is prepared by adding OA–X to a polar solvent such as DMF, and the mixture is then added swiftly to the existing NCs.[37]

Figure 1.3. Schematic illustration of the various synthetic methods of colloidal NCs.

1.3.2 Surface Chemistry and Defects in Colloidal Perovskites.

In LHPs, surface chemistry plays a critical role in determining the stability and optoelectronic properties. Especially for NCs, although their nanoscale size confers quantum-mechanical properties, they exhibit increased sensitivity to surface chemistry and interface defects because their surface-to-volume ratio is higher. As mentioned in the synthesis section, the combination of long-chain acids (OA) and long-chain amines (OLA) is used as ligands in the synthesis of colloidal LHP NCs.  In that base-acid pair, ammonium cations (R-NH3+) and carboxylic anions (R-COO⁻) will be formed by the proton exchange from the acid (R-COOH) to the amine (R-NH2). Thereafter, as shown in Figure 1.4, ammonium cations tend to occupy the ‘A’ site positions on the LHP NC surface. Based on practical and theoretical studies, ~50% of the ‘A’ cations on the surface are replaced by ammonium cation ligands, which help to establish the colloidal stability of LHP NCs.[38, 39] On the other hand, the role of carboxylate anions in the colloidal stability of LHP NCs is still under debate. There are different views regarding the role of carboxylate anions. Few reports say that R-COO− ions do not bind to the NC surface, but form an equilibrium with surface-bound R-NH3+ ions to maintain charge neutrality that is essential for the colloidal stability of LHP NCs.[39] In contrast, few studies have shown that both oleylamine and oleic acid ligands bind to the surface of LHP NCs. The hypothesis is that long-chain R-COO− anions replace some of the surface halides and fulfil the octahedral coordination of lead, thereby passivating the mid-gap defect states (Figure 1.4).[40] In addition, amine-free synthesis methods were reported in which the NCs were capped solely with oleic acid, yielding oleate-terminated surfaces.[41] It is worth mentioning that the surface is properly passivated only in the presence of excess free ligands in the colloidal solution, as the long-chain ligands binding to an LHP NC surface are highly labile towards detachment. As the interactions between the NC surface and ligands are highly dynamic, purification and ageing processes can lead to surface defects that eventually reduce PLQY.[42] Therefore, understanding and controlling this ligand detachment mechanism is vital to the performance and stability of these materials. In this case, the binding affinity of the capping ligand for the LHP NC surface is the primary parameter to be tailored. Few studies have leveraged zwitterionic ligands, which significantly improve the stability of NCs by tightly binding to their surfaces. As shown in Figure 1.4, it is claimed that in the zwitterionic molecules, ammonium cation occupies the ‘A’-site position, while the sulfonate or carboxylate groups bind to uncoordinated Pb to complete its octahedral coordination.[43]

Figure 1.4. Schematic illustration of the LHP NCs with capping ligands and an enlarged view of the NC surface with defects and different types of surface ligands used for the stabilisation.[44]

Inherently, LHP NCs have defects similar to those in bulk perovskites. In addition, they undergo ligand desorption, which creates surface vacancies. To address this issue, a wide range of post-synthetic passivation strategies have been developed to enhance their PLQYs and stability. In general, formation energies in different charge states are used to study the defects. The point defects in the bulk form shallow traps, attributed to their low formation energy. On the other hand, surface halide vacancies create deep traps and can significantly affect nonradiative recombination rates, depending on the halides in the system.[44] When oleylammonium ion get detached from the NC surface, it will take a counterion to preserve charge neutrality. If the oleate ions are absent, then halide ions are the available options, which will cause further halide vacancies.[39, 42, 45] Nenon et al. have demonstrated a composition dependent relationship between surface halide vacancy concentration and PLQY with a dilution experiment to induce controlled halide vacancies by shifting the ligand pair equilibrium towards free species. They have observed a trend in which the impact is low for CsPbI3, moderate for CsPbBr3, and prominent for CsPbCl3 NCs (Figure 1.5(a)). It is worth noting that in all three cases, halide vacancies were created, as confirmed by 1H NMR spectroscopy. This experiment shows a significant shift in defect tolerance in LHP NCs with respect to which halides are present in the system. Figure 1.4 clearly confirms that chloride-based LHP NC has lower defect tolerance, whereas surface halide vacancies have minimal impact on iodide-based LHP NCs. Ab initio calculations have supported the observation, wherein the chloride-based NCs, deep localised defects formed due to halide vacancies and in the case of bromide-based and iodide-based NCs, defect states are formed near the conduction band minimum as shallow defects (Figure 1.5(b)).[46]

Considering all the challenges with the dynamic surface chemistry of the LHP NCs, extensive research was done on the passivation ligands to improve the stability and performance (PLQY) of the NCs. Healing of the surface defect requires filling halide vacancies and forming a robust passivation layer around the NCs. Established principles of coordination chemistry must be considered when selecting effective passivating ligand pairs. Figure 1.5 (c) illustrates a few varieties of ligands that have been reported for the electronic passivation of LHP NCs.

Figure 1.5. (a) Absolute PLQY as a function of NCs concentration for CsPbCl3, CsPbBr3, and CsPbI3[46] (b) Transition level in the band gaps of CsPbCl3, CsPbBr3, and CsPbI3 NCs with halide vacancies. (c) Different types of passivation ligands that are used in the LHP NCs post-synthesis process.

1.4 Quasi-2D LHP for Deep Blue emission

LHP LEDs have progressed rapidly over the last few years, as mentioned in section 1.1 above; red and green LED devices have already reached external quantum efficiencies above 20%, establishing LHPs as a capable alternative for next-generation display and lighting technologies. However, blue perovskite LEDs remain the least mature branch of the field, lagging behind in efficiency, spectral stability, and operational lifetime because they are more vulnerable to defect-assisted nonradiative recombination due to their wider bandgaps. This problem is not a minor colour-specific limitation; rather, it is a technological bottleneck, since full-colour displays, high-resolution microdisplays, and balanced white-light generation all require a stable, efficient blue emitter, along with red and green light components.[47] [48]

From a materials perspective, this difficulty has gradually redirected attention away from treating blue emission as a simple extension of green or red perovskite design. In the case of NC systems, blue emission can be achieved by quantum confinement or halide-composition tuning, but these approaches often intensify surface sensitivity, as the surface-to-volume ratio increases further and, as discussed above, defect tolerance drops significantly in chloride-based NCs.[46]  In addition, from a device point of view, carrier injection will be impeded by insulating ligand shells, thereby aggravating spectral instability under electrical bias.[48] Therefore, the need of the hour is no longer merely to widen the bandgap, but to do so in a way that preserves transport and sustains spectrally pure electroluminescence. Considering all the challenges associated with LHP NCs, quasi-2D perovskites (Q2DPes) emerged as a more compelling blue-emission-active material. Their layered structures provide built-in dielectric and quantum confinement, enhanced exciton binding, and a multiple-quantum-well-like energy landscape that can favour efficient radiative recombination without relying exclusively on extreme size reduction. At the same time, the bulky organic spacers in quasi-2D frameworks offer an additional degree of control over phase distribution, defect passivation, and lattice rigidity.[31]

1.4.1 Layer-structured Q2DPes

Additional bulky organic cations (BOCs) (Aʹ) have been introduced into 3D perovskites (ABX3) for the formation of layered perovskites (Aʹ2An-1BnX3n+1), where Aʹ is a monoamine BOC, n is a stacked inorganic octahedron (PbX6)4–: n=1 are two-dimensional (2D) LHPs, n=2,3,4… are the Q2DPes (Figure 1.6 (a)), and n= are the conventional 3D LHPs.[49] Structurally, the BOCs are connected to the inorganic (PbX6)4– octahedra of perovskites through hydrogen bonding between the amine groups and halides. Additionally, the van der Waals interactions between the tails of bilayer BOCs form a spacer. The resultant structure is an inorganic (PbX6)4– octahedra sandwiched between the bilayers of BOCs, known as Ruddlesden-Popper (RP) phase Q2DPes.[49] Instead, the organic spacer between the perovskite sheets can be composed of a diamine BOC. The perovskite sheets are connected by the direct linkage of the diamine cation, thereby eliminating the van der Waals gap;  referred to as Dion-Jacobson (DJ) phase Q2DPes with the chemical formula AʹʹAn-1BnX3n+1, where Aʹʹ is a diamine organic cation.[50] The insulating nature of the organic spacers creates energetically high potential barriers on both sides of inorganic octahedra, resulting in the formation of a quantum well structure consisting of inorganic layers with low bandgap and high dielectric constant (εw), and the spacer cation barrier with high bandgap and low dielectric constant (εb) (Figure 1.6 (b)).[51] Consequently, the charge carriers are confined strongly within the inorganic octahedra of the perovskite framework and increase/tailor the exciton binding energies through the dielectric and quantum confinement effects.[51] Furthermore, the hydrophobic nature of the spacer cations isolates the inorganic octahedra from external moisture and oxygen, and enhances the stability of the resultant layered perovskite structures.[49, 50]

The striking optoelectronic properties of Q2DPes are tailored by modulating the widths of both the inorganic octahedral layer and the organic spacer. The promising strategies include engineering the perovskite layer composition, various size-dependent BOCs and dielectric constant, and regulating the number of layers (n = 2, 3, 4, etc.).[49, 51] The compositional engineering entailed by incorporation of mixed A-site cations, caesium (Cs), methylammonium (MA), formamidinium (FA), and mixed BOCs, phenylethylammonium (PEA), iso-propylammonium (IPA), butylammonium (BA) allows the flexibility to ameliorate the structural, optical properties and its stability (Figure 1.6c).[52, 53] The number of layers in Q2DPes can be reduced by increasing the stoichiometric ratio of BOCs to A-site cations (Aʹ/A) in the precursor solution. As the number of layers decreases, the corresponding energy bandgap increases [52], thereby enhancing the ability to regulate efficient emitters in the blue region by optimising the number of layers in Q2DPes, which were previously difficult to prepare from conventional 3D or nanostructured perovskites. However, achieving the phase purity (constant n value), i.e., homogeneous distribution, is arduous. Most reports documented that Q2DPe thin films prepared from mixed-cation compositions exhibit a heterogeneous distribution, i.e., a mixed phase (a combination of different n values).[54, 55] The heterogeneous distribution leads to the presence of dissimilar energy band gaps and corresponding conduction/valence band energy levels. In this scenario, charge-carrier excitation occurs in the high-bandgap (lower-n phase) region. Due to the presence of an energy bandgap or energy level gradient, the charge transfer occurs from the lower n phase to the higher n phase on a picosecond timescale through the phenomenon of exciton funnelling, where the effective radiative recombination ensues (Figure 1.6 (d)).[55] The ultrafast charge transfer through exciton funnelling can surpass the nonradiative recombinations at the grain boundaries and surface defects that exist within the high bandgap phase, thereby improving the overall PLQYs.[56, 57] The energy landscape colour-gradient representation illustrates the charge transfer process between the heterogeneous phases (each colour indicates a different n value) present within the thin-films, i.e. from lower n region to higher n region (Figure 1.6 (e)). However, a major challenge exists to achieve the deep blue emission and colour purity by limiting the extent of exciton funnelling to large n within the broad n distributed heterogeneous phase of Q2DPe thin-films.

The Q2DPe thin-films can be easily prepared by spin-coating the perovskite precursor solution onto the target substrates. The size distribution, orientation, and packing density of the layered perovskites within the thin-film can be controlled through the additional solvent or additive engineering during the spin-coating process (Figure 1.6 (f)). The orientation of the layered perovskites may be random, vertical, or horizontal (Figure 1.6 (g)), depending on processing conditions and the solvents used. Mixed DMSO/ DMF solvent engineering promotes the formation of one intermediate complex, and further annealing induces the perovskite growth in one direction with a preferred vertical orientation.[58] Recent reports have demonstrated the fabrication of blue LEDs from Q2DPes through various strategies, including compositional engineering, processing conditions, and solvent engineering.[59-64]

Figure 1.6. Schematic illustration of: (a) Unit cell of cubic 3D perovskite crystal structure and layered structure of Q2DPe with different phases from n = 1 to n = 4. (b)  Single-quantum well structure of Q2DPe; inorganic octahedra sandwiched between the barriers of organic spacers. (c)  Compositional engineering of Q2DPe by using bulky organic multi-cations, A-site multi-cations, and mixed halides. (d) Charge transfer or funneling of excitons between Q2DPe of small n to large n phase through energy band diagram. (e) Schematic energy landscape of the Q2DPe with different n phase. (f)  Preparation of Q2DPe thin-films via spin-coating method. (g)  Orientation (Random, Vertical, and Horizontal) or growth of the layers in Q2DPe thin-film.

1.4.2 Recent progress on Q2DPe blue emitters and blue PeLEDs

1.4.2.1 Compositional engineering

The recent remarkable improvements in the performance and stability of Q2DPe-based blue LEDs compared to their 3D counterparts are due to their striking optical properties and tunable exciton binding energies arising from the regulation of the number of inorganic octahedra layers (n). The first 2D perovskite-based blue LED ((PEA)2PbBr4, n = 1) was prepared using PEA as the BOC.[60]  These 2D perovskites form a single quantum well structure, where the charge carriers are strongly confined in the inorganic octahedra of the perovskite framework and exhibit very large exciton binding energies. These devices exhibited meagre performance, with a maximum EQE of 0.04% at 410 nm, limited by strong phonon scattering and exciton-phonon coupling.[60] Considering the poor efficiencies in both pure 2D perovskites (n = 1) and conventional 3D perovskites (n = ), new strategies have been developed to combine the colour purity of 2D perovskites with the high electron mobility and conductivity of 3D perovskites into a single system. Therefore, Q2DPes are devised by tailoring the number of layers to tune exciton binding energies and emission spectra, thereby producing efficient, bright, and stable blue emitters.

To achieve the efficient blue emission, two strategies have been developed: a) through the precise regulation of the ratio of mixed halides (Cl/Br)[53, 54, 59, 61, 65, 66] (Figure 1.7 (a)), b) size-dependent quantum confinement (small n = 2,3,4…) effect[55, 57, 59, 61, 63, 67, 68] through the utilisation of the rationalised amount of BOCs (Figure 1.7 (b)) in the precursor solution. The first Q2DPe blue emitters (BA2MAn−1Pbn(Br/Cl)3n+1) were prepared from the MA and BA cations with an appropriate ratio to tailor the number of layers to tune exciton binding energies/adjust the exciton confinement effect accompanied by the mixed-halide (Br/Cl) ratio of 7:3. The Q2DPe thin-films exhibited a uniform morphology, dense packing and better quality as compared to the conventional 3D perovskite counterparts.[61] The corresponding blue perovskite LED exhibited an EQE of 0.01% at 468 nm.[61]

Blue emission from Br-only Q2DPe films was produced by incorporating the amine-based small molecule, such as 2-phenoxyethylamine (POEA)[69] and ethylammonium (EA)[70] BOCs into the MAPbBr3 system, which induced the quantum confinement effect. The PeLEDs displayed  maximum EQEs of 0.06%, 1.1%, and 2.6% at 462 nm, 480 nm,[69] and 485 nm,[70] respectively. Similarly, LEDs designed from BA2Csn−1Pbn(Br/Cl)3n+1[54] and PBA2Csn−1Pbn(Br/Cl)3n+1[59] Q2DPes have achieved maximum EQEs of 2.4%, 6.2%, and  0.52% at 467 nm (blue), 487 nm (sky-blue) [54], and 490 nm[59], respectively. These reports established that the stoichiometric ratio of the BOCs to the A-site cations in the precursor solution strongly influences the formation and phase distribution in the resultant Q2DPe thin-films. Increasing the ratio results in the formation of lower-n phases, and vice versa.

Numerous reports showed that the presence of mixed (n = 1, 2, 3 ,4, 5….) phases in the resultant perovskite thin-films, i.e. the presence of 2D perovskites (n=1) as well as Q2DPes (n = 2, 3, 4..). [54-57, 61] Subsequently, efficient cascade charge transfer (exciton funnelling) between the different n phases has been observed, i.e., the excitons in the lower n phase are efficiently transferred to the higher n phase and result in a dramatic improvement in their PLQYs.[57] Incorporation of an excess amount of BOCs or an increased ratio yields Q2DPes with lower n phases, favouring deep-blue emission through the strong quantum confinement effect.[63, 71] Nevertheless, due to the low formation energies of higher n phases[72], the resultant Q2DPe thin-film contains the inhomogeneous phase distribution. The formation probability of lower phases  (n = 1, 2)  increases with excessive BOCs, leading to the incomplete charge transfer from the n = 1 phase to the higher n phase[73], due to their very large exciton binding energies (320 meV).[74] As a result, emission occurs from both the lower-n and higher-n phases, producing multiple emission peaks in the spectrum and leading to colour impurity.[73] Hence, it is essential to achieve the desired and intermediate n-phase distribution by suppressing both the n=1 and n>4 phases in the resultant Q2DPe thin-films to achieve the narrow spectral pure blue emission.

Figure 1.7. (a) Normalised PL spectra of Q2DPe thin-films (PBABr:CsPbBrxCl3−x) with increased chloride content from 0 to 50% (from right to left).[59] (b) Blue PeLED’s energy band diagram and corresponding energy level positions of Q2DPes with increased content of PEABr from 0 to 120%.[63] (c) Tunable PL emission spectra of Q2DPes composed of PEA2IPA1.5Pb2.5Br8.5 with different percentages of IPABr additive (0−60%). The inset shows digital photographs of the corresponding thin films under 365 nm excitation.[52] (d) Formation energies of Q2DPes prepared from the BOCs PEABr, IPABr, and their mixture consisting of different n values. The inset shows the quasi-2D perovskite (n = 3) with PEA/IPA, and a digital photograph of the operating PeLED.[52] (e) Schematic illustration of the possible arrangement of bulky organic and short-chain multi-cations within the Q2DPe.[75] (f) Schematic representation of Q2DPes structures with different monovalent and divalent BOCs and their interaction with the consecutive inorganic octahedra layers.[73] (g) Schematic illustration of low-dimensional components engineering for achieving the narrow domain concentration to obtain the desired blue emission.[73] (h) Digital photographic images of Q2DPe thin-films with different BOCs and their combination under the irradiation of 365 nm UV light (left), and working PeLED at applied bias voltage of 5V (right).[76] (i) Schematic illustration of the spin-coated Q2DPe thin-films with and without doping and the variation in their thin-film morphologies.[53] (j) Digital photographic PL images of perovskite thin-films doped with different cations under the excitation of 380 nm.[53] (k) Multilayer PeLED device configuration with a pair of thin LiF layers at the perovskite interface.[53] (l) Recorded EL spectra of blue PeLEDs operating under different bias voltages from 4V - 10V. The inset shows the digital photographic image of the operating PeLED.[53] (m) Recorded PL spectra and PLQYs of Rb0.6Cs0.4PbBr3, pristine, and RbBr-rich Q2DPes of 〈n〉Rb0.6 = 3 thin-films. The inset shows a digital photographic PL image of RbBr-rich Q2DPe thin films under UV irradiation.[77] (n) EQE vs current density curves of PeLEDs with pristine and RbBr-rich Q2DPes. The inset shows a digital photograph of the working PeLED.[77]

Given the significance of the intermediate (desired n) phase for achieving narrow, pure blue emission in the specific wavelength region, mixed dual BOC strategies have been developed.[52, 73, 75, 78, 79] Where Q2DPes were prepared from the phenethylammonium bromide (PEABr) by combining with the additional cations, such as iso-propylammonium bromide (IPABr), ethylammonium bromide (EABr), n-propylammonium bromide (PABr) and butylammonium bromide (BABr) organic cations to regulate the phase and improve the emission properties.[52] Systematic investigations revealed that the combination of PEABr and IPABr resulted in high PLQYs from the (IPA/PEA)2(MA/Cs)n−1PbnBr3n+1 Q2DPes, and increased IPA content led to the blue-shifted emission spectra (Figure 1.7 (c)).[52] Here, the IPA was utilized to slow down the crystallization of unwanted n = 1 phase by concentrating the monodispersed and desired phases (n = 2,3,4..), since IPA has a reduced van der Waals force, is believed to have suppressed the formation of n=1 phase. The small amount of PEA facilitates the formation of higher n phases. From the precise regulation of the ratio of PEA/IPA cations, the desired and highly concentrated phases (n = 2, 3, 4) have been obtained. Formation energies of the Q2DPe with different n phases designed from individual and mixed BOCs (IPA, PEA) are shown in Figure 1.7 (d). The corresponding PeLEDs have produced a maximum EQE of 1.9% at 490 nm.[52] The devices displayed sky-blue emission, caused by the presence of broad and intermediate phase distribution (n= 2,3,4,5), which led to red-shifted emission spectra via exciton funnelling.[52]

The Q2DPes have been prepared from the combination of bulky and short-chain ligands, such as dimethylammonium (DMA)+BA and DMA+PEA (Figure 1.7 (e)).[75] BOCs (PEA, BA) capped the inorganic octahedra and hence limited the formation of higher n phases within the Q2DPe thin-films.[75] Accommodating the short-chain cations (DMA) with its relatively small positive charge and weak coordination suppressed the formation of n = 1 phase, and improved the charge injection efficiency and successive transportation within the Q2DPe thin-film of PeLEDs.[75] Additionally, a short-chain cationic DMA, in combination with the BOCs (PEA, BA) at a precise ratio, regulates the desired n-phase and improves the charge injection and transport properties of Q2DPe thin films due to their higher conductivity than the BOCs.[75] The PeLEDs fabricated from the only Br halide-based  BA2DMA1.6Cs2Pb3Br11.6 and PEA2DMA1.2Cs2Pb3Br11.2 Q2DPes showed maximum EQEs of 2.4% at 490 nm (sky-blue) and 1.58%  at 499 nm (bluish-green).[75]

Typical organic spacers (BA, PEA) used in Q2DPes are inhomogeneous and unstable.[73] Existence of weak interaction between these BOCs and inorganic octahedron of the Q2DPe framework lead to the growth of higher n phases from the smaller n phases during the thermal annealing and ageing of the thin-films for several hours in moisture, radiation and ambient conditions.[73] The formation of higher-n phases reduces the bandgap and results in red-shifted emission spectra, thereby hampering the pure blue emission of Q2DPes. Hence, developing strategies to achieve a stable, narrow/desired n phase distribution in Q2DPe thin films is crucial for producing efficient, stable blue emitters and corresponding high-performance blue PeLEDs.

To achieve the narrow phase distribution and phase stability, diamine BOC (P-PDABr2 (1,4-Bis(aminomethyl)benzene bromide)) is used in combination with the monoamine BOC (PEABr) for the preparation of stable Q2DPe blue emitters (Figure 1.7 (f)).[73] The P-PDA cation with double functional amido terminals on both ends provides a strong binding force by directly connecting the two inorganic octahedra layers, and leads to the formation of stable lower n phases.[73] In contrast to the monoamine cations, the P-PDA-based Q2DPes exhibited improved phase stability under external conditions such as temperature, moisture, and UV irradiation, and produced the concentrated n = 1 and 3 phases.[73] With the introduction of PEABr, the formation probability of the n=2 phase was enhanced considerably and the formation of the n=1 phase was dramatically suppressed.[73] The precisely controlled ratio of P-PDABr2/PEABr (3:1) produced the desired and concentrated narrow n = 2, 3 phase distribution in the Q2DPe thin-films (Figure 1.7 (g)). Optimisation of concentrated phase distribution promoted the exciton transfer from n=2 to n=3 phase. The charge carriers recombined radiatively, producing strong blue emission solely from the n = 3 phase, accompanied by improved PLQYs.[73] The PeLEDs displayed a stable blue emission with a maximum EQE of 2.6% at 465 nm.[73] Analogously, the combination of monoamine  - PEABr and diamine - N-(2-Bromoethyl)-1,3-propanediamine dihydrobromide (NPABr2) BOCs has been utilised to modulate and amplify the resultant emission and phase stability in the blue emissive region.[79] The independent PEA and NPA cation-based Q2DPe thin-films have exhibited the emission at 508 nm and 478 nm, respectively (Figure 1.7(h)).[79] The Q2DPe thin-films prepared from the combination of both the organic cations PEA+NPA produced the uniformly concentrated n = 2, 3 phases and showed the resultant emission at 482 nm.[79] Corresponding PeLEDs designed from the only Br halide-based PEA2NPA1Cs2Pb3Br12 Q2DPe  exhibited a maximum EQE of 2.62% at 485 nm and showed the applied bias independent spectral stability.[79] The presence of PEABr remarkably increased the PLQYs of Q2DPe thin-films, whereas the NPABr2 favoured the formation of narrowed phase distribution with blue-shifted emission spectra; consequently, the sky-blue emission with improved PLQY has been achieved.[79]

1.4.2.2 Passivation and doping in Q2DPes

Low-temperature solution-processed perovskite thin films exhibit poor morphology. It further increases the probability of high defect density at the grain boundaries and/or within the crystal structure, which is almost inevitable. The presence of defect density increases nonradiative recombination.[80] In particular, the defect density is prominent in wide-bandgap blue emitters, thereby reducing overall PLQYs.[80]

To improve both the efficiency and stability of the Q2DPes, a multi-cation (Cs/FA/PEA/Rb/K) strategy has been developed, resulting in the high-quality uniform thin-film morphology (Figure 1.7 (i)) and reduced defect density.[53] Each cation used in this composition has played a consequential role in scoring the high-performance blue PeLED devices. Rb doping greatly modified the crystal growth orientation, improved the thin-film morphology, enhanced the PLQYs, and blue-shifted the emission spectra due to an increased bandgap caused by octahedral tilting.[53] The inclusion of PEA/K cations played an important role in reducing the trap-state density by passivating defect states at the grain boundary and surface, thereby enhancing the PLQYs.[53] The introduction of FA cations increased the current density in PeLEDs by improving thin-film conductivity.[53] Optimising the content of the multi-cations resulted in reduced grain size, smooth and pin-hole free improved thin-film coverage with enhanced PLQYs(Figure 1.7 (j)).[53] Besides, the multi-cation strategy pronouncedly reduced the large band offset from 1.28 eV for CsPb(Cl/Br)3 perovskite nanocrystals to 0.86 eV for (Cs/Rb/FA/PEA/K)Pb(Cl/Br)3 Q2DPes, which promoted the efficient hole charge injection due to reduced band offset.[53] The PeLEDs fabricated with the insulator lithium fluoride (LiF)/Q2DPe/LiF structure (Figure 1.7 (k)) suppressed the luminescence quenching at the interface, showed the maximum EQE of  2.01% at 484 nm and improved device half-lifetime of 300 minutes under continuous operation.[53] Propitiously, the PeLEDs withstand up to the operating voltages of  14 V implying the robust durability of the devices prepared from the multi-cation strategy.[53] The recorded electroluminescence (EL) spectra at various bias voltages (4V – 10V) shown in Figure 1.7 (l). Nevertheless, the PeLED devices also showed a spectral shift of 8 nm under continuous operation, due to the ion migration and phase segregation under the applied electric fields.[53]

All inorganic A-site multi-cations (Rb-Cs) and exclusive Br halide-based alloyed Q2DPe blue emitters (PEA2(RbCs)Pb3Br10) have been developed to improve the PLQY and ambient stability.[77] The insertion of pure inorganic A-site cations (Cs, Rb) appreciably improved the spectral stability of the Q2DPe. Furthermore, the rubidium bromide (RbBr)-rich compositional engineering increased the overall PLQYs up to 82% (Figure 1.7 (m)) by reducing the deep trap states through the in-situ passivation, produced very smooth and uniform thin-films of root mean square (rms) roughness less than 1 nm.[53, 77] Nonetheless, the excess cesium bromide (CsBr) induced the cation exchange, led to the red-shifted emission spectra.[77] Systematic study and comprehensive investigation confirm that the excess RbBr effectively passivates the defect states and improves the radiative recombination efficiency.[77] The unaltered stable PL spectra even after annealing for 4h at  100 C, indicated the excellent thermal stability of Cs/Rb-alloyed based Q2DPe.[77] The RbBr-rich PeLEDs (PEA2(Rb0.6Cs0.4)Pb3Br10) displayed blue emission (Inset of Figure 1.7(n)) with excellent spectral stability under various applied bias voltages and exhibited a maximum EQE  1.35% at  475 nm (Fig. 2n).[77] Here, the halide migration – spectral instability in mixed halide (Cl/Br) blue PeLEDs was completely circumvented by developing the efficient blue emitters from the only Br halide Q2DPe. Forbye, tailoring the RbBr content in the precursor solution demonstrated the ability to tune the emission color, and foster the efficient blue emitters and PeLEDs in the whole blue spectral region from 454 nm to 492 nm.[77] However, the PeLEDs produced marginal efficiencies in the deep blue region (0.13, 1.11, 1.22, 1.35% in 460 nm - 480 nm) compared to the sky-blue region (1.48% at 490 nm).

Figure 1.8. (a) Temperature-dependent conductivity measurements and corresponding fittings to calculate the IMAEs of mixed-halide perovskite thin-films of CsPbBr2.4Cl0.6, CsPbBr2.4Cl0.6 with 2% YCl3, and CsPbBr3:PEACl (1:1).[64] (b) Digital photographic PL images of perovskite thin-films with different YCl3 percentage under UV irradiation.[64] (c) Schematic illustration of the yttrium distribution within the CsPbBr3:PEACl:YCl3 thin-film and its effect on the bandgap modulation at the grain boundaries or surface.[64] (d) EQE vs current density curves of PeLEDs with different YCl3 percentages. The inset shows the digital photographic image of the operating PeLED.[64] (e) Schematic illustration of the possible mechanism of migration and immobilisation of Cl- halide in Q2DPes prepared from the conventional chloride-doping and treated with DPPOCl, respectively.[81] (f) Q2DPe LED’s energy band diagram and corresponding energy level positions of Q2DPe thin-films treated with DPPOCl of 10, 20 and 30 mg/ml.[81] (g) Schematic illustration of Q2DPe orientation within the thin-films through different thin-film processing conditions and possible charge transport mechanism.[82] (h) Schematic representation of the strategy to develop strong blue emissive Q2DPes by controlling the optimum phase through the interplay between the concentration of A-site and BOCs in the perovskite precursor solution. The inset shows the effect of the antisolvent on the phase distribution (right). The inset shows digital photographs of working PeLEDs with different compositions (left).[71] (i) Schematic representation of the recombination zone modulation for efficient blue emission.[63] (j) Current density and luminance vs voltage characteristic curves of PeLEDs designed with different PEDOT: PSS layer thicknesses. The dotted and solid lines correspond to current density and luminance, respectively.[63] (k) EQE vs current density curves of PeLEDs designed with different PEDOT: PSS layer thickness. The inset shows a digital photograph of a working PeLED at a constant applied voltage of 4.4V.[63]

To manipulate the advantage of Cl incorporation into the perovskites to achieve efficient deep blue emission and color tunability, it is pivotal to block the ion migration and phase segregation for obtaining the spectral stability and color purity. New strategies have been developed to prospect the ion migration activation energies (IMAEs) of the Q2DPes with different combinations of BOCs and additives. [64] The combination of the BOC phenethylammonium chloride (PEACl) and additive yttrium chloride (YCl3) in CsPbBr3 perovskites increased the IMAEs of the resultant perovskites from 0.26 eV (in CsPbBr2.4Cl0.6) to 0.75 eV (in PEACl:2%YCl3: CsPbBr3) (Figure 1.8 (a)), and also substantially increased the PLQYs (Figure 1.8 (b)).[64] Addition of YCl3 lead to the accumulation of more yttrium (Y) ions on the thin-film surface or at grain boundaries. Y-rich region acts as a shell for the perovskite grains by imposing an energetically high potential barrier, and strongly confines the charge carriers within the perovskite grains (Figure 1.8 (c)).[64]  The confined charge carriers isolate from the nonradiative recombination channels and high-defect density states, which commonly exists at the grain boundaries and on the thin-film surfaces, thereby improving the overall PLQYs. The PEACl:CsPbBr3: YCl3 based PeLEDs showed improved spectral stability in mixed halide (Br/Cl) system, ascribing to the marked suppression of ion migration and phase segregation effects through the increased IMAEs.[64] The PeLEDs with 2% YCl3 displayed the record EQE in the sky-blue emissive region of  11% at 485 nm (Figure 1.8 (d)). Increased content of YCl3 in the precursor solution resulted in the blue-shifted emission spectra. Further increasing the YCl3 to 5% and 10% reduced the PeLEDs EQE to 8.7% and 4.8% at 483 nm and 477 nm, respectively.[64] The increased content led to the formation of YCl3 clusters and may hinder the growth of the perovskite grains. Interestingly, it is worth mentioning that the shape and stable peak position of the EL spectra upon continuously operating the blue PeLEDs over 120 minutes under various bias voltages, revealed the enhanced spectral stability in mixed halide Q2DPes through the increased IMAEs.[64]

In addition, Cl insertion−immobilization strategy through additional organic chlorides has been developed to produce the spectrally stable Q2DPe blue emitters and blue PeLEDs by blocking the ion migration and phase segregation effect through the increased IMAEs.[81] The PEA2Cs1.6MA0.4Pb3Br10-xClx Q2DPes have been prepared from the compositional engineering and dynamically treating with the additional series of organic chloride components while preparing the thin-films via two-step spin-coating process.[81] The organic component diphenylphosphinic chloride (DPPOCl) is sensitive to water traces, inserts the in-situ immobilized Cl halide in the crystal structure by saturating the halide vacancies through the hydrogen bonding (Figure 1.8 (e)), and resulted in the blue-shifted emission spectra through the bandgap enlargement (Figure 1.8 (f)).[81] The Q2DPes treated with DPPOCl (30 mg/ml) exhibited an increased IMAE of 1.1 eV, is much higher than the conventional mixed halide (Cl/Br) Q2DPe (PEA2Cs1.6MA0.4Pb3Br7Cl3) of 0.7 eV.[81] Corresponding DPPOCl-treated blue PeLEDs displayed an EQE of 5.2% at 479 nm, showing no obvious EL spectral shift under operating conditions, and revealing an excellent spectral stability with an operating half-life time of  90 min at 100 cd/m2.[81] In contrast, the blue PeLEDs designed from the conventional mixed halides (Br/Cl) exhibited a small EL spectral shift under applied bias voltages due to ion migration and phase segregation.[81] Q2DPes treated with DPPOCl demonstrated the immobilisation of halides and suppression of the ion migration and phase segregation effect.[81] These reports demonstrated that increasing IMAE is an effective method to block ion migration and phase segregation in mixed-halide Q2DPes, thereby achieving spectral stability in efficient deep-blue PeLEDs.[64, 81]

1.4.2.3 Thin-film and interface engineering

Reduced NC or grain size eventually strengthens charge-carrier confinement and increases radiative recombination, thereby improving PLQYs.[82] To consummate it, a two-step spin-coating process is widely employed.[71, 82, 83] At first, the perovskite precursor solution is spin-coated onto the target substrates, followed by anti-solvent (chloroform, toluene, chlorobenzene with or without additives) dripping few seconds after the beginning of the initial spin-coating process. Dripping the antisolvent in the second step removes excess DMSO/DMF molecules and induces immediate crystallisation of perovskite NCs by reducing the solvent evaporation time, a process known as nanocrystal pinning (NCP).[82] In Q2DPe, during the spin coating process, DMSO/DMF molecules form a stack on (001) plane of inorganic octahedra and evaporate slowly. Crystal growth occurs primarily in the in-plane direction.[82] The directional growth of Q2DPe further hinders charge injection and transport due to the presence of insulating BOCs between consecutive inorganic octahedral layer frameworks. The NCP process was applied by dripping the toluene solvent to promote the random orientation of the Q2DPe crystals, which facilitates better connectivity between the inorganic octahedra layers and improves charge transportation.[82] During the NCP process, the toluene molecules instantaneously replace the DMSO/DMF molecules, which initiates the rapid crystallisation of perovskite layer crystals without any preferential growth direction, leading to the formation of randomly oriented crystals with reduced size and lower n phase  (Figure 1.8 (g)).[82] The PeLEDs prepared from the Q2DPe (PEA)2MAn−1PbnBr3n+1 with random orientation showed an improved device efficiency.[82]

In conjunction, solvent engineering (DMSO/DMF) and dripping toluene during the preparation of the Q2DPe thin-films induce faster nucleation and further reduce the formation of a broad n distribution.[71] The rationally engineered cation composition and crystallisation kinetics lead to the formation of the desired intermediate n phases with a narrow distribution and produce the strong blue emission (Figure 1.8 (h)).[71] The PeLEDs designed with only Br halide from this strategy showed efficient performance in tandem with the spectral stability, covering the broad blue emissive region with EQEs of  2.34%, 4.34%, and 5.08% at 465 nm, 486 nm, and 493 nm, respectively.[71] In addition, the integration of BOCs into the perovskites eliminated pinholes in the thin films, improved thin-film morphology, and enhanced PLQYs and PeLED efficiencies.[53, 63]

Recently, several reports have demonstrated the existence of vertically non-uniform distribution of perovskite layers in Q2DPe thin-film within the multi-layered PeLED device structures.[63, 84, 85] The layer thickness in LEDs determines the position of the effective recombination zone within the perovskite emissive layer, which is imperative to achieve efficient device performance (Figure 1.8 (i)).[63] The thickness of poly(3,4-ethylenedioxythiophene): poly(styrene sulfonate) (PEDOT: PSS) layer is regulated from 15 nm to 60 nm to optimize the position of the effective recombination zone.[63]  Q2DPes prepared by precisely regulating the composition of PEABr from 0-120%, tailoring the Cl/Br halide ratio. The blue PeLEDs with an optimum thickness of PEDOT: PSS  30 nm displayed a turn-on voltage of 3.2 V, the maximum luminance of 3780 cd/m2 (Figure 1.8 (j)) and EQE of  5.7% at 480 nm (Figure 1.8 (k)).[63] In contrast, the PeLEDs with PEDOT: thicknesses of 60 nm and 45 nm showed decreased performance, with maximum EQEs of 2.6% and 3.6%, respectively.  Due to the higher PEDOT: PSS thickness, the charge carriers relatively take longer time to reach the recombination zone A, and subsequently injects into the perovskite crystals within the weak emissive zone B (Figure 1.8 (i)), which reduces the overall device efficiency.[63] The effective recombination zone, when modulated and gradually shifted from the weak-emissive zone B to the strong-emissive zone A by controlling the PEDOT:PSS thickness, led to improved device performance.[63]

A guest-host system is used in place of exclusive Q2DPe thin-film, as the active emissive layer for the fabrication of efficient blue PeLEDs.[83] The active emissive layer is composed of quantum-confined perovskite nanoparticles embedded within Q2DPe phases with higher bandgaps achieved through the compositional engineering and followed by using the ethyl acetate as antisolvent (NCP process). [83] The resultant thin-films showed improved PLQYs (>60%) than the exclusive Q2DPe thin-films (38%). The increased concentration of phenylbutylammonium bromide (PBABr) in the precursor solution resulted in the blue-shifted emission spectra. The corresponding blue PeLEDs showed maximum EQEs of 9.5%, 6.3%, 4.8% and 4% at 483 nm, 478 nm, 476 nm and 474 nm, respectively.  This work establishes the improved PLQYs, efficient performances along with the spectral stability from the only  Br halide-based Q2DPe quantum-confined perovskite nanostructures blue PeLEDs.[83]

Along with the intrinsic issues, it is worth noting that blue PeLEDs suffer from poor charge injection and accumulation of charge carriers at the perovskite/hole transport layer (HTL) interface due to the deep VB position of wide-bandgap blue emitters and interface losses.[78, 86] To meticulously improve the charge injection efficiency and the radiative recombination within the perovskite layer, the LiF/perovskite/LiF structure is used for the fabrication of blue PeLEDs.[53] Additional LiF layer with controlled thickness at the Q2DPe interface is employed to induce and balance the charge injection into the Q2DPe crystals. The LiF layer at the indium tin oxide (ITO)/Q2DPe interface suppresses the luminescence quenching by reducing the energy band offset and interface losses.[53] The blue PeLEDs showed the maximum EQE of 2.01% and revealed the improved device lifetime (300 min) compared to the reference device (20 min). The improved device stability is mainly attributed to high-quality, uniform thin-film and to the inhibition of ion migration under the electric field by the pair of LiF layers at the Q2DPe interface.[53]

1.4.3 Challenges for Q2DPe blue emitters and blue PeLEDs

In the last two years, the Q2DPe blue emitters and blue PeLEDs have made considerable progress in their efficiencies. However, the mechanisms are yet to be explored; it requires much more effort for the optimisation and reproducibility of the methods to realise the efficient and stable performances of the blue PeLEDs. The large defect densities of wide-bandgap blue emitters act as nonradiative recombination centres, leading to poor PLQYs.  The applied large electric fields induce the ion migration and phase segregation, which lead to the red-shift of the EL spectra and spectral instability. The non-uniform distribution of the n (phase impurity) within the Q2DPe thin-film lead to the broad emission and red-shift of the emission spectra. The deep VB position of the perovskite blue emitters causes inefficient charge injection and accumulation at the interface. Hence, the blue PeLEDs are experiencing low EQEs and faster degradation. Therefore, in this section, we shed light on the challenges that need to be addressed to obtain efficient Q2DPe blue LEDs.

1.4.3.1 High defect densities and low PLQYs

The wide-bandgap perovskite blue emitters have been suffering from low PLQYs due to the formation of interband states that originate from the presence of defects on the thin-film surface or point defects that exist within the crystal structure. Interband states acting as nonradiative recombination centres reduce the overall PLQYs.[62, 78, 80, 86] Another occurrence is due to the partial radiative recombination from the interband states that may result in the red-shift of the emission spectra or multi-peak emission hinders the colour purity. Low PLQYs contribute to one of the major difficulties for the realisation of high-performance blue PeLEDs. Hence, designing strategies to enhance PLQYs is crucial for the development of efficient Q2DPe blue PeLEDs.

1.4.3.2 Phase impurity and orientation

The Q2DPes have been prepared by judicious loading of BOCs and A-site cations, with their ratio strongly influencing the formation and distribution of n phases.[63, 71] Desired n = 2, 3 phases are highly suitable for strong deep blue emission. Despite that, the low formation energies of the higher n phases cause the inhomogeneous phase distribution.[72] The broad n phase distribution (n = 1,2,3,4 5..) with the dominant n=1, 2 phases leads to the incomplete charge transfer, resulting in the multipeak emission and color impurity.[73] The presence of higher n phases leads to the exciton funnelling from lower n to higher n phases, resulting in the red-shift of the emission spectra and producing the cyan and green emissions. These factors hinder the desired deep-blue emission.

Various reports documented different growth mechanisms and layer orientations despite the use of similar preparation methods. Hence, it’s necessary to conduct focused and detailed studies for a profound understanding of the exact underlying mechanism of how the solvent processing conditions can impact the crystallisation, layer growth and orientation. Subsequently, it is also essential to discern the crystallisation dynamics for the development and optimisation of the strategies to achieve the phase purity (constant n) and their orientation for high-performance deep blue PeLEDs.

1.4.3.3 Ion migration and phase segregation – spectral instability

The blue PeLEDs have been suffering from severe spectral instability. It is the most substantial challenge to be addressed to achieve the stable efficient performance. Mixed halide composition (Cl/Br) is a practical approach to precisely tune emission in the blue-emissive region. Rationally increasing the Cl halide content in the composition blue-shifts the emission spectra. However, the only Cl-based efficient blue emitters are infeasible to achieve due to the very low solubility of PbCl2 in common solvents. Several reports have shown degradation of colour purity and red-shifted emission spectra in mixed-halide perovskite blue emitters under applied electric fields, due to ion migration and phase segregation within the crystal structure.[59] Furthermore, the organic A-site cations (MA, FA) are highly sensitive to the external parameters, such as temperature, moisture, oxygen, and humidity. On the contrary, inorganic A-site cations (Cs, Rb) are considered relatively stable and can improve spectral stability. Hence, it is essential to develop strategies to completely block ion migration and phase segregation to achieve spectrally stable, efficient blue PeLEDs.

1.4.3.4 Inefficient charge injection and interface losses

The wide-bandgap blue emitters have lower VB and higher CB positions, resulting in large band offsets between the perovskite emissive layer and the charge transport layers (CTLs). Due to the energy level mismatch, especially from the conventional HTLs with inappropriate VB position, holes experience a high energy potential barrier leading to poor charge injection into the Q2DPe emissive layer. Weak charge injection leads to high turn-on voltages, thereby reducing device efficiency. Besides, imbalanced charge injection into the emissive perovskites from both the ETL and HTL leads to the accumulation of charge carriers at the interface and results in faster degradation of blue PeLEDs. The presence of insulating BOCs (low conductivity) completely isolates the consecutive inorganic octahedral layers within the Q2DPe thin film and increases the devices' resistivity.  It further hinders out-of-plane or adjacent-layer charge transport within PeLEDs, thereby limiting overall device performance. Moreover, the presence of surface trap states at the Q2DPe layer/CTLs interface acts as a nonradiative recombination centre, and pin-holes within the Q2DPe thin-film act as leakage-current channels, reducing the overall device efficiency. Figure 1.9 (a) illustrates the schematic representation of the plausible energy level band diagram of the LED device structure with Q2DPe blue emitters and conventional HTLs/ETLs.

1.4.3.5 Device degradation

It is established that the operational stability and lifetime of the blue PeLEDs are being influenced by the intrinsic stability of perovskite blue emitters as well as CTLs, and importantly the energy-band-alignment with the CTLs/interfaces. Most of the Q2DPe blue emitters have been prepared by regulating the mixed halide (Cl/Br) composition, in which the Cl¯ vacancies relatively create deeper trap states than the Br¯ or I¯ within the energy bandgap.[87] These states irrevocably trap the charge carriers, suppress the radiative recombination, catalyse the device performance degradation through the ion migration, and make the perovskite more vulnerable to external atmospheric and operational conditions.[87] Hence, the inhibition of Cl¯ vacancies is believed to be a prerequisite for achieving the stability and improved lifetime of blue PeLEDs. Notably, the organic CTL materials have been widely employed for the fabrication of blue PeLEDs. The intrinsic instability of the CTLs also influences the device stability. The limited availability of stable CTLs makes it more challenging to fabricate stable blue PeLEDs with increased lifetime. Moreover, the large band offset at the perovskite/HTL interface, where the charge carriers experience an energetically high-potential barrier, causes the imbalanced charge injection and accumulation of charge carriers at the interface, further leading to the faster degradation of the blue PeLEDs. Therefore, minimising the band offsets can also effectively enhance the device stability and increase the device lifetime.

Figure 1.9. Schematic illustration of strategies to improve the performance of Q2DPe blue LEDs: (a) Energy levels of conventional hole-transport layer (HTL), electron-transport layer (ETL) materials available, and, group of blue and sky-blue emissive Q2DPe. (b) Passivation of surface defect states, and, blocking the ion migration and phase segregation to improve the emission properties and spectral stability of Q2DPe and blue PeLEDs performance. (c) Achieving the phase purity (constant n) for spectral purity and layer orientation for effective charge injection and transportation. (d) Designing the efficient multilayer LED device architectures through band-alignment optimization by reducing the large band offsets via interface engineering and designing new HTLs having deep VB. (e) Light out-coupling strategies for improving the PeLEDs EQE as marked in the figure (three panels).

1.4.4 Future directions and strategies for further improvements

For future directions and further improvements in blue PeLEDs, still more efforts are needed to design and optimize the new strategies. High-performance blue PeLEDs can be achieved through: (i) improving the PLQYs, (ii) obtaining the phase purity, better interconnectivity and conductivity, (iii) spectral stability and color purity in mixed halide systems, (iv) improving and balancing the charge injection efficiency and reducing the interface losses, (v) enhancing the ambient and thermal stability, and (vi) effective light out-coupling strategies.

Reducing the high defect densities and surface trap states through the effective passivation, doping and compositional engineering (Figure 1.9 (b)) through the additives significantly enhance the PLQYs of Q2DPe blue emitters. Also, preparation of the thin-films through the hot-casting considerably reduce the defect densities. Harvesting the triplet excitons along with the singlet excitons significantly increase the PLQYs to near unity.[88] The Q2DPe designed from the BOCs with high triplet energy states reduce the triplet quenching losses and improves the PLQYs.

The Q2DPe with n = 2, 3 phases are highly suitable for strong deep blue emission. Need to optimize the crystallization process through the compositional engineering of multiple BOCs/A-site cations and their thin-film processing conditions to achieve the phase purity (Figure 1.9 (c)) for stable blue emission. Doping and alloyed A-site cation composition also be an effective way to influence the rate of crystallization process through the modulation of crystallization dynamics which produces the concentrated and desired phase distribution, and uniform full coverage thin-film morphologies. In addition, the Q2DPe needs to be prepared from the BOCs of high binding energies, which forms a strong interaction with the inorganic octahedra of the perovskite framework that reduces the Ostwald ripening and enhance the phase stability under harsh external conditions.

Developing the Q2DPe with enhanced IMAEs through the proper selection of BOCs, additives, compositional engineering and other strategies will improve the spectral stability by blocking the ion migration and phase segregation (Figure 1.9 (b)) in mixed halide Q2DPe blue emitters. Pure inorganic A-site cations can also enhance the spectral stability. Moreover, designing the reduced-dimensional perovskites through the quantum confinement in pristine Br halide-based Q2DPe eliminates the chances of halide segregation, and lead to the spectral stability under applied electric fields.

Establishing the better conductivity between the consecutive inorganic octahedra layers within the thin-film through short-chain ligands in combination with the stable BOCs improves the out-of-plane and adjacent layer charge transport properties.  Preferential vertical growth/orientation (Figure 1.9 (c)) on the substrate via solvent engineering (DMSO: DMF) significantly enhances the charge injection efficiency between the Q2DPe-CTLs, and induces better charge transportation within the adjacent inorganic octahedra layers of the Q2DPe thin-film, and further improves the overall device efficiency.

Energy landscape through the incorporation of the intermediate layers with the appropriate thickness (ex. poly(methyl methacrylate) (PMMA), poly(ethylene oxide) (PEO), polyvinylpyrrolidone (PVP), and LIF)  at the perovskite/CTLs interface (Figure 1.9 (d)) reduces the band offsets, balance the charge injection into the perovskite emissive layer and suppress the emission quenching at the interface. Alternatively, designing the new HTLs with suitable deep VB is expected to be an effective way to reduce the large band offsets (Figure 1.9 (d)) and improve the hole charge injection efficiency. The modulation of the crystallization dynamics of perovskite blue emitters strongly depend on the new HTL surfaces upon which it is deposited. Importantly, the crystallization kinetics with improved morphological cleavage, to produce high quality, pin-hole flatter films besides maintaining the electron-hole balance are paramount for better device performances. Empathetically, the choice of new HTLs with deep valence band (VB) to balance the charge injection efficiency without compromising the crystallization dynamics of perovskites is at infancy. As future directions, more efforts are still needed for the comprehensive understanding to devise high-performance blue PeLEDs. Hence, designing the new HTLs are desired to promote the better hole injection and achieve the stable, high-performance blue PeLEDs. In addition, the optical down-conversion through self-absorption leads to the emissive losses and should be avoided by employing the CTLs that are transparent to the blue.

A possible approach to enhance the ambient, thermal and operational stability is, designing the perovskites from the compositional engineering through inorganic A-site cations in combination with stable monoamine and diamine BOCs possessing high binding energies. Developing strategies to enhance the perovskites ambient stability is paramount for practical solid-state lighting and display applications.

The fabrication of PeLEDs with the incorporation of additional nanophotonic engineering layer such as photonic crystals, nanodome array, nanowire array, microlens array, bioinspired moth-eye nanostructures, half-ball lens, low-index grids significantly enhance the extraction of light and out-coupling efficiency (Figure 1.9 (e)), which further improve the PeLEDs’ EQE.54 The presence of various nanostructures at the interface between the glass substrate/perovskite layer act as light couplers and optical antennas. These nanostructures scatter and guide the light out effectively by relatively suppressing the light losses arising from the mismatched refractive indices between the perovskite layer and the glass substrate (waveguide mode). Moreover, reducing the out-coupling losses arising from total internal reflection at the glass substrate/air interface (substrate mode) using photonic crystals, glass surface patterning, and surface texturing is also an attractive approach to enhance the EQE of PeLEDs.54 Overall, the efficient light-out-coupling strategy is believed to be a promising direction for achieving high-EQE blue PeLEDs.

1.5 Machine Learning

1.	U.S. Department of Energy, Life-Cycle Assessment of Energy and Environmental Impacts of LED Lighting Products: Part 2, LED Manufacturing and Performance. Pacific Northwest National Laboratory. Report No. PNNL-21443, 2012.

2.	Liu, W., et al., Advancements and Challenges of Highly Efficient and Stable Perovskite Light-Emitting Diodes. Laser & Photonics Reviews, 2026. 20(2): p. e01787.

3.	International Energy Agency. "The next wave of LED lighting: Smarter, circular and more efficient." IEA Commentary, Paris. 2024.

4.	Cui, D., et al., High-performance full-color afterglow organic light-emitting diodes with tri-mode emission and efficient energy transfer. npj Flexible Electronics, 2026.

5.	Sreejith, S., et al., Recent advancements in high efficiency deep blue organic light emitting diodes. Micro and Nanostructures, 2025. 200: p. 208101.

6.	Jacintha, V., et al., Advancing gallium nitride LED technology: principles, challenges, and future directions. Journal of Materials Science, 2025. 60(32): p. 13781-13834.

7.	Li, G., et al., Recent advances in III–V nitrides: properties, applications and perspectives. Journal of Materials Chemistry C, 2024. 12(32): p. 12150-12178.

8.	Ali, A., et al., Exploring the Recent Progress in InP Quantum Dots and QLEDs: Advances in Synthesis, Architecture, and Applications. 2025. 19(22): p. e01169.

9.	Cui, Z., et al., Advances, Challenges, and Perspectives for Heavy-Metal-Free Blue-Emitting Indium Phosphide Quantum Dot Light-Emitting Diodes. Advanced Optical Materials, 2023. 11(4): p. 2202036.

10.	Ye, J., et al., Defect Passivation in Lead-Halide Perovskite Nanocrystals and Thin Films: Toward Efficient LEDs and Solar Cells. Angewandte Chemie, 2021. 133(40): p. 21804-21828.

11.	Singh, D., et al., LEDs for energy efficient greenhouse lighting. Renewable and Sustainable Energy Reviews, 2015. 49: p. 139-147.

12.	Melnykov, S., et al., Thermally Activated Delayed Fluorescence in Organic Semiconductors and Its Application in Light-Emitting Diodes. East European Journal of Physics, 2024: p. 31-42.

13.	International Telecommunication Union. (2015). Parameter values... (ITU-R BT.2020-2).

14.	Wang, S., et al., Perovskite Nanocrystals: Synthesis, Stability, and Optoelectronic Applications. Small Structures, 2021. 2(3): p. 2000124.

15.	Rakshit, S., et al., Combining Perovskites and Quantum Dots: Synthesis, Characterization, and Applications in Solar Cells, LEDs, and Photodetectors. Advanced Optical Materials, 2022. 10(14): p. 2102566.

16.	Zakutayev, A., et al., Defect Tolerant Semiconductors for Solar Energy Conversion. The Journal of Physical Chemistry Letters, 2014. 5(7): p. 1117-1125.

17.	Queisser, H.J., Solidity is an imperfect state. Journal of Physics and Chemistry of Solids, 2008. 69(2): p. 256-258.

18.	Kojima, A., et al., Organometal Halide Perovskites as Visible-Light Sensitizers for Photovoltaic Cells. Journal of the American Chemical Society, 2009. 131(17): p. 6050-6051.

19.	Tavakoli, M.M., et al., Synergistic Crystal and Interface Engineering for Efficient and Stable Perovskite Photovoltaics. Advanced Energy Materials, 2019. 9(1): p. 1802646.

20.	Wang, Z., et al., Efficient ambient-air-stable solar cells with 2D–3D heterostructured butylammonium-caesium-formamidinium lead halide perovskites. Nature Energy, 2017. 2(9): p. 17135.

21.	Chiba, T., et al., Anion-exchange red perovskite quantum dots with ammonium iodine salts for highly efficient light-emitting devices. Nature Photonics, 2018. 12(11): p. 681-687.

22.	Tan, Z.-K., et al., Bright light-emitting diodes based on organometal halide perovskite. Nature Nanotechnology, 2014. 9(9): p. 687-692.

23.	Zhao, B., et al., High-efficiency perovskite–polymer bulk heterostructure light-emitting diodes. Nature Photonics, 2018. 12(12): p. 783-789.

24.	Lin, K., et al., Perovskite light-emitting diodes with external quantum efficiency exceeding 20 per cent. Nature, 2018. 562(7726): p. 245-248.

25.	Mathies, F., et al., Inkjet-Printed Triple Cation Perovskite Solar Cells. ACS Applied Energy Materials, 2018. 1(5): p. 1834-1839.

26.	Hermerschmidt, F., et al., Finally, inkjet-printed metal halide perovskite LEDs – utilizing seed crystal templating of salty PEDOT:PSS. Materials Horizons, 2020.

27.	Mathies, F., E.J.W. List-Kratochvil, and E.L. Unger, Advances in Inkjet-Printed Metal Halide Perovskite Photovoltaic and Optoelectronic Devices. Energy Technology, 2020. 8(4): p. 1900991.

28.	Tran, T.K.T., H.N. Nyiera, and J. Zhao, Instability of colloidal lead halide perovskite nanocrystals: Causes, improvement, and evaluation. Nano Research, 2024. 17(12): p. 10607-10619.

29.	Dirin, D.N., et al., Harnessing Defect-Tolerance at the Nanoscale: Highly Luminescent Lead Halide Perovskite Nanocrystals in Mesoporous Silica Matrixes. Nano Letters, 2016. 16(9): p. 5866-5874.

30.	Chen, Z., et al., Blue-Emitting CsPbBr3 Quantum Dots with Enhanced Performance through In Situ Aminosilane Passivation. The Journal of Physical Chemistry C, 2026. 130(19): p. 6777-6786.

31.	Kumar, G.S., R.R. Sumukam, and B. Murali, Quasi-2D perovskite emitters: a boon for efficient blue light-emitting diodes. Journal of Materials Chemistry C, 2020. 8(41): p. 14334-14347.

32.	Zhang, Q., et al., Perovskite Light-Emitting Diodes with Quantum Wires and Nanorods. Advanced Materials, 2025. 37(23): p. 2405418.

33.	de Mello Donegá, C., P. Liljeroth, and D. Vanmaekelbergh, Physicochemical Evaluation of the Hot-Injection Method, a Synthesis Route for Monodisperse Nanocrystals. Small, 2005. 1(12): p. 1152-1162.

34.	Protesescu, L., et al., Nanocrystals of Cesium Lead Halide Perovskites (CsPbX3, X = Cl, Br, and I): Novel Optoelectronic Materials Showing Bright Emission with Wide Color Gamut. Nano Letters, 2015. 15(6): p. 3692-3696.

35.	Tong, Y., et al., Highly Luminescent Cesium Lead Halide Perovskite Nanocrystals with Tunable Composition and Thickness by Ultrasonication. Angewandte Chemie International Edition, 2016. 55(44): p. 13887-13892.

36.	Li, S., et al., Continuous Nanomanufacturing of Inorganic Lead Halide Perovskite Nanocrystals with High-Concentration Precursors. ACS Applied Materials & Interfaces, 2024. 16(9): p. 11704-11714.

37.	Li, M., et al., Review on Anion Exchange of Lead-Halide Perovskite Nanocrystals: Process, Methods, and Applications. Advanced Engineering Materials, 2025. 27(4): p. 2401776.

38.	ten Brinck, S. and I. Infante, Surface Termination, Morphology, and Bright Photoluminescence of Cesium Lead Halide Perovskite Nanocrystals. ACS Energy Letters, 2016. 1(6): p. 1266-1272.

39.	Ravi, V.K., et al., Origin of the Substitution Mechanism for the Binding of Organic Ligands on the Surface of CsPbBr3 Perovskite Nanocubes. The Journal of Physical Chemistry Letters, 2017. 8(20): p. 4988-4994.

40.	Almeida, G., I. Infante, and L. Manna, Resurfacing halide perovskite nanocrystals. Science, 2019. 364(6443): p. 833-834.

41.	Yassitepe, E., et al., Amine-Free Synthesis of Cesium Lead Halide Perovskite Quantum Dots for Efficient Light-Emitting Diodes. Advanced Functional Materials, 2016. 26(47): p. 8757-8763.

42.	De Roo, J., et al., Highly Dynamic Ligand Binding and Light Absorption Coefficient of Cesium Lead Bromide Perovskite Nanocrystals. ACS Nano, 2016. 10(2): p. 2071-2081.

43.	Krieg, F., et al., Colloidal CsPbX3 (X = Cl, Br, I) Nanocrystals 2.0: Zwitterionic Capping Ligands for Improved Durability and Stability. ACS Energy Letters, 2018. 3(3): p. 641-646.

44.	Ye, J., et al., Defect Passivation in Lead-Halide Perovskite Nanocrystals and Thin Films: Toward Efficient LEDs and Solar Cells. Angewandte Chemie International Edition, 2021. 60(40): p. 21636-21660.

45.	Udayabhaskararao, T., et al., A Mechanistic Study of Phase Transformation in Perovskite Nanocrystals Driven by Ligand Passivation. Chemistry of Materials, 2018. 30(1): p. 84-93.

46.	Nenon, D.P., et al., Design Principles for Trap-Free CsPbX3 Nanocrystals: Enumerating and Eliminating Surface Halide Vacancies with Softer Lewis Bases. Journal of the American Chemical Society, 2018. 140(50): p. 17760-17772.

47.	Kumawat, N.K., et al., Band Gap Tuning of CH3NH3Pb(Br1–xClx)3 Hybrid Perovskite for Blue Electroluminescence. ACS Applied Materials & Interfaces, 2015. 7(24): p. 13119-13124.

48.	Ren, Z., et al., Strategies Toward Efficient Blue Perovskite Light-Emitting Diodes. Advanced Functional Materials, 2021. 31(30): p. 2100516.

49.	Mao, L., C.C. Stoumpos, and M.G. Kanatzidis, Two-Dimensional Hybrid Halide Perovskites: Principles and Promises. Journal of the American Chemical Society, 2019. 141(3): p. 1171-1190.

50.	Ahmad, S., et al., Dion-Jacobson Phase 2D Layered Perovskites for Solar Cells with Ultrahigh Stability. Joule, 2019. 3(3): p. 794-806.

51.	Zheng, K. and T. Pullerits, Two Dimensions Are Better for Perovskites. The Journal of Physical Chemistry Letters, 2019. 10(19): p. 5881-5885.

52.	Xing, J., et al., Color-stable highly luminescent sky-blue perovskite light-emitting diodes. Nature Communications, 2018. 9(1): p. 3541.

53.	Yuan, F., et al., A Cocktail of Multiple Cations in Inorganic Halide Perovskite toward Efficient and Highly Stable Blue Light-Emitting Diodes. ACS Energy Letters, 2020. 5(4): p. 1062-1069.

54.	Vashishtha, P., et al., High Efficiency Blue and Green Light-Emitting Diodes Using Ruddlesden–Popper Inorganic Mixed Halide Perovskites with Butylammonium Interlayers. Chemistry of Materials, 2019. 31(1): p. 83-89.

55.	Lei, L., et al., Efficient Energy Funneling in Quasi-2D Perovskites: From Light Emission to Lasing. Advanced Materials, 2020. 32(16): p. 1906571.

56.	Kim, H., et al., 2D and Quasi-2D Halide Perovskites: Applications and Progress. physica status solidi (RRL) – Rapid Research Letters, 2020. 14(2): p. 1900435.

57.	Chen, P., et al., Charge-transfer versus energy-transfer in quasi-2D perovskite light-emitting diodes. Nano Energy, 2018. 50: p. 615-622.

58.	Gao, L., et al., Improving Charge Transport via Intermediate-Controlled Crystal Growth in 2D Perovskite Solar Cells. Advanced Functional Materials, 2019. 29(47): p. 1901652.

59.	Wang, K.-H., et al., Efficient and Color-Tunable Quasi-2D CsPbBrxCl3–x Perovskite Blue Light-Emitting Diodes. ACS Photonics, 2019. 6(3): p. 667-676.

60.	Liang, D., et al., Color-Pure Violet-Light-Emitting Diodes Based on Layered Lead Halide Perovskite Nanoplates. ACS Nano, 2016. 10(7): p. 6897-6904.

61.	Hu, H., et al., Molecularly Engineered Organic-Inorganic Hybrid Perovskite with Multiple Quantum Well Structure for Multicolored Light-Emitting Diodes. Scientific Reports, 2016. 6(1): p. 33546.

62.	Liu, R. and K. Xu, Blue perovskite light-emitting diodes (LEDs): A minireview. Instrumentation Science & Technology, 2020: p. 1-21.

63.	Li, Z., et al., Modulation of recombination zone position for quasi-two-dimensional blue perovskite light-emitting diodes with efficiency exceeding 5%. Nature Communications, 2019. 10(1): p. 1027.

64.	Wang, Q., et al., Efficient sky-blue perovskite light-emitting diodes via photoluminescence enhancement. Nature Communications, 2019. 10(1): p. 5633.

65.	Hou, S., et al., Efficient Blue and White Perovskite Light-Emitting Diodes via Manganese Doping. Joule, 2018. 2(11): p. 2421-2433.

66.	Pan, G., et al., Bright Blue Light Emission of Ni2+ Ion-Doped CsPbClxBr3–x Perovskite Quantum Dots Enabling Efficient Light-Emitting Devices. ACS Applied Materials & Interfaces, 2020. 12(12): p. 14195-14202.

67.	Zou, Y., et al., Spectral-Stable Blue Emission from Moisture-Treated Low-Dimensional Lead Bromide-Based Perovskite Films. ACS Photonics, 2019. 6(7): p. 1728-1735.

68.	Zhang, C., et al., Surface Ligand Engineering toward Brightly Luminescent and Stable Cesium Lead Halide Perovskite Nanoplatelets for Efficient Blue-Light-Emitting Diodes. The Journal of Physical Chemistry C, 2019. 123(43): p. 26161-26169.

69.	Chen, Z., et al., High-Performance Color-Tunable Perovskite Light Emitting Devices through Structural Modulation from Bulk to Layered Film. Advanced Materials, 2017. 29(8): p. 1603157.

70.	Wang, Q., et al., Efficient Sky-Blue Perovskite Light-Emitting Devices Based on Ethylammonium Bromide Induced Layered Perovskites. ACS Applied Materials & Interfaces, 2017. 9(35): p. 29901-29906.

71.	Yantara, N., et al., Designing the Perovskite Structural Landscape for Efficient Blue Emission. ACS Energy Letters, 2020. 5(5): p. 1593-1600.

72.	Quan, L.N., et al., Ligand-Stabilized Reduced-Dimensionality Perovskites. Journal of the American Chemical Society, 2016. 138(8): p. 2649-2655.

73.	Yuan, S., et al., Optimization of Low-Dimensional Components of Quasi-2D Perovskite Films for Deep-Blue Light-Emitting Diodes. Advanced Materials, 2019. 31(44): p. 1904319.

74.	Gao, X., et al., Ruddlesden–Popper Perovskites: Synthesis and Optical Properties for Optoelectronic Applications. Advanced Science, 2019. 6(22): p. 1900941.

75.	Zeng, S., et al., Mixed-ligand engineering of quasi-2D perovskites for efficient sky-blue light-emitting diodes. Journal of Materials Chemistry C, 2020. 8(4): p. 1319-1325.

76.	Jin, Y., et al., Synergistic Effect of Dual Ligands on Stable Blue Quasi-2D Perovskite Light-Emitting Diodes. 2020. 30(6): p. 1908339.

77.	Jiang, Y., et al., Spectra stable blue perovskite light-emitting diodes. Nature Communications, 2019. 10(1): p. 1868.

78.	Luo, M., et al., Metal halide perovskites for blue light emitting materials. APL Materials, 2020. 8(4): p. 040907.

79.	Jin, Y., et al., Synergistic Effect of Dual Ligands on Stable Blue Quasi-2D Perovskite Light-Emitting Diodes. Advanced Functional Materials, 2020. 30(6): p. 1908339.

80.	Li, C.H.A., et al., The Future Is Blue (LEDs): Why Chemistry Is the Key to Perovskite Displays. Chemistry of Materials, 2019. 31(16): p. 6003-6032.

81.	Ma, D., et al., Chloride Insertion–Immobilization Enables Bright, Narrowband, and Stable Blue-Emitting Perovskite Diodes. Journal of the American Chemical Society, 2020. 142(11): p. 5126-5134.

82.	Lee, H.-D., et al., Efficient Ruddlesden–Popper Perovskite Light-Emitting Diodes with Randomly Oriented Nanocrystals. Advanced Functional Materials, 2019. 29(27): p. 1901225.

83.	Liu, Y., et al., Efficient blue light-emitting diodes based on quantum-confined bromide perovskite nanostructures. Nature Photonics, 2019. 13(11): p. 760-764.

84.	Shang, Y., et al., Quasi-2D Inorganic CsPbBr3 Perovskite for Efficient and Stable Light-Emitting Diodes. Advanced Functional Materials, 2018. 28(22): p. 1801193.

85.	Wang, N., et al., Perovskite light-emitting diodes based on solution-processed self-organized multiple quantum wells. Nature Photonics, 2016. 10(11): p. 699-704.

86.	Kumawat, N.K., et al., Blue perovskite light-emitting diodes: progress, challenges and future directions. Nanoscale, 2019. 11(5): p. 2109-2120.

87.	Zheng, X., et al., Chlorine Vacancy Passivation in Mixed Halide Perovskite Quantum Dots by Organic Pseudohalides Enables Efficient Rec. 2020 Blue Light-Emitting Diodes. ACS Energy Letters, 2020. 5(3): p. 793-798.

88.	Qin, C., et al., Triplet management for efficient perovskite light-emitting diodes. Nature Photonics, 2020. 14(2): p. 70-75.