Strategic Compositional Engineering in Quasi-2D Ruddlesden-Popper Perovskites to Decipher Deep Blue Emission

Experimental Section

Materials and Methods: Lead Bromide (>98%) and Lead Chloride (>98%) were procured from TCI, Cesium Bromide (CsBr > 99.9%), Phenethylamine, Hydrochloric acid solution 37%, and Yttrium Chloride (anhydrous) were purchased from Sigma Aldrich, Dimethylsulfoxide (anhydrous 99.8%) purchased from Alfa Aesar. All these materials were used as received.

PEACl synthesis: For the synthesis of PEACl salt, equimolar phenethylamine and hydrochloric acid solution were reacted for 2 hours at 0º C under nitrogen conditions while stirring. After the completion of the reaction, PEACl (White powder) was recovered by rotary evaporation at 80 °C, followed by recrystallization using diethyl ether. Finally, the obtained recrystallized PEACl powder was dried in a vacuum oven for one day at room temperature.

Precursor solution of (PEA)2(Cs)n-1Pbn(BrxCl1-x)3n+1: Initially, individual solutions of CsPbBr3, PbCl2 (0.15 M), YCl3 (0.25 M), and PEACl (1.00 M) were prepared in DMSO. Whereas precursor CsPbBr3 was prepared by dissolving 1:1.5 molar ratios of PbBr2 (293.6 mg) and CsBr (424.0 mg) in 6.4 ml DMSO, PbCl2 solution was prepared by dissolving 333.8 mg PbCl2 in 1.6 ml DMSO, YCl3 solution was prepared by dissolving 49.0 mg YCl3 in 1.0 ml DMSO, and PEACl solution was prepared by dissolving 316.0 mg PEACl in 2 ml DMSO. All the solutions were kept for stirring overnight at 70º C in the glove box. Finally, after 12 hours the temperature of the solutions was brought down to room temperature, and (PEA)2(Cs)n-1Pbn(BrxCl1-x)3n+1 precursor was prepared by sequential mixing of CsPbBr3 (0.8 ml) and PbCl2 (0.2 ml) in such a way that molar ratios of the CsBr: PbBr2: PbCl2 equal to 2.5: 1.0: 1.5, then 20 µl of YCl3 (2% of Cs), and a variable amount of PEACl with respect to  Cs concentration (0.25 M) ( 0% (0.0 ml), 30% (0.075 ml), 60% (0.150 ml), 80% (0.200 m), 100% (0.250 ml), 120% (0.300 ml), and 140% (0.350 ml) ) was added for fixed composition of CsPbBr3, PbCl2, and YCl3.

Q2DPe thin films fabrication: Glass substrates were used for the preparation of Q2DPe thin films. Firstly, the substrates were cleaned in the standard cleaning procedure. Then cleaned glass substrates were UV-ozone treated for 20 minutes before coating the perovskite. Thereafter, the substrates were transferred into the glove box for the spin coating. The final (PEA)2(Cs)n-1Pbn(BrxCl1-x)3n+1 precursor solution (200 µl) was spin-coated on the substrate statically at 3000 rpm for 1 min, where antisolvent toluene (300 µl) was poured dynamically on perovskite film at the 20 second time point of that one minute, followed by annealing the thin film at 80º C for 10 minutes.

Q2DPe thin films characterization: UV-Vis Absorption spectra were recorded with JASCO V-750 Spectrophotometer equipped with an integrating sphere. Photoluminescence spectra (PLQY using an integrating sphere) were measured with JASCO FP-8500 Spectrofluorometer. Fluorescence intensity decay measurements were done using PicoQuant MicroTime 200 time-resolved confocal fluorescence microscope system (IRF=144 ps) where samples were excited by a pulsed picosecond diode laser (λex = 405 nm) to obtain the average lifetime of the charge carriers. The structural and crystalline characterizations were determined by Powder XRD patterns and TEM obtained from Bruker D8 Advance X-ray diffractometer using Cu Kα radiation (of wavelength λ = 0.15406 nm) and JEM-F200 multi-purpose microscope (JOEL) with an accelerating voltage of 200 kV, respectively. The microstructural investigation was done by Atomic Force Microscopy (AC tapping mode) and Field-Emission Scanning Electron Microscope (electron beam accelerated to 3 kV was used) using MFP-3D Origin Asylum Instrument and Merlin compact model of Carl Zeiss, respectively.

Figure 1: PL spectra of 100% PEACl composition thin film at 372 nm and 393 nm excitation wavelength.

Figure 2: SEM micrograms showing the morphological changes in the thin films with the incorporation of PEACl into the 3D CsPbBr1.8Cl1.2 system for a) 0% PEACl. b) 30% PEACl. c) 60% PEACl. d) 80% PEACl. e) 100% PEACl. f) 120% PEACl. g) 140% PEACl.

Figure 3: TEM images of the 100% PEACl sample in sequence (a-f) showing the formation of multiple domains in the thin films upon continuous irradiation of electrons.