Post Synthesis Treatment of CsPbBr3 Nanocrystals to Suppress Surface Traps and Non-Radiative Recombination Rates

EXPERIMENTAL SECTION

Materials and Methods: Lead Bromide (>98%) and Cesium carbonate (99.9%) were procured from TCI, octadecene (ODE, 90%), oleic acid (OA, 90%), oleylamine (OLA, 70%), YCl3, PDABr2, GuSCN, KSCN, Choline Bromide, and NH4SCN were purchased from Sigma-Aldrich. HPLC grade Toluene, brought from Finar Chemicals. All these materials were used as received.

Preparation of Cs-oleate: Cs-oleate were prepared by following a reported procedure.1 In brief, 0.1628 g of Cs2CO3, 8 mL of ODE, and 0.5 mL of OA were mixed in a 50 mL double-necked round-bottom flask (RB), which was heated under vacuum at 120°C for an hour and then under nitrogen atmosphere until all Cs2CO3 reacted with OA to form a clear solution of Cs-oleate complex. This solution was maintained at this temperature for its use to avoid precipitation.

Preparation of CsPbBr3 NCs: CsPbBr3 NCs were prepared by following a reported procedure.1 In a 50 mL double/triple-necked RB, 0.069 g of PbBr2 along with 5 mL of ODE, 0.5 mL of OA, and 0.5 mL of OLA were mixed and heated under vacuum at 120°C for an hour. The temperature was then increased to 170°C under nitrogen atmosphere and 0.4 mL of pre-heated Cs-oleate solution was injected swiftly, followed by immediate cooling of the solution in ice-cold water. The NCs were obtained by collecting the precipitate upon centrifuging the whole dispersion at ∼7000 rpm and dispersing in Toluene for further measurements.

Post synthesis surface treatment: The surface treatment involved the preparation of 1 M solution of each passivating agent (YCl3, PDABr2, GuSCN, KSCN, Choline Bromide, and NH4SCN) in toluene. All the solutions were stirred for 30 minutes. Then, each solution was added in the discrete 0.25 ml, 0.5 ml, 0.75 ml, 1.0 ml, 1.25 ml, 1.5 ml, 1.75 ml, 2.0 ml, and 2.25 ml to the fixed amount of pristine CsPbBr3 NCs and stirred for 30 mins in ambient conditions. Thereafter, the mixtures were investigated.

NCs thin films fabrication: Glass substrates were used for the preparation of CsPbBr3 NCs thin films. Firstly, the substrates were cleaned in the standard cleaning procedure. Then cleaned glass substrates were UV-ozone treated for 20 minutes before coating the perovskite. Thereafter, the substrates were transferred into the glove box for the spin coating. QDs solution of ~50 L was spin-coated at 2000 rpm for 30 seconds.

NCs characterization: UV-Vis Absorption spectra were recorded with JASCO V-750 Spectrophotometer in solution state. Photoluminescence spectra were measured with JASCO FP-8500 Spectrofluorometer. PLQY of the NCs we measure by coating them on glass slide and then using an JASCO FP-8500 Spectrofluorometer with integrating sphere setup. Fluorescence intensity decay measurements were done using PicoQuant MicroTime 200 time-resolved confocal fluorescence microscope system (IRF=144 ps) where samples were excited by a pulsed picosecond diode laser (λex = 405 nm) to obtain the average lifetime of the charge carriers. The structural and crystalline characterizations were determined by Powder XRD patterns and TEM obtained from Bruker D8 Advance X-ray diffractometer using Cu Kα radiation (of wavelength λ = 0.15406 nm) and JEM-F200 multi-purpose microscope (JOEL) with an accelerating voltage of 200 kV, respectively. The microstructural investigation was done by Field-Emission Scanning Electron Microscope (electron beam accelerated to 3 kV was used) using Merlin compact model of Carl Zeiss.

Figure S1. Powder XRD graph of the PDABr2 treated CsPbBr3 NCs coated on a thin film.

Figure S2. TEM images of a) pristine CsPbBr3 NCs b) PDABr₂:CsPbBr3 NCs, c) GuSCN:CsPbBr3 NCs, d) YCl₃:CsPbBr3 NCs, and e) NH₄SCN:CsPbBr3 NCs.

1.	Protesescu, L.;  Yakunin, S.;  Bodnarchuk, M. I.;  Krieg, F.;  Caputo, R.;  Hendon, C. H.;  Yang, R. X.;  Walsh, A.; Kovalenko, M. V., Nanocrystals of Cesium Lead Halide Perovskites (CsPbX3, X = Cl, Br, and I): Novel Optoelectronic Materials Showing Bright Emission with Wide Color Gamut. Nano Letters 2015, 15 (6), 3692-3696.