Solar Cells and Photonics Research Laboratory, School of Chemistry, University of

- Hyderabad, Hyderabad, Telangana, 500046, India.

*Corresponding Author: murali.banavoth@uohyd.ac.in

Received 00th January 20xx,

Accepted 00th January 20xx

DOI: 10.1039/x0xx00000x

Quasi-2D Perovskite Emitters: A Boon for Efficient Blue Light-Emitting-Diodes

Gundam Sandeep Kumar, Ranadeep Raj Sumukam and Banavoth Murali*

Metal halide perovskites have accomplished excellent progress as forefront materials for near-infrared, red and green perovskite light-emitting-diodes (PeLEDs) with external quantum efficiencies (EQEs) reaching above 20%, promising a bright future for next-generation printable energy-efficient lighting and display technologies. Empathetically, the perovskite blue emitters and corresponding PeLEDs with inherent circumscribed progression, are lagging far behind in performance compared to their other color counterparts, owing to low photoluminescence quantum yields (PLQYs), poor stability and inefficient charge injection. Thanks to the layered quasi-2D perovskites (Q2DPe) for exhibiting enhanced PLQYs, color-tunability, improved environmental and operational stability owing to their tunable exciton binding energies arising from the bulky organic cation incorporation. Hence, acknowledging the progressive evolution of blue emitters and the performance of blue PeLEDs from Q2DPe, they are believed to be the best solution so far to address the challenges associated with the blue LEDs and is indubitably an emerging research area in the present scenario. A comprehensive and profound understanding of compositional engineering to achieve high PLQYs by reducing defect states density, blocking the ion migration effects in mixed halide systems for spectral stability and promising design strategies to achieve phase purity (desired and concentrated n) for narrow emission is need of the hour. Therefore, this perspective builds on the envelope of an overview of Q2DPe blue emitters and blue PeLEDs, where, we have reinforced our critical views on the evolution of the recent attempts to tune Q2DPe structural, chemical and optical properties. Moreover, this perspective has emphasised on passivation, thin-film morphology, interface engineering and the substantial progress accomplished till date to obtain better performing Q2DPe LEDs. Finally, we have presented a roadmap for further investigations addressing the current challenges and plausible potential prospects in the pursuit of efficient Q2DPe blue emitters and blue LEDs.

1. Introduction

Solution-processed hybrid organic-inorganic lead halide perovskites [ABX3, where A is a monovalent cation (MA, Cs, FA), B is divalent metal cation (Pb2, Sn2), X is a halide (Cl, Br, I)] have captivated the research interests in the frontline of next-generation photovoltaic1-3 and light-emitting-diode (LED)4-7 applications. Recently, perovskites have emerged as potential active emitters, where the near-infrared, red and green-emissive perovskite LEDs (PeLEDs) have expeditiously increased, and thanks to the corresponding external quantum efficiencies (EQE) for exceeding over 20%.5-7 Importantly, the phenomenal performances of PeLEDs owing to their unprecedented attributes such as wider color gamut, high color purity, high photoluminescence quantum yields (PLQYs), and high charge carrier mobilities.8-10 Besides, their low temperature and easy solution-processability facilitates the utilization of low-cost solution-based techniques for the preparation of thin-films such as roll-to-roll processing or screen or inkjet printing to fabricate the cost-effective large-area flexible display devices.11-13 The current progress strengthens the belief that PeLEDs can be the best substitute for organic LEDs to accelerate the development of next-generation lighting/display applications through encouraging solution-processable printing technologies. However, research on perovskite blue emitters and blue PeLEDs still in infancy and it remains arduous, lagging far behind in its both the efficiency and stability, which is detrimental to the development of full-color solid-state lighting and display technologies.

High bandgap perovskite blue emitters possess low PLQYs, due to their high defect density assisted nonradiative recombinations.14 Additional hitches, such as ion migration and phase segregation in mixed halide (Cl/Br) perovskite blue emitters lead to spectral instability and poor device performance.15 Intrusively, intrinsic deep valence band (VB) energy level of wide-bandgap perovskite blue emitters acts as a high potential barrier, causing poor charge carrier injection and accumulation of charge carriers at the interface thereby limiting the overall device performance.16 Top three champion blue PeLEDs’ EQEs found to be 2.12% in Mn-doped CsPb(BrxCl1−x)3 quantum dots (QDs), 2.4% in Ni-doped CsPbCl0.99Br2.01 QDs 17, 18 and 6.3% in n-dodecyl ammonium thiocyanate (DAT) treated CsPb(BrxCl1−x)3 QDs19 are considerably low compared to other color counterparts, a prerequisite for successful display marketing. In a nutshell, the scanty blue PeLED device performance, spectral and operational instabilities are impeding their further development and application. Moreover, the three-dimensional (3D) bulk and nanocrystals (NCs) occupying structure ABX3 suffers from severe intrinsic chemical instability to the external moisture/oxygen, poor thermal stability, low film-coverage, and high defect density, remains the most critical bottleneck, which impedes their further development for efficient LEDs performance. Hence, it’s essential to reframe these perovskite building blocks more resistive to external conditions to make them suitable for real-time applications. Therefore, designing new materials preparation strategies are required to achieve performance parity for high PLQYs, excellent color and structural stability, high EQEs that foster the scalable commercial application of PeLEDs. Else, these perovskite materials may become yet another down-converting materials/color filters for subsisting technologies akin to colloidal semiconductor QDs and few organic molecules.

2. Layer structured quasi-2D perovskites

Additional bulky organic cations (BOCs) (Aʹ) have been introduced into 3D perovskites (ABX3) for the formation of layered perovskites (Aʹ2An-1BnX3n+1), where Aʹ is a monoamine BOC, n is a stacked inorganic octahedron (PbX6)4–: n=1 are two-dimensional (2D) perovskites, n=2,3,4… are the Q2DPe (Fig. 1a), and n= are the conventional 3D perovskites.20 Structurally, the BOCs are connected to the inorganic (PbX6)4– octahedra of perovskites through hydrogen bonding between the amine groups and halides. Additionally, the van der Waals interaction existing between the tails of bilayer BOCs forms a spacer. The resultant structure is an inorganic (PbX6)4– octahedra sandwiched between the bilayers of BOCs, known as Ruddlesden-Popper (RP) phase Q2DPe.20 Instead, the organic spacer between the perovskite sheets can be composed of a diamine BOC. The perovskite sheets are connected by the direct linkage of the diamine cation thereby eliminating the van der Waals gap;  referred as Dion-Jacobson (DJ) phase Q2DPe with the chemical formula AʹʹAn-1BnX3n+1; where Aʹʹ is a diamine organic cation.21 The insulating nature of the organic spacers creates energetically high potential barriers on both sides of inorganic octahedra, resulting in the formation of a quantum well structure consisting of inorganic layers with low bandgap and high dielectric constant (εw), and the spacer cation barrier with high bandgap and low dielectric constant (εb) (Fig. 1b).22 Consecutively, the charge carriers confine strongly within the inorganic octahedra of perovskite framework and increase/tailor the exciton binding energies through the dielectric (n=1) and quantum (n=2,3,4..) confinement effects.22 Furthermore, the hydrophobic nature of the spacer cations isolates the inorganic octahedra from the external moisture, oxygen and possibly enhances the stability of the resultant layered perovskite structures.20, 21

The striking optoelectronic properties of the Q2DPe are tailored by modulating the width of both the inorganic octahedra layer as well as the organic spacer. The promising strategies include engineering the perovskites layer composition, various size-dependent BOCs and dielectric constant, and regulating the number of layers (n = 2, 3, 4..) etc.20, 22 The compositional engineering entailed by incorporation of mixed A-site cations; cesium (Cs), methylammonium (MA), formamidinium (FA), and mixed BOCs; phenylethylammonium (PEA), iso-propylammonium (IPA), butylammonium (BA) allows the flexibility to ameliorate the structural, optical properties and its stability (Fig. 1c).23, 24 The number of layers in Q2DPe can be reduced by increasing the stoichiometric ratio of BOCs to A-site cations (Aʹ/A) in the precursor solution. As the number of layers decreases, the corresponding energy bandgap increases,23 augmenting the adjustability to regulate the efficient emitters in the blue region by optimizing the number of layers in Q2DPe, which are previously difficult to prepare from the conventional 3D or nanostructure perovskites. However, achieving the phase purity (constant n value) i.e., homogeneous distribution is arduous. Most of the reports documented that the Q2DPe thin-films prepared from the mixed-cation compositions consist of the heterogeneous distribution, i.e. mixed-phase (a combination of different n values).25, 26 The heterogeneous distribution leads to the presence of dissimilar energy bandgaps and corresponding conduction/valance band energy levels. The presence of insulating organic spacers between the perovskite layers results in multiple quantum well structures (Fig. 1d). In this scenario, the excitation of charge carriers takes place at the high bandgap (lower n phase) region. Due to the presence of energy bandgap or energy level gradient, the charge transfer occurs from lower n phase to the higher n phase on a picosecond timescale through the phenomenon of exciton funneling, where the effective radiative recombination ensues (Fig. 1d).26 The ultrafast charge transfer through exciton funneling can surpass the nonradiative recombinations at the grain boundaries and surface defects that exists within the high bandgap phase, thereby improving the overall PLQYs.27, 28 The energy landscape color-gradient representation illustrates the charge transfer process between the heterogeneous phases (each color indicates a different n value) present within the thin-films, i.e. from lower n region to higher n region (Fig. 1e). However, a major challenge exists to achieve the deep blue emission and color purity by limiting the extent of exciton funneling to large n within the broad n distributed heterogeneous phase of Q2DPe thin-films.

The Q2DPe thin-films can be easily prepared by spin-coating the perovskite precursor solution onto the target substrates. The size distribution, orientation, packing density of the layered perovskites within the thin-film can be controlled through the additional solvent or additive engineering during the spin-coating process (Fig. 1f). The orientation of the layered perovskites may be random, vertical, and horizontal (Fig. 1g), subject to various processing conditions and the solvents used. Mixed dimethylsulfoxide (DMSO)/ dimethylformamide (DMF) solvent engineering promotes the formation of one intermediate complex and further annealing induces the perovskite growth in one direction with a preferred vertical orientation.29 Recent reports demonstrated the fabrication of PeLEDs in the blue region from Q2DPe through various compositional engineering, different processing conditions, and solvent engineering strategies.30-35 The annual progresses and performance evolution of the Q2DPe-based blue and sky-blue PeLEDs are presented in Fig. 1h, and maximum EQE of blue and sky-blue PeLEDs are found to be  5.7%34 and 11%35 respectively.

Fig. 1 Schematic illustration of: (a) Unit cell of cubic 3D perovskite crystal structure and layered structure of Q2DPe with different phases from n = 1 to n = 4. (b)  Single-quantum well structure of Q2DPe; inorganic octahedra sandwiched between the barriers of organic spacers. (c)  Compositional engineering of Q2DPe by using bulky organic multi-cations, A-site multi-cations, and mixed halides. (d) Charge transfer or funneling of excitons between Q2DPe of small n to large n phase through energy band diagram. (e) Schematic energy landscape of the Q2DPe with different n phase. (f)  Preparation of Q2DPe thin-films via spin-coating method. (g)  Orientation (Random, Vertical, and Horizontal) or growth of the layers in Q2DPe thin-film. (h)  Year wise EQE progression of Q2DPe based blue and sky-blue LEDs from 2016 to till date.

Table 1 summarizes the performance parameters of Q2DPe-based blue and sky-blue LEDs.

3. Recent progress on quasi-2D perovskite blue emitters and blue PeLEDs

3.1 Compositional engineering

The recent remarkable improvements in the performance and stabilities of Q2DPe-based blue LEDs compared to their 3D counterparts are due to their striking optical properties and tunable exciton binding energies arising from the regulation of the number of inorganic octahedra layers (n). The first 2D perovskites ((PEA)2PbBr4, n =1) based blue LED was prepared by using the PEA as BOC.31  These 2D perovskites formed a single quantum well structure, where the charge carriers were strongly confined in the inorganic octahedra of perovskite framework and had exhibited very large exciton binding energies. These devices displayed meagre performances with a maximum EQE of 0.04% at 410 nm, limited by the strong phonon scattering and exciton-phonon coupling effect.31 Considering the poor efficiencies in both the pure 2D perovskites (n = 1) and conventional 3D perovskites (n = ), alternatively new strategies have been developed to harvest the combined advantages of color purity of 2D-perovskites, and high electron mobility and conductivities of the 3D perovskites into a single system. Therefore, Q2DPes are devised by tailoring the number of layers to tune the exciton binding energies, emission spectra and to produce the efficient, bright and stable blue emitters.

To achieve the efficient blue emission, two strategies have been developed: a) through the precise regulation of the ratio of mixed halides (Cl/Br)17, 18, 24, 25, 30, 32 (Fig. 2a), b) size-dependent quantum confinement (small n = 2,3,4…) effect26, 28, 30, 32, 34, 36, 37 through the utilization of the rationalized amount of BOCs (Fig. 2b) in the precursor solution. The first Q2DPe blue emitters (BA2MAn−1Pbn(Br/Cl)3n+1) were prepared from the MA and BA cations with an appropriate ratio to tailor the number of layers to tune exciton binding energies/adjust the exciton confinement effect accompanied by the mixed-halide (Br/Cl) ratio of 7:3. The Q2DPe thin-films exhibited a uniform morphology, dense packing and better quality as compared to the conventional 3D perovskite counterparts.32 Corresponding blue PeLEDs displayed an EQE of 0.01% at 468 nm.32

To produce the blue emission from the only Br halide-based perovskites, Q2DPe were prepared only through quantum confinement effect by incorporating the amine-based small molecule 2-phenoxyethylamine (POEA)38 and ethylammonium (EA)39 BOCs into the MAPbBr3 system, respectively. The PeLEDs displayed  maximum EQEs of 0.06%, 1.1% at 462 nm, 480 nm,38 and 2.6% at 485 nm39 respectively. Similarly, blue

Fig. 2 (a) Normalized PL spectra of Q2DPe thin-films (PBABr:CsPbBrxCl3−x) with increased chloride content from 0 to 50% (from right to left). Copyright 2019, American Chemical Society.30 (b) Blue PeLED’s energy band diagram and corresponding energy level positions of Q2DPe with increased content of PEABr from 0 to 120%. Copyright 2019, Nature Communications.34 (c) Tunable PL emission spectra of Q2DPe composed of PEA2IPA1.5Pb2.5Br8.5 with different percentage of IPABr additive (0−60%). Inset shows the digital photographic images of the corresponding thin-films under the excitation of 365 nm. Copyright 2018, Nature Communications.23 (d) Formation energies of Q2DPe prepared from the BOCs PEABr, IPABr, and their mixture consisting of different n values. Inset shows the Q2DPe structure (n = 3) with PEA/IPA and digital photographic image of the operating PeLED. Copyright 2018, Nature Communications.23 (e) Schematic illustration of the possible arrangement of bulky organic and short-chain multi-cations within the Q2DPe. Copyright 2019, Royal Society of Chemistry.44 (f) Schematic representation of Q2DPe structures with different monovalent and divalent BOCs and their interaction with the consecutive inorganic octahedra layers. Copyright 2019, Wiley-VCH.42 (g) Schematic illustration of low-dimensional components engineering for achieving the narrow domain concentration to obtain the desired blue emission. Copyright 2019, Wiley-VCH.42 (h) Digital photographic images of: Q2DPe thin-films with different BOCs and their combination under the irradiation of 365 nm UV light (left), and working PeLED at applied bias voltage of 5V (right). Copyright 2020, Wiley-VCH.45 (i) Schematic illustration of the spin-coated Q2DPe thin-films with and without doping and the variation in their thin-film morphologies.   Copyright 2020, American Chemical Society.24 (j) Digital photographic PL images of perovskite thin-films doped with different cations under the excitation of 380 nm. Copyright 2020, American Chemical Society.24 (k) Multilayer PeLED device configuration with the pair of thin LiF layers at the perovskite interface. Copyright 2020, American Chemical Society.24 (l) Recorded EL spectra of blue PeLEDs operating under different bias voltages from 4V - 10V. Inset shows the digital photographic image of the operating PeLED. Copyright 2020, American Chemical Society.24 (m) Recorded PL spectra and PLQYs of Rb0.6Cs0.4PbBr3, pristine, and RbBr-rich Q2DPe of 〈n〉Rb0.6 = 3 thin-films. Inset shows the digital photographic PL image of RbBr-rich Q2DPe thin-films under UV irradiation. Copyright 2019, Nature Communications.46 (n) EQE vs current density curves of PeLEDs with pristine and RbBr-rich Q2DPe. Inset shows the digital photographic image of the working PeLED. Copyright 2019, Nature Communications.46

PeLEDs designed from BA2Csn−1Pbn(Br/Cl)3n+125 and PBA2Csn−1Pbn(Br/Cl)3n+130 Q2DPe have achieved maximum EQEs of 2.4%, 6.2% at 467 nm (blue), 487 nm (sky-blue) 25 and  0.52% at 490 nm30 respectively. These reports established that the stoichiometric ratio of the BOCs to the A-site cations in the precursor solution strongly influence the formation and phase distribution in the resultant Q2DPe thin-films. Increasing the ratio results in the formation of lower n phases and vice versa.

Numerous reports showed the presence of mixed (n = 1, 2, 3 ,4, 5….) phases in the resultant perovskite thin-films, i.e. the presence of 2D perovskites (n=1) as well as Q2DPe (n = 2, 3, 4..). 25-28, 32 Subsequently, efficient cascade charge transfer (exciton funneling) between the different n phases have been observed, i.e., the excitons in lower n phase efficiently transferred to higher n phase and resulted in a dramatic improvement in their PLQYs.28 Incorporation of excess amount of BOCs or increased ratio produces the Q2DPe with lower n phases favouring the deep blue emission through the strong quantum confinement effect.34, 40 Nevertheless, due to the low formation energies of higher n phases41 and the resultant Q2DPe thin-film contains the inhomogeneous phase distribution. The formation probability of lower phases  (n = 1, 2)  increases with excessive BOCs, lead to the incomplete charge transfer from n=1 phase to higher n phase42, due to their very large exciton binding energies (320 meV).43 As a result, the emission takes place from both the lower n as well as higher n phases distinctly, results in multiple emission peaks in the spectrum, lead to color impurity.42 Hence, it is essential to achieve the desired and intermediate n phase distribution by suppressing both the n=1 and n>4 phases in the resultant Q2DPe thin-films to achieve the narrow spectral pure blue emission.

Considering the significance of the intermediate (desired n) phase to achieve the narrow pure blue emission in the specific wavelength region; mixed dual BOC strategies have been developed.16, 23, 42, 44, 45   On augmentation Q2DPe were also prepared from the phenethylammonium bromide (PEABr) by combining with the additional cations, such as iso-propylammonium bromide (IPABr), ethylammonium bromide (EABr), n-propylammonium bromide (PABr) and butylammonium bromide (BABr) organic cations to regulate the phase and improve the emission properties.23 Systematic investigations revealed the combination of PEABr and IPABr resulted in high PLQYs from the (IPA/PEA)2(MA/Cs)n−1PbnBr3n+1 Q2DPe, and by increased IPA content also led to the blue-shifted emission spectra (Fig. 2c).23 Here, the IPA was utilized to slow down the crystallization of unwanted n = 1 phase by concentrating the monodispersed and desired phases (n = 2,3,4..), since IPA has a reduced van der Waals force, is believed to have suppressed the formation of n=1 phase. The small amount of PEA facilitates the formation of higher n phases. From the judicious precise regulation of the ratio of PEA/IPA cations, the desired and highly concentrated phases (n = 2, 3, 4) have been obtained. Formation energies of the Q2DPe with different n phases designed from individual and mixed BOCs (IPA, PEA) showed in Fig. 2d. The corresponding PeLEDs have produced a maximum EQE of 1.9% at 490 nm.23 The devices displayed the sky-blue emission, caused by the presence of broad and intermediate phase distribution (n= 2,3,4,5), led to the red-shifted emission spectra via exciton funneling.23

The Q2DPe have been prepared from the combination of bulky and short-chain ligands, such as dimethylammonium (DMA)+BA and DMA+PEA (Fig. 2e).44 BOCs (PEA, BA) capped the inorganic octahedra and hence limiting the formation of higher n phases within the Q2DPe thin-films.44 Accommodating the short-chain cations (DMA) with its relatively small positive charge and weak coordination suppressed the formation of n = 1 phase, and improved the charge injection efficiency and successive transportation within the Q2DPe thin-film of PeLEDs.44 Besides, additional short-chain cation DMA in combination with the BOCs (PEA, BA) of precise ratio regulates the desired n phase  as well as improves the charge injection and transportation properties of Q2DPe thin-films due to their better conductivity than the BOCs.44 The PeLEDs fabricated from the only Br halide-based  BA2DMA1.6Cs2Pb3Br11.6 and PEA2DMA1.2Cs2Pb3Br11.2 Q2DPe showed maximum EQEs of 2.4% at 490 nm (sky-blue) and 1.58%  at 499 nm (bluish-green) emissive region respectively.44

Typical organic spacers (BA, PEA) used in Q2DPe are inhomogeneous and unstable.42 Existence of weak interaction between these BOCs and inorganic octahedron of the Q2DPe framework lead to the growth of higher n phases from the smaller n phases during the thermal annealing and ageing of the thin-films for several hours in moisture, radiation and ambient conditions.42 Formation of higher n phases causes the reduced bandgap and results in red-shifted emission spectra, which hampers the pure blue emission of Q2DPe. Hence, developing the strategies to achieve the stable and narrow/desired n phase distribution in the Q2DPe thin-films are vitally important to produce the efficient, stable blue emitters and corresponding high-performance blue PeLEDs.

To achieve the narrow phase distribution and phase stability, diamine BOC (P-PDABr2 (1,4-Bis(aminomethyl)benzene bromide)) is used in combination with the monoamine BOC (PEABr) for the preparation of stable Q2DPe blue emitters (Fig. 2f).42 The P-PDA cation with double functional amido terminals on both the ends provides a strong binding force by directly connecting the two inorganic octahedra layers, and lead to the formation of stable lower n phases.42 In contrast to the monoamine cations, the P-PDA cations based Q2DPe exhibited the improved phase stability under external conditions such as temperature, moisture, and UV-irradiation, and produced the concentrated dominant n = 1, 3 phases.42 With the introduction of PEABr, the formation probability of n=2 phase enhanced considerably and dramatically suppressed the formation of n=1 phase.42 The precisely controlled ratio of P-PDABr2/PEABr (3:1) produced the desired and concentrated narrow n = 2, 3 phase distribution in the Q2DPe thin-films (Fig. 2g). Optimization of concentrated phase distribution promoted the exciton transfer from n=2 to n=3 phase. The charge carriers recombined radiatively and produced the strong blue emission solely from the n = 3 phase accompanied by improved PLQYs.42 The PeLEDs displayed a stable blue emission with a maximum EQE of 2.6% at 465 nm.42 Analogously, the combination of monoamine  - PEABr and diamine - N-(2-Bromoethyl)-1,3-propanediamine dihydrobromide (NPABr2) BOCs have been utilized to modulate and amplify the resultant emission and phase stability in the blue emissive region.45 The independent PEA and NPA cation based Q2DPe thin-films have exhibited the emission at 508 nm and 478 nm, respectively (Fig. 2h).45 The Q2DPe thin-films prepared from the combination of both the organic cations PEA+NPA produced the uniformly concentrated n = 2, 3 phases and showed the resultant emission at 482 nm.45 Corresponding PeLEDs designed from the only Br halide-based PEA2NPA1Cs2Pb3Br12 Q2DPe  exhibited a maximum EQE of 2.62% at 485 nm and showed the applied bias independent spectral stability.45 The presence of PEABr remarkably increased the PLQYs of Q2DPe thin-films, whereas the NPABr2 favoured the formation of narrowed phase distribution with blue-shifted emission spectra; consequently, the sky-blue emission with improved PLQY has been achieved.45

3.2 Passivation and doping

Low-temperature solution-processed perovskite thin-films possesses poor thin-film morphologies. It further increases the probability of high defect density at the grain boundaries and/or within the crystal structure, which is almost inevitable. Existence of defect density increases the nonradiative recombinations.15 Particularly, the defect density is prominent in wide-bandgap blue emitters, which reduces the overall PLQYs.15

To improve both the efficiency and stability of the Q2DPe, a multi-cation (Cs/FA/PEA/Rb/K) strategy has been developed, and resulted in the high-quality uniform thin-film morphology (Fig. 2i) and reduced defect density.24 Each cation used in this composition has played a consequential role in scoring the high-performance blue PeLED devices. The Rb-doping greatly modified the crystal growth orientation, improved the thin-film morphology, enhanced the PLQYs and blue-shifted the emission spectra due to increased bandgap caused by octahedral tilting.24 Inclusion of PEA/K cations played an important role in reducing the trap states density through the passivation of defect states at the grain boundary and surface thereby enhancing the PLQYs.24 Introduction of FA cations increased the current density in PeLEDs by improving the conductivity of the thin-films.24 Optimizing the content of the multi-cations resulted in reduced grain size, smooth and pin-hole free improved thin-film coverage with enhanced PLQYs(Fig. 2j).24 Besides, the multi-cation strategy pronouncedly reduced the large band offset from 1.28 eV for CsPb(Cl/Br)3 perovskite nanocrystals to 0.86 eV for (Cs/Rb/FA/PEA/K)Pb(Cl/Br)3 Q2DPe, which promoted the efficient hole charge injection due to reduced band offset.24 The PeLEDs fabricated with the insulator lithium fluoride (LiF)/Q2DPe/LiF structure (Fig. 2k) suppressed the luminescence quenching at the interface, showed the maximum EQE of  2.01% at 484 nm and improved device half-lifetime of 300 minutes under continuous operation.24 Propitiously, the PeLEDs withstand up to the operating voltages of  14 V implying the robust durability of the devices prepared from the multi-cation strategy.24 The recorded electroluminescence (EL) spectra at various bias voltages (4V – 10V) shown in fig. 2l. Nevertheless, the PeLED devices also showed a spectral shift of 8 nm under continuous operation, due to the ion migration and phase segregation under the applied electric fields.24

All inorganic A-site multi-cations (Rb-Cs) and exclusive Br halide-based alloyed Q2DPe blue emitters (PEA2(RbCs)Pb3Br10) have been developed to improve the spectral and ambient stability, PLQYs.46 The insertion of pure inorganic A-site cations (Cs, Rb) appreciably improved the spectral stability of the Q2DPe. Furthermore, the rubidium bromide (RbBr)-rich compositional engineering increased the overall PLQYs up to 82% (Fig. 2m) by reducing the deep trap states through the in-situ passivation, produced very smooth and uniform thin-films of root mean square (rms) roughness less than 1 nm.24, 46 Nonetheless, the excess cesium bromide (CsBr) induced the cation exchange, led to the red-shifted emission spectra.46 Systematic study and comprehensive investigation confirm that the excess RbBr effectively passivates the defect states and improves the radiative recombination efficiency.46 The unaltered stable PL spectra even after annealing for 4h at  100 C, indicated the excellent thermal stability of Cs/Rb-alloyed based Q2DPe.46 The RbBr-rich PeLEDs (PEA2(Rb0.6Cs0.4)Pb3Br10) displayed blue emission (Inset of Fig. 2n) with excellent spectral stability under various applied bias voltages and exhibited a maximum EQE  1.35% at  475 nm (Fig. 2n).46 Here, the halide migration – spectral instability in mixed halide (Cl/Br) blue PeLEDs completely circumvented by developing the efficient blue emitters from the only Br halide Q2DPe. Forbye, tailoring the RbBr content in the precursor solution demonstrated the ability to tune the emission color, and foster the efficient blue emitters and PeLEDs in the whole blue spectral region from 454 nm to 492 nm.46 However, the PeLEDs produced marginal efficiencies in the deep blue region (0.13, 1.11, 1.22, 1.35% in 460 nm - 480 nm) compared to the sky-blue region (1.48% at 490 nm).

To manipulate the advantage of Cl incorporation into the perovskites to achieve efficient deep blue emission and color tunability, it is pivotal to block the ion migration and phase segregation for obtaining the spectral stability and color purity. New strategies have been developed to prospect the ion migration activation energies (IMAEs) of the Q2DPe with different combinations of BOCs and additives. 35 The combination of the BOC phenethylammonium chloride (PEACl) and additive yttrium chloride (YCl3) in CsPbBr3 perovskites increased the IMAEs of the resultant perovskites from 0.26 (in CsPbBr2.4Cl0.6) to 0.75 eV (in PEACl:2%YCl3: CsPbBr3) (Fig. 3a), and also substantially increased the PLQYs (Fig. 3b).35 Addition of YCl3 lead to the accumulation of more yttrium (Y) ions on the thin-film surface or at grain boundaries. Y-rich region acts as a shell for the perovskite grains by imposing an energetically high potential barrier, and strongly confines the charge carriers within the perovskite grains (Fig. 3c).35  The confined charge carriers isolate from the nonradiative recombination channels and high-defect density states, which commonly exists at the grain boundaries and on the thin-film surfaces, thereby improving the overall PLQYs. The PEACl:CsPbBr3: YCl3 based PeLEDs showed improved spectral stability in mixed halide (Br/Cl) system, ascribing to the marked suppression of ion migration and phase segregation effects through the increased IMAEs.35 The PeLEDs with 2% YCl3 displayed the record EQE in the sky-blue emissive region of  11% at 485 nm (Fig. 3d). Increased content of YCl3 in the precursor solution resulted in the blue-shifted emission spectra. Further increasing the YCl3 to 5% and 10% reduced the PeLEDs EQE to 8.7% and 4.8% at 483 nm and 477 nm, respectively.35 The increased content led to the formation of YCl3 clusters and may hinder the growth of the perovskite grains. Interestingly, it is worth mentioning that the shape and stable peak position of the EL spectra upon continuously operating the blue PeLEDs over 120 minutes under various bias voltages, revealed the enhanced spectral stability in mixed halide Q2DPe through the increased IMAEs.35

Complementarily, Cl insertion−immobilization strategy through additional organic chlorides has been developed to produce the spectrally stable Q2DPe blue emitters and blue PeLEDs by blocking the ion migration and phase segregation effect through the increased IMAEs.47 The PEA2Cs1.6MA0.4Pb3Br10-xClx Q2DPe have been prepared from the compositional engineering and dynamically treating with the additional series of organic chloride components while preparing the thin-films via two-step spin-coating process.47 The organic component diphenylphosphinic chloride (DPPOCl)

Fig. 3 (a) Temperature-dependent conductivity measurements and corresponding fittings to calculate the IMAEs of mixed-halide perovskite thin-films of CsPbBr2.4Cl0.6, CsPbBr2.4Cl0.6 with 2% YCl3, and CsPbBr3:PEACl (1:1). Copyright 2019, Nature Communications.35 (b) Digital photographic PL images of perovskite thin-films with different YCl3 percentage under UV irradiation. Copyright 2019, Nature Communications.35 (c) Schematic illustration of the yttrium distribution within the CsPbBr3:PEACl:YCl3 thin-film and its effect on the bandgap modulation at the grain boundaries or surface. Copyright 2019, Nature Communications.35 (d) EQE vs current density curves of PeLEDs with different YCl3 percentages. Inset shows the digital photographic image of the operating PeLED. Copyright 2019, Nature Communications.35 (e) Schematic illustration of the possible mechanism of migration and immobilization of Cl- halide in Q2DPe prepared from the conventional chloride-doping and treated with DPPOCl respectively. Copyright 2020, American Chemical Society.47 (f) Q2DPe LED’s energy band diagram and corresponding energy level positions of Q2DPe thin-films treated with DPPOCl of 10, 20 and 30 mg/ml. Copyright 2020, American Chemical Society.47 (g) Schematic illustration of Q2DPe orientation within the thin-films through different thin-film processing conditions and possible charge transport mechanism. Copyright 2019, Wiley-VCH.48 (h) Schematic representation of the strategy to develop strong blue emissive Q2DPe by controlling the optimum phase through the interplay between the concentration of A-site and BOCs in the perovskite precursor solution. Inset shows the effect of antisolvent on phase distribution (right). Inset shows the digital photographic images of working PeLEDs with different compositions (left). Copyright 2020, American Chemical Society.40 (i) Schematic representation of the recombination zone modulation for efficient blue emission. Copyright 2019, Nature Communications.34 (j) Current density and luminance vs voltage characteristic curves of PeLEDs designed with different PEDOT: PSS layer thicknesses. The lines with dots and solid lines correspond to current density and luminance respectively. Copyright 2019, Nature Communications.34 (k) EQE vs current density curves of PeLEDs designed with different PEDOT: PSS layer thickness. Inset shows the digital photographic image of a working PeLED at constant applied voltage of 4.4V. Copyright 2019, Nature Communications.34

is sensitive to water traces, inserts the in-situ immobilized Cl halide in the crystal structure by saturating the halide vacancies through the hydrogen bonding (Fig. 3e), and resulted in the blue-shifted emission spectra through the bandgap enlargement (Fig. 3f).47 The Q2DPe treated with DPPOCl (30 mg/ml) exhibited an increased IMAE of 1.1 eV, is much higher than the conventional mixed halide (Cl/Br) Q2DPe (PEA2Cs1.6MA0.4Pb3Br7Cl3) of 0.7 eV.47 Corresponding DPPOCl treated blue PeLEDs displayed an EQE of 5.2% at 479 nm, showing no obvious EL spectral shift under operating conditions, and revealing an excellent spectral stability with an operating half-life time of  90 min at 100 cd/m2.47 In contrast, the blue PeLEDs designed from the conventional mixed halides (Br/Cl) exhibited a small EL spectral shift under applied bias voltages due to ion migration and phase segregation.47 Q2DPe treated with DPPOCl demonstrated the immobilization of halides, and suppression of the ion migration and phase segregation effect.47 These reports demonstrated the increased IMAEs as one of the effective methods to block the ion migration and phase segregation in mixed halide Q2DPe to obtain the spectral stability in the efficient deep blue PeLEDs.35, 47

3.3 Thin-film and interface engineering

Reduced NC or grain size eventually strengthened the charge carriers’ confinement and increased the radiative recombination and PLQYs.48 To consummate it, a two-step spin-coating process is widely employed.40, 48, 49 At first, the perovskite precursor solution was spin-coated onto the target substrates, followed by anti-solvent (chloroform, toluene, chlorobenzene with or without additives) dripping few seconds after the beginning of the initial spin-coating process. Dripping the antisolvent in the second step removes the excess DMSO/DMF solvent molecules and induces the immediate crystallization of perovskite NCs by reducing solvent evaporation time, known as nanocrystal pinning process (NCP).48 In Q2DPe, during the spin coating process, DMSO/DMF molecules form a stack on (001) plane of inorganic octahedra and evaporate slowly. The crystal growth occurs mostly in the in-plane direction.48 The directional growth of Q2DPe further hinders the charge injection and transportation, due to the presence of insulating BOCs between the consecutive inorganic octahedra layer frameworks. NCP process was applied by dripping the toluene solvent to promote the random orientation of the Q2DPe crystals, which facilitates the better connectivity between the inorganic octahedra layers, and improves the charge transportation.48 During the NCP process, the toluene molecules instantaneously replace the DMSO/DMF molecules, which initiates the rapid crystallization of perovskite layer crystals without any preferential growth direction, lead to the formation of randomly oriented crystals with reduced size and lower n phase  (Fig. 3g).48 The PeLEDs prepared from the Q2DPe (PEA)2MAn−1PbnBr3n+1 with random orientation showed an improved device efficiency.48

In conjunction, solvent engineering (DMSO/DMF) and dripping the toluene during the preparation of the Q2DPe thin-films, induces the faster nucleation and further reduces the formation of broad n distribution.40 The rationally engineered cation composition and crystallization kinetics lead to the formation of the desired intermediate n phases with a narrow distribution and produces the strong blue emission (Fig. 3h).40 The PeLEDs designed with only Br halide from this strategy showed the efficient performance in tandem with the spectral stability, covered the broad blue emissive region with EQEs of  2.34%, 4.34%, and 5.08% at 465 nm, 486 nm, and 493 nm, respectively.40 Over the above, the integration of BOCs into the perovskites eliminated the pin-holes within the thin-films, improved the thin-film morphologies and enhanced the PLQYs and PeLED efficiencies.24, 34

Recently, several reports have demonstrated the existence of vertically non-uniform distribution of perovskite layers in Q2DPe thin-film within the multi-layered PeLED device structures.34, 50, 51 The layer thickness in LEDs determines the position of the effective recombination zone within the perovskite emissive layer, which is imperative to achieve the efficient device performance (Fig. 3i).34 The thickness of poly(3,4-ethylenedioxythiophene): poly(styrene sulfonate) (PEDOT: PSS) layer is regulated from 15 nm to 60 nm to optimize the position of the effective recombination zone.34  Q2DPe prepared by precisely regulating the composition of PEABr from 0-120%, tailoring the Cl/Br halide ratio. The blue PeLEDs with an optimum thickness of PEDOT: PSS  30 nm displayed a turn-on voltage of 3.2 V, the maximum luminance of 3780 cd/m2 (Fig. 3j) and EQE of  5.7% at 480 nm (Fig. 3k).34 In contrast, the PeLEDs with the thickness of PEDOT: PSS 60 nm and 45 nm showed a decreased performance with the maximum EQEs of 2.6% and 3.6%.  Due to the higher PEDOT: PSS thickness, the charge carriers relatively take longer time to reach the recombination zone A, and subsequently injects into the perovskite crystals within the weak emissive zone B (Fig. 3i), which reduces the overall device efficiency.34 The effective recombination zone when modulated and gradually shifted from weak emissive zone B to strong emissive zone A by controlling the PEDOT: PSS thickness led to the improved device performance.34

A guest-host system is used in place of exclusive Q2DPe thin-film, as the active emissive layer for the fabrication of efficient blue PeLEDs.49 The active emissive layer is composed of quantum-confined perovskite nanoparticles embedded within Q2DPe phases with higher bandgaps achieved through the compositional engineering and followed by using the ethyl acetate as antisolvent (NCP process). 49 The resultant thin-films showed improved PLQYs (>60%) than the exclusive Q2DPe thin-films (38%). The increased concentration of phenylbutylammonium bromide (PBABr) in the precursor solution resulted in the blue-shifted emission spectra. The corresponding blue PeLEDs showed maximum EQEs of 9.5%, 6.3%, 4.8% and 4% at 483 nm, 478 nm, 476 nm and 474 nm.  This work establishes the improved PLQYs, efficient performances along with the spectral stability from the only  Br halide-based Q2DPe quantum-confined perovskite nanostructures blue PeLEDs.49

Along with the intrinsic issues, it is to be noted that the blue PeLEDs are suffering from poor charge injection and accumulation of charge carriers at the perovskite/hole transport layer (HTL) interface due to the deep VB position of wide-bandgap blue emitters, and interface losses.14, 16 To meticulously improve the charge injection efficiency and the radiative recombination within the perovskite layer, the LiF/perovskite/ LiF structure is used for the fabrication of blue PeLEDs.24 Additional LiF layer with controlled thickness at the Q2DPe interface is employed to induce and balance the charge injection into the Q2DPe crystals. The LiF layer at the indium tin oxide (ITO)/Q2DPe interface suppresses the luminescence quenching by reducing the energy band offset and interface losses.24 The blue PeLEDs showed the maximum EQE of 2.01% and revealed the improved device lifetime (300 min) compared to the reference device (20 min). The better device stability is mainly ascribed to high-quality uniform thin-film and the inhibition of the ion migration under the electric field by the pair of LiF layers at the Q2DPe interface.24

4. Challenges for quasi-2D perovskite blue emitters and blue PeLEDs

In the last two years, the Q2DPe blue emitters and blue PeLEDs have made considerable progress in their efficiencies. However, the mechanisms are yet to be explored; it requires much more efforts for the optimization and reproducibility of the methods to realise the efficient and stable performances of the blue PeLEDs. The large defect densities of wide-bandgap blue emitters act as nonradiative recombination centres leading to poor PLQYs.  The applied large electric fields induce the ion migration and phase segregation, which lead to the red-shift of the EL spectra and spectral instability.

Table 1.

Summary of performance parameters of recently reported Q2DPe-based blue and sky-blue LEDs.

| Perovskite Material | Device Structure | EL Peak (nm) | Lmax (Cd/m2) | CE (Cd/A) | EQE (%) | Vt (V) | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| (PEA)2PbBr4 | ITO/PEDOT: PSS/2D perovskite/TPBi/Ca/Al | 410 | -- | -- | 0.04 | 2.5 | 31 |
| OLA2MAn−1PbnBr3n+1 | ITO/PEDOT: PSS/PVK/Q2DPe/TPBi/LiF/Al | 456 | 2 | 0.0027 | 0.0046 | 3.4 | 52 |
| BA2MA2Pb3Br7Cl3 | ITO/PEDOT: PSS/Poly -TPD /Q2DPe/TPBi/LiF/Al | 468 | 21 | 0.006 | 0.01 | 5.2 | 32 |
| POEA2MAn−1PbnBr3n+1 | ITO/PEDOT: PSS/Q2DPe/TPBi/Ba/Al | 480 462 | 19.3 1.26 | 2.1 0.07 | 1.1 0.06 | 3.6 7 | 38 |
| EA2(MA)n−1PbnBr3n+1 | ITO/PEDOT: PSS/Q2DPe/TmPyPB/CsF/Al | 485 | 200 | -- | 2.6 | 3.4 | 39 |
| BA2Csn−1Pbn(Br/Cl)3n+1 | ITO/PEDOT: PSS/Q2DPe/TPBi/Al | 467 487 | 962 3340 | 1 1 | 2.4 6.2 | 5 4.5 | 25 |
| PBA2Csn−1Pbn(Br/Cl)3n+1 | ITO/NiOx/LiF/Q2DPe/TPBi/LiF//Al | 490 481 473 | 1446 509 217 | -- -- -- | 0.52 0.25 0.16 | -- -- -- | 30 |
| (IPA:PEA)2(MA:Cs)n−1PbnBr3n+1 | ITO/PEDOT: PSS/Q2DPe/TPBI/LiF/Al | 490 | 2480 | 2.8 | 1.9 | 5 | 23 |
| BA2DMA1.6Cs2Pb3Br11.6 | ITO/PEDOT: PSS or NiOx/Q2DPe/TPBI/LiF/Al | 490 | 2825 | 3.67 | 2.4 | 3.3 | 44 |
| PEA2DMA1.2Cs2Pb3Br11.2 | ITO/PEDOT: PSS or NiOx/Q2DPe/TPBI/LiF/Al | 499 | 7760 | 3.18 | 1.58 | 4.4 | 44 |
| P-PDA,PEACsn-1Pbn Br3n+1 | ITO/PVK/PFI/Q2DPe/3TPYMB/Liq/Al | 465 | 211 | 1.3 | 2.6 | -- | 42 |
| (PEA:NPA)Csn−1PbnBr3n+1 | ITO/poly(N-vinylcarbazole)/ PVK/Q2DPe/PO-T2T/Liq/Al | 485 | 1200 | -- | 2.62 | 2.6 | 45 |
| (Cs/Rb/FA/PEA/K)Pb(Cl/Br)3 | ITO//LiF/Q2DPe/LiF/Bphen/LiF/Al | 484 | 4015 | 2.11 | 2.01 | -- | 24 |
| PEA2(Rb0.6Cs0.4)Pb3Br10 | ITO/PEDOT: PSS/Q2DPe/TmPyPB/LiF/Al | 475 | 100.6 | 1 | 1.35 | 3 | 46 |
| CsPbBr3:PEACl:YCl3 | ITO/PEDOT: PSS/PVK/Q2DPe/TPBi/LiF/Al | 485 | 9040 | -- | 11 | 3 | 35 |
| (PBABr):(Cs/FA/MA)Br:PbBr2 | ITO/PEDOT: PSS/Q2DPe/POT2T/LiF/Al | 465 487 493 | 144.9 643.8 1151 | -- -- -- | 2.34 4.34 5.08 | 2.8 2.9 2.7 | 40 |
| PEA2Csn−1Pbn(Br/Cl)3n+1 | ITO/PEDOT: PSS/Q2DPe/TPBi/LiF/Al | 480 | 3740 | 6.1 | 5.7 | 3.2 | 34 |
| PBA2(FACs)n−1PbnBr3n+1 | ITO/NiOx/TFB/PVK/Q2DPe/TPBi/LiF/Al | 483 478 476 474 | 700 -- -- -- | 12 -- -- -- | 9.5 6.3 4.8 4 | 3.3 3.4 3.3 3.3 | 49 |
| PEA2Cs1.6MA0.4Pb3Br10 treated with DPPOCl | ITO/ PEDOT:PSS:PFI/Q2DPes/ TPBi/ LiF/ Al | 479 489 | 468 5141 | -- -- | 5.2 1.3 | -- -- | 47 |

The non-uniform distribution of the n (phase impurity) within the Q2DPe thin-film lead to the broad emission and red-shift of the emission spectra. Deep VB position of the perovskite blue emitters cause the inefficient charge injection and accumulation at the interface. Hence, the blue PeLEDs are experiencing low EQEs and faster degradation. Therefore, in this section, we shed light on the challenges that need to be addressed to obtain the efficient Q2DPe blue LEDs.

4.1 High defect densities and low PLQYs

The wide-bandgap perovskite blue emitters have been suffering from low PLQYs due to the formation of interband states that originate from the presence of defects on the thin-film surface or point defects exists within the crystal structure. Interband states acting as nonradiative recombination centres, reduces the overall PLQYs.14-16, 33 Another occurrence is due to the partial radiative recombination from the interband states that may result in the red-shift of the emission spectra or multi-peak emission hinders the color purity. Low PLQYs contributes to one of the major difficulties for the realization of high-performance blue PeLEDs. Hence, designing the strategies to enhance PLQYs are crucial for the development of efficient Q2DPe blue PeLEDs.

4.2 Phase impurity and orientation

The Q2DPe have been prepared from judicious loading of BOCs and A-site cations, where their ratio strongly influences the formation and distribution of n phases .34, 40 Desired n = 2, 3 phases are highly suitable for strong deep blue emission. Despite that, due to the low formation energies of the higher n phases causes the inhomogeneous phase distribution.41 The broad n phase distribution (n = 1,2,3,4 5..) with the dominant n=1, 2 phases lead to the incomplete charge transfer, resulting in the multipeak emission and color impurity.42 The presence of higher n phases lead to the exciton funneling from lower n to higher n phases, results in the red-shift of the emission spectra and produces the cyan, green emission. These factors hamper the desired deep blue emission.

Various reports documented the different growth mechanisms and layer orientation despite using similar preparation methods. Hence, it’s necessary to conduct focused and detailed studies for profound understanding of the exact underlying mechanism of how the solvent processing conditions can impact the crystallization, layer growth and orientation. Subsequently, it is also essential to discern the crystallization dynamics for the development and optimization of the strategies to achieve the phase purity (constant n) and their orientation for high-performance deep blue PeLEDs.

4.3 Ion migration and phase segregation – spectral instability

The blue PeLEDs have been suffering from severe spectral instability. It is the most substantial challenge to be addressed to achieve the stable efficient performance. Mixed halide composition (Cl/Br) is one of the practical approaches to precisely tune the emission in the blue emissive region. Rationally increasing the Cl halide content in the composition blue-shifts the emission spectra. However, the only Cl halide-based efficient blue emitters are unfeasible to achieve because of the very low solubility of PbCl2 in common solvents. Several reports have shown the degradation of color purity and red-shifted emission spectra in mixed halide perovskite blue emitters under the applied electric fields due to the ion migration and phase segregation within the crystal structure.30 Furthermore, the organic A-site cations (MA, FA) are highly sensitive to the external parameters, such as temperature, moisture, oxygen, and humidity. In contrary, inorganic A-site cations (Cs, Rb) are considered to be relatively stable and can improve the spectral stability. Hence, it is essential to develop the strategies to completely block the ion migration and phase segregation effects for the development of spectrally stable, efficient blue PeLEDs.

4.4 Inefficient charge injection and interface losses

The wide-bandgap blue emitters have a lower VB and higher CB positions, resulting in the large band offsets between the perovskite emissive layer and charge transport layers (CTLs). Due to the energy level mismatch, especially from the conventional HTLs with inappropriate VB position, holes experience a high energy potential barrier and lead to the poor charge injection into the Q2DPe emissive layer. The weak charge injection results in high turn-on voltages, thereby reducing the device efficiency. Besides, imbalanced charge injection into the emissive perovskites from both the ETL and HTL leads to the accumulation of charge carriers at the interface, and results in the faster degradation of the blue PeLEDs. The presence of insulating BOCs (low conductivity) completely isolates the consecutive inorganic octahedra layers within the Q2DPe thin-film and increases the resistivity of the devices.  It further hinders the out-of-plane or adjacent layer charge transportation within the PeLEDs, thereby limiting the overall device performance. Moreover, the presence of surface trap states at the Q2DPe layer/CTLs interface acts as nonradiative recombination centres, and presence of pin-holes within the Q2DPe thin-film acts as leakage current channels and reduces the overall device efficiency. Fig. 4a illustrates the schematic representation of the plausible energy level band diagram of the LED device structure with Q2DPe blue emitters and conventional HTLs/ETLs.

4.5 Device degradation

It is established that the operational stability and lifetime of the blue PeLEDs are being influenced by the intrinsic stability of perovskite blue emitters as well as CTLs, and importantly the energy-band-alignment with the CTLs/interfaces. Most of the Q2DPe blue emitters have been prepared by regulating the mixed halide (Cl/Br) composition, in which the Cl¯ vacancies relatively creates deeper trap states than the Br¯ or I¯ within the energy bandgap.19 These states irrevocably trap the charge carriers, suppress the radiative recombination, catalyze the device performance degradation through the ion migration, and make the perovskite more vulnerable to external atmospheric and operational conditions.19 Hence, the inhibition of Cl¯ vacancies is believed to be a prerequisite for achieving the stability and improved lifetime of blue PeLEDs. Notably, the organic CTL materials have widely been employed for the fabrication of blue PeLEDs. The intrinsic instability of the CTLs

Fig.4 Schematic illustration of strategies to improve the performance of Q2DPe blue LEDs: (a) Energy levels of conventional hole-transport layer (HTL), electron-transport layer (ETL) materials available, and, group of blue and sky-blue emissive Q2DPe. (b) Passivation of surface defect states, and, blocking the ion migration and phase segregation to improve the emission properties and spectral stability of Q2DPe and blue PeLEDs performance. (c) Achieving the phase purity (constant n) for spectral purity and layer orientation for effective charge injection and transportation. (d) Designing the efficient multilayer LED device architectures through band-alignment optimization by reducing the large band offsets via interface engineering and designing new HTLs having deep VB. (e) Light out-coupling strategies for improving the PeLEDs EQE as marked in the figure (three panels).

also influence the device stability. Limited availability of stable CTLs turn out to be more challenging to fabricate the stable blue PeLEDs with increased lifetime. Moreover, the large band offset at the perovskite/HTL interface, where the charge carriers experience energetically high-potential barrier, causing the imbalanced charge injection and accumulation of charge carriers at the interface further leading to the faster degradation of the blue PeLEDs. Therefore, minimising the band offsets can also effectively enhance the device stability and increases the device lifetime.

5. Future directions and strategies for further improvements

For future directions and further improvements in blue PeLEDs, still more efforts are needed to design and optimize the new strategies. High-performance blue PeLEDs can be achieved through: (i) improving the PLQYs, (ii) obtaining the phase purity, better interconnectivity and conductivity, (iii) spectral stability and color purity in mixed halide systems, (iv) improving and balancing the charge injection efficiency and reducing the interface losses, (v) enhancing the ambient and thermal stability, and (vi) effective light out-coupling strategies.

Reducing the high defect densities and surface trap states through the effective passivation, doping and compositional engineering (Fig. 4b) through the additives significantly enhance the PLQYs of Q2DPe blue emitters. Also, preparation of the thin-films through the hot-casting considerably reduce the defect densities. Harvesting the triplet excitons along with the singlet excitons significantly increase the PLQYs to near unity.53 The Q2DPe designed from the BOCs with high triplet energy states reduce the triplet quenching losses and improves the PLQYs.

The Q2DPe with n = 2, 3 phases are highly suitable for strong deep blue emission. Need to optimize the crystallization process through the compositional engineering of multiple BOCs/A-site cations and their thin-film processing conditions to achieve the phase purity (Fig. 4c) for stable blue emission. Doping and alloyed A-site cation composition also be an effective way to influence the rate of crystallization process through the modulation of crystallization dynamics which produces the concentrated and desired phase distribution, and uniform full coverage thin-film morphologies. In addition, the Q2DPe needs to be prepared from the BOCs of high binding energies, which forms a strong interaction with the inorganic octahedra of the perovskite framework that reduces the Ostwald ripening and enhance the phase stability under harsh external conditions.

Developing the Q2DPe with enhanced IMAEs through the proper selection of BOCs, additives, compositional engineering and other strategies will improve the spectral stability by blocking the ion migration and phase segregation (Fig. 4b) in mixed halide Q2DPe blue emitters. Pure inorganic A-site cations can also enhance the spectral stability. Moreover, designing the reduced-dimensional perovskites through the quantum confinement in pristine Br halide-based Q2DPe eliminates the chances of halide segregation, and lead to the spectral stability under applied electric fields.

Establishing the better conductivity between the consecutive inorganic octahedra layers within the thin-film through short-chain ligands in combination with the stable BOCs improves the out-of-plane and adjacent layer charge transport properties.  Preferential vertical growth/orientation (Fig. 4c) on the substrate via solvent engineering (DMSO: DMF) significantly enhances the charge injection efficiency between the Q2DPe-CTLs, and induce the better charge transportation within the adjacent inorganic octahedra layers of Q2DPe thin-film, and further improves the overall device efficiency.

Energy landscape through the incorporation of the intermediate layers with the appropriate thickness ( ex. poly(methyl methacrylate) (PMMA), poly(ethylene oxide) (PEO), polyvinylpyrrolidone (PVP), and LIF)  at the perovskite/CTLs interface (Fig. 4d)  reduces the band offsets, balance the charge injection into the perovskite emissive layer and suppress the emission quenching at the interface. Alternatively, designing the new HTLs with suitable deep VB is expected to be an effective way to reduce the large band offsets (Fig. 4d) and improve the hole charge injection efficiency. The modulation of the crystallization dynamics of perovskite blue emitters strongly depend on the new HTL surfaces upon which it is deposited. Importantly, the crystallization kinetics with improved morphological cleavage, to produce high quality, pin-hole flatter films besides maintaining the electron-hole balance are paramount for better device performances. Empathetically, the choice of new HTLs with deep valence band (VB) to balance the charge injection efficiency without compromising the crystallization dynamics of perovskites is at infancy. As future directions, more efforts are still needed for the comprehensive understanding to devise high-performance blue PeLEDs. Hence, designing the new HTLs are desired to promote the better hole injection and achieve the stable, high-performance blue PeLEDs. In addition, the optical down-conversion through self-absorption leads to the emissive losses and should be avoided by employing the CTLs that are transparent to the blue.

A possible approach to enhance the ambient, thermal and operational stability is, designing the perovskites from the compositional engineering through inorganic A-site cations in combination with stable monoamine and diamine BOCs possessing high binding energies. Developing strategies to enhance the perovskites ambient stability is paramount for practical solid-state lighting and display applications.

The fabrication of PeLEDs with the incorporation of additional nanophotonic engineering layer such as photonic crystals, nanodome array, nanowire array, microlens array, bioinspired moth-eye nanostructures, half-ball lens, low-index grids significantly enhance the extraction of light and out-coupling efficiency (Fig. 4e), which further improve the PeLEDs’ EQE.54 The presence of various nanostructures at the interface between the glass substrate/perovskite layer act as light couplers and optical antennas. These nanostructures scatter and guide the light out effectively by relatively suppressing the light losses arising from the mismatched refractive indices (n) between the perovskite layer and the glass substrate (waveguide mode). Moreover, reducing the out-coupling losses that result from total internal reﬂection at the glass substrate/air interface (substrate mode) through photonic crystals, glass surface patterning, and surface texturing is also an attractive approach to enhance the EQE of PeLEDs.54 Overall, the efficient light out-coupling strategy is henceforth believed to be a potential direction for achieving the high EQE blue PeLEDs, since internal quantum efficiencies (IQEs) have reached high values (over 80%).

6. Conclusions

To conclude, Q2DPe are believed to be the best alternative candidates to their 3D bulk and NC counterparts for the realization of efficient and stable blue PeLEDs, yet underexploited. We have summarized the recent attempts and progress on Q2DPe blue LEDs based on their compositional engineering, passivation, doping, thin-film and interface engineering. In addition, we have discussed the possible future strategies and directions for further development of Q2De blue emitters and blue PeLEDs. Intensive research on Q2DPe blue emitters allows the more profound understanding of the involute mechanisms and strategic optimizations in achieving the high PLQYs by reducing the defect densities, regulating the phase purity for narrow emission, complex environment in mixed halide perovskites under applied electric fields for spectral stability and regulating the layer orientation. In augmentation, interface engineering, reducing the band offsets and discovery of suitable new HTLs with deep VB will significantly improve the performance and stability of blue PeLEDs. Undoubtedly, the in-depth study of the combination of materials processing, compositional engineering, appropriate large and short-chain organic cations, suitable deep VB HTLs, energy band-aligned device architectures and enhanced ambient stability will pave for the further development of efficient and stable blue PeLEDs.

Conflicts of interest

There are no conflicts to declare.

Acknowledgements

GSK, RRS acknowledges the Council of Scientific and Industrial Research (CSIR), BM acknowledges the Department of Science and Technology (DST), Indo-Korea grant (No. INT/Korea/P-40) and (EEQ/2017/000304), Science & Engineering Research Board (SERB).

References

1.	A. Kojima, K. Teshima, Y. Shirai and T. Miyasaka, J. Am. Chem. Soc., 2009, 131, 6050-6051.

2.	M. M. Tavakoli, M. Saliba, P. Yadav, P. Holzhey, A. Hagfeldt, S. M. Zakeeruddin and M. Grätzel, Adv. Energy Mater., 2019, 9, 1802646.

3.	Z. Wang, Q. Lin, F. P. Chmiel, N. Sakai, L. M. Herz and H. J. Snaith, Nat. Energy, 2017, 2, 17135.

4.	T. Chiba, Y. Hayashi, H. Ebe, K. Hoshi, J. Sato, S. Sato, Y.-J. Pu, S. Ohisa and J. Kido, Nat. Photonics, 2018, 12, 681-687.

5.	Z.-K. Tan, R. S. Moghaddam, M. L. Lai, P. Docampo, R. Higler, F. Deschler, M. Price, A. Sadhanala, L. M. Pazos, D. Credgington, F. Hanusch, T. Bein, H. J. Snaith and R. H. Friend, Nat. Nanotechnol., 2014, 9, 687-692.

6.	B. Zhao, S. Bai, V. Kim, R. Lamboll, R. Shivanna, F. Auras, J. M. Richter, L. Yang, L. Dai, M. Alsari, X.-J. She, L. Liang, J. Zhang, S. Lilliu, P. Gao, H. J. Snaith, J. Wang, N. C. Greenham, R. H. Friend and D. Di, Nat. Photonics, 2018, 12, 783-789.

7.	K. Lin, J. Xing, L. N. Quan, F. P. G. de Arquer, X. Gong, J. Lu, L. Xie, W. Zhao, D. Zhang, C. Yan, W. Li, X. Liu, Y. Lu, J. Kirman, E. H. Sargent, Q. Xiong and Z. Wei, Nature, 2018, 562, 245-248.

8.	C. S. Ponseca, T. J. Savenije, M. Abdellah, K. Zheng, A. Yartsev, T. Pascher, T. Harlang, P. Chabera, T. Pullerits, A. Stepanov, J.-P. Wolf and V. Sundström, J. Am. Chem. Soc., 2014, 136, 5189-5192.

9.	L. Protesescu, S. Yakunin, M. I. Bodnarchuk, F. Krieg, R. Caputo, C. H. Hendon, R. X. Yang, A. Walsh and M. V. Kovalenko, Nano Lett., 2015, 15, 3692-3696.

10.	J. Song, J. Li, X. Li, L. Xu, Y. Dong and H. Zeng, Adv. Mater., 2015, 27, 7162-7167.

11.	F. Mathies, H. Eggers, B. S. Richards, G. Hernandez-Sosa, U. Lemmer and U. W. Paetzold, ACS Appl. Energy Mater., 2018, 1, 1834-1839.

12.	F. Hermerschmidt, F. Mathies, V. R. F. Schröder, C. Rehermann, N. Z. Morales, E. L. Unger and E. J. W. List-Kratochvil, Mater. Horiz., 2020, DOI: 10.1039/D0MH00512F.

13.	F. Mathies, E. J. W. List-Kratochvil and E. L. Unger, Energy Technol., 2020, 8, 1900991.

14.	N. K. Kumawat, X.-K. Liu, D. Kabra and F. Gao, Nanoscale, 2019, 11, 2109-2120.

15.	C. H. A. Li, Z. Zhou, P. Vashishtha and J. E. Halpert, Chem. Mater., 2019, 31, 6003-6032.

16.	M. Luo, Y. Jiang, T. He and M. Yuan, APL Mater., 2020, 8, 040907.

17.	S. Hou, M. K. Gangishetty, Q. Quan and D. N. Congreve, Joule, 2018, 2, 2421-2433.

18.	G. Pan, X. Bai, W. Xu, X. Chen, Y. Zhai, J. Zhu, H. Shao, N. Ding, L. Xu, B. Dong, Y. Mao and H. Song, ACS Appl. Mater. Interfaces, 2020, 12, 14195-14202.

19.	X. Zheng, S. Yuan, J. Liu, J. Yin, F. Yuan, W.-S. Shen, K. Yao, M. Wei, C. Zhou, K. Song, B.-B. Zhang, Y. Lin, M. N. Hedhili, N. Wehbe, Y. Han, H.-T. Sun, Z.-H. Lu, T. D. Anthopoulos, O. F. Mohammed, E. H. Sargent, L.-S. Liao and O. M. Bakr, ACS Energy Lett., 2020, 5, 793-798.

20.	L. Mao, C. C. Stoumpos and M. G. Kanatzidis, J. Am. Chem. Soc., 2019, 141, 1171-1190.

21.	S. Ahmad, P. Fu, S. Yu, Q. Yang, X. Liu, X. Wang, X. Wang, X. Guo and C. Li, Joule, 2019, 3, 794-806.

22.	K. Zheng and T. Pullerits, J. Phys. Chem. Lett., 2019, 10, 5881-5885.

23.	J. Xing, Y. Zhao, M. Askerka, L. N. Quan, X. Gong, W. Zhao, J. Zhao, H. Tan, G. Long, L. Gao, Z. Yang, O. Voznyy, J. Tang, Z.-H. Lu, Q. Xiong and E. H. Sargent, Nat. Commun., 2018, 9, 3541.

24.	F. Yuan, C. Ran, L. Zhang, H. Dong, B. Jiao, X. Hou, J. Li and Z. Wu, ACS Energy Lett., 2020, 5, 1062-1069.

25.	P. Vashishtha, M. Ng, S. B. Shivarudraiah and J. E. Halpert, Chem. Mater., 2019, 31, 83-89.

26.	L. Lei, D. Seyitliyev, S. Stuard, J. Mendes, Q. Dong, X. Fu, Y.-A. Chen, S. He, X. Yi, L. Zhu, C.-H. Chang, H. Ade, K. Gundogdu and F. So, Adv. Mater., 2020, 32, 1906571.

27.	H. Kim, K. A. Huynh, S. Y. Kim, Q. V. Le and H. W. Jang, Phys. Status Solidi RRL, 2020, 14, 1900435.

28.	P. Chen, Y. Meng, M. Ahmadi, Q. Peng, C. Gao, L. Xu, M. Shao, Z. Xiong and B. Hu, Nano Energy, 2018, 50, 615-622.

29.	L. Gao, F. Zhang, C. Xiao, X. Chen, B. W. Larson, J. J. Berry and K. Zhu, Adv. Funct. Mater., 2019, 29, 1901652.

30.	K.-H. Wang, Y. Peng, J. Ge, S. Jiang, B.-S. Zhu, J. Yao, Y.-C. Yin, J.-N. Yang, Q. Zhang and H.-B. Yao, ACS Photonics, 2019, 6, 667-676.

31.	D. Liang, Y. Peng, Y. Fu, M. J. Shearer, J. Zhang, J. Zhai, Y. Zhang, R. J. Hamers, T. L. Andrew and S. Jin, ACS Nano, 2016, 10, 6897-6904.

32.	H. Hu, T. Salim, B. Chen and Y. M. Lam, Sci. Rep., 2016, 6, 33546.

33.	R. Liu and K. Xu, Instrum. Sci. Technol., 2020, 48, 616-636.

34.	Z. Li, Z. Chen, Y. Yang, Q. Xue, H.-L. Yip and Y. Cao, Nat. Commun., 2019, 10, 1027.

35.	Q. Wang, X. Wang, Z. Yang, N. Zhou, Y. Deng, J. Zhao, X. Xiao, P. Rudd, A. Moran, Y. Yan and J. Huang, Nat. Commun., 2019, 10, 5633.

36.	Y. Zou, H. Xu, S. Li, T. Song, L. Kuai, S. Bai, F. Gao and B. Sun, ACS Photonics, 2019, 6, 1728-1735.

37.	C. Zhang, Q. Wan, B. Wang, W. Zheng, M. Liu, Q. Zhang, L. Kong and L. Li, J. Phys. Chem. C, 2019, 123, 26161-26169.

38.	Z. Chen, C. Zhang, X.-F. Jiang, M. Liu, R. Xia, T. Shi, D. Chen, Q. Xue, Y.-J. Zhao, S. Su, H.-L. Yip and Y. Cao, Adv. Mater., 2017, 29, 1603157.

39.	Q. Wang, J. Ren, X.-F. Peng, X.-X. Ji and X.-H. Yang, ACS Appl. Mater. Interfaces, 2017, 9, 29901-29906.

40.	N. Yantara, N. F. Jamaludin, B. Febriansyah, D. Giovanni, A. Bruno, C. Soci, T. C. Sum, S. Mhaisalkar and N. Mathews, ACS Energy Lett., 2020, 5, 1593-1600.

41.	L. N. Quan, M. Yuan, R. Comin, O. Voznyy, E. M. Beauregard, S. Hoogland, A. Buin, A. R. Kirmani, K. Zhao, A. Amassian, D. H. Kim and E. H. Sargent, J. Am. Chem. Soc., 2016, 138, 2649-2655.

42.	S. Yuan, Z.-K. Wang, L.-X. Xiao, C.-F. Zhang, S.-Y. Yang, B.-B. Chen, H.-T. Ge, Q.-S. Tian, Y. Jin and L.-S. Liao, Adv. Mater., 2019, 31, 1904319.

43.	X. Gao, X. Zhang, W. Yin, H. Wang, Y. Hu, Q. Zhang, Z. Shi, V. L. Colvin, W. W. Yu and Y. Zhang, Adv. Sci., 2019, 6, 1900941.

44.	S. Zeng, S. Shi, S. Wang and Y. Xiao, J. Mater. Chem. C, 2020, 8, 1319-1325.

45.	Y. Jin, Z.-K. Wang, S. Yuan, Q. Wang, C. Qin, K.-L. Wang, C. Dong, M. Li, Y. Liu and L.-S. Liao, Adv. Funct. Mater., 2020, 30, 1908339.

46.	Y. Jiang, C. Qin, M. Cui, T. He, K. Liu, Y. Huang, M. Luo, L. Zhang, H. Xu, S. Li, J. Wei, Z. Liu, H. Wang, G.-H. Kim, M. Yuan and J. Chen, Nat. Commun., 2019, 10, 1868.

47.	D. Ma, P. Todorović, S. Meshkat, M. I. Saidaminov, Y.-K. Wang, B. Chen, P. Li, B. Scheffel, R. Quintero-Bermudez, J. Z. Fan, Y. Dong, B. Sun, C. Xu, C. Zhou, Y. Hou, X. Li, Y. Kang, O. Voznyy, Z.-H. Lu, D. Ban and E. H. Sargent, J. Am. Chem. Soc., 2020, 142, 5126-5134.

48.	H.-D. Lee, H. Kim, H. Cho, W. Cha, Y. Hong, Y.-H. Kim, A. Sadhanala, V. Venugopalan, J. S. Kim, J. W. Choi, C.-L. Lee, D. Kim, H. Yang, R. H. Friend and T.-W. Lee, Adv. Funct. Mater., 2019, 29, 1901225.

49.	Y. Liu, J. Cui, K. Du, H. Tian, Z. He, Q. Zhou, Z. Yang, Y. Deng, D. Chen, X. Zuo, Y. Ren, L. Wang, H. Zhu, B. Zhao, D. Di, J. Wang, R. H. Friend and Y. Jin, Nat. Photonics, 2019, 13, 760-764.

50.	Y. Shang, G. Li, W. Liu and Z. Ning, Adv. Funct. Mater., 2018, 28, 1801193.

51.	N. Wang, L. Cheng, R. Ge, S. Zhang, Y. Miao, W. Zou, C. Yi, Y. Sun, Y. Cao, R. Yang, Y. Wei, Q. Guo, Y. Ke, M. Yu, Y. Jin, Y. Liu, Q. Ding, D. Di, L. Yang, G. Xing, H. Tian, C. Jin, F. Gao, R. H. Friend, J. Wang and W. Huang, Nat. Photonics, 2016, 10, 699-704.

52.	S. Kumar, J. Jagielski, S. Yakunin, P. Rice, Y.-C. Chiu, M. Wang, G. Nedelcu, Y. Kim, S. Lin, E. J. G. Santos, M. V. Kovalenko and C.-J. Shih, ACS Nano, 2016, 10, 9720-9729.

53.	C. Qin, T. Matsushima, W. J. Potscavage, A. S. D. Sandanayaka, M. R. Leyden, F. Bencheikh, K. Goushi, F. Mathevet, B. Heinrich, G. Yumoto, Y. Kanemitsu and C. Adachi, Nat. Photonics, 2020, 14, 70-75.

54.	Q. Zhang, D. Zhang, Y. Fu, S. Poddar, L. Shu, X. Mo,
and Z. Fan, Adv. Funct. Mater., 2020, 2002570. (In Press) DOI.org/10.1002/adfm.202002570.